## Slide 1
Solid state chemistry

## Slide 3
Sustainability, Transformation and Progress
Good quality of the air
Clean water
Natural and fresh food
Fire / agricolture

## Slide 4
Life Cycle Assessment

## Slide 5
Depletion
Once you eat the cake, you don't have it any more

## Slide 6
Depletion:
EROEI = Energy Delivered / Energy Required to Deliver that Energy

## Slide 7
Depletion:
As you eat the cake, it becomes less and less tasty

## Slide 8
Mining requires energy

## Slide 9
Mirny Mine, Russia
Incredible Open-Pit Mines

## Slide 10
The tremendous potential of deep-sea mud as a source of rare-earth elements
Scientific Reports volume 8, Article number: 5763 (2018)

## Slide 11
Ethical Cobalt extraction
Replacing noble metals with base metal

## Slide 12
Secondary lead recovery
Storage Batteries
Metal Fabrications
Other producion
Industrial Waste 20.000
Industrial Waste 42.000
Industrial Waste 38.000
Product 800.000
Product
Product
16.000
600
700.000
Postconsumer recycle
recycle
Industrial Waste 93.000
940.000
60.000
240.000
760.000
670.000
4.000
100.000
41.400
Primary Pb
Pb cycle 1993

## Slide 13: Platinum group recycling
Mining and refining
Metal fabrication
Metal production
Chemical conversion for catalyst and other uses
Automotive catalyst manufacture
Automotive catalytic converters
Chemical catalysts and chemicals
Petroleum catalysts
100%
waste
85%
143 tons
60%
40%
11%
4%
85%
97%
12%
88%
scrap
100%
of plant waste

## Slide 14: INTRODUCTION
Three States of Matter:
  Solids
  Liquids
  Gases
  Solids:
  The aggregates of atoms which preserve their volumes and shapes unless subjected to large external force are called solids”.
  There are two types of solids :
  Amorphous (non-crystalline) and
  Crystalline

## Slide 21: Difference Between Amorphous and Crystalline Solids
Amorphous
Amorphous solids (means without form) are the solids which lacks the regular arrangement of atoms or molecules and hence they have a short range order or no order in their structure
Do not have sharp melting point (because all bonds are not equally strong)
Isotropic (Physical properties are same in different directions)
Examples: glass, wax, plastics, etc.
Crystalline
A crystalline solid is the one in which there is a regular repeating pattern in the structure, or in other words, there is long-range order
Have sharp melting point (because all bond are equally strong)
Anisotropic (Physical properties are different in different directions)
Examples: diamond, table salt, ice, methanol, sodium chloride, etc.

## Slide 22: CRYSTAL LATTICES
A lattice is an infinite, regular array of points in space.
# In the definition it should be noticed that no mention is made of atoms or any physical objects, just points in space - no more, no less. Hence we treat the lattice as a mathematical abstraction. Therefore, it is clear that there is no lattice inside the crystal. Even if we look the crystal through a powerful microscope we will not be able to see the lattice points, but rather atoms or groups of atoms. The lattice provides the 'recipe' that determines how the atomic or molecular units are to be repeated throughout the space to make the crystal structure.

## Slide 23
Plane Lattice
Consider an array of points in such a way that the environment about any point is identical with the environment about any other point. Such an array of points in two dimensions is shown in Fig. and is called a plane lattice.
For constructing a two dimensional lattice, choose any two convenient axis such that the points lie at equal intervals a and b along these axis as shown in the Fig. There are generally 5 lattices in two dimensions: Oblique, Square, Hexagonal, Rectangular and Centered Rectangular lattice.

## Slide 24
Space Lattice
If this array of points is extended to three dimensions then the array of points is called space lattice. For constructing the space lattice the points are arranged at equal intervals c in the third direction also. There are 14 space lattices in total, called Bravais Lattice.
Thus a lattice may also be defined as a parallel net like arrangement of points such that the environment about any point is identical with the environment about any other point.

## Slide 25
Basis
A basis is defined as an assembly of atoms, ions or molecules identical in composition, arrangement and orientation.
Basis consists of the simplest arrangement of atoms which is repeated at every point in the lattice to build up the crystal structure.
The number of atoms in a basis may be one as in case of many metals and inert gases, but could be as large as 1000 in many structures.
In ionic crystals, a basis is composed of two distinct types of ions. For example, Na+ and Cl- in a NaCl crystal.

## Slide 26
When basis is attached identically to each lattice point, the actual crystal structure is formed as shown in the Fig.
The relation can be written as
Lattice + Basis = Crystal Structure

## Slide 32: UNIT CELL
A unit cell is a region of space which when repeated by primitive translation vectors fills all space. Thus a unit cell is defined as the smallest geometrical figure, the repetitions of which give the actual crystal structure.
The choice of the unit cell is not unique. It can be constructed in a number of ways, but the unit cell should be chosen in such a way that it conveys all the symmetry of a crystal lattice, by having shortest possible size, which makes the mathematical calculations easy.
Each atom or molecule in a unit cell is considered as a lattice point. The distance between the two atoms or ions of the same type is the ‘length of the unit cell’.

## Slide 33
In general, a unit cell may be defined as the smallest volume of a solid from which the entire crystal may be constructed by translational repetitions in 3-dimension and which represent fully all the characteristics of a particular crystal. In Fig. a three dimensional unit cell is shown by the shaded portion.

## Slide 34
For a three dimensional case, the unit cell is a parallelepiped formed by basic vectors a, b and c as concurrent edges and the angles ,  and , between (b, c), (c, a), and (a, b) respectively as explained in the following Figures.
Lattice parameters
a, b, c
a, b, c

## Slide 35
Primitive and Non - primitive unit cell
contain just one lattice point
contain more than one lattice point

## Slide 54
Type of unit cells
P Simple
I Body-centred
F Face-centred
C Base(side)-centred

## Slide 55: CRYSTAL SYSTEMS AND BRAVAIS LATTICES
Crystals of different substances have similar shapes and hence the crystals are classified into the so called crystal systems depending upon their axial ratio and the interfacial angles ,  and . In three-dimension, there are 7 crystal systems. Bravais showed that throughout the seven crystal systems there are fourteen unique lattice types possible. These are known as Bravais or space lattices.

## Slide 56
No. | Crystal class | Intercepts on Axes | Angles between Axes | Bravais space lattice
1 | Cubic | a  b  c |       900 | Simple, body-centred, face-centred
2 | Tetragonal | a  b  c |       900 | Simple, body-centred
3 | Orthorhombic | a  b  c |       900 | Simple, body-centred, face-centred, Base(side)-centred
4 | Trigonal | a  b  c |       900 | Simple
5 | Hexagonal | a  b  c |    900,   1200 | Simple
6 | Monoclinic | a  b  c |     900   | Simple, base-centred
7 | Triclinic | a  b  c |      | Simple

## Slide 67
No. | Crystal class | Intercepts on Axes | Angles between Axes | Bravais space lattice
1 | Cubic | a  b  c |       900 | Simple, body-centred, face-centred
2 | Tetragonal | a  b  c |       900 | Simple, body-centred
3 | Orthorhombic | a  b  c |       900 | Simple, body-centred, face-centred, Base(side)-centred
4 | Trigonal | a  b  c |       900 | Simple
5 | Hexagonal | a  b  c |    900,   1200 | Simple
6 | Monoclinic | a  b  c |     900   | Simple, base-centred
7 | Triclinic | a  b  c |      | Simple

## Slide 70: MILLER INDICES
The crystal structure may be regarded as made up of an aggregate of a set of parallel equidistant planes passing through at least one lattice point or a number of lattice points. These planes are known as Lattice Planes. For a given crystal, lattice planes can be chosen in different ways as shown in Fig.

## Slide 71
In order to designate a lattice plane, British mineralogist William H. Miller, in 1839, developed a method by using three numbers (h k l) which are known as Miller Indices.
Miller Indices are the three smallest possible integers, which have the same ratio as the reciprocals of intercepts of the plane concerned on the three axis.
# Miller indices are integer sets that were created to distinguish directions and planes in a lattice. They are used primarily in crystalline structures because they describe planes in relation to a larger lattice in relative terms, as opposed to absolute terms. An example of this is describing planes in a building, Miller indices would distinguish the floor from the walls, and north wall from west wall, however it would not distinguish the 4th floor from the 5th floor. This is useful in crystal lattices because the planes are the same in many directions(like floors in a tall building).

## Slide 73
Important points:
Miller indices define the orientation of the plane within the unit cell
If a set of planes is parallel to any of the axes, it would cut that axes at , hence the Miller index along that direction is 1/ = 0.
If a plane to be indexed has an intercept along the negative portion of a coordinate axis, a minus sign is placed over the corresponding index.
The Miller Index defines a set of planes parallel to one another (remember the unit cell is a subset of the “infinite” crystal), e.g., (002) planes are parallel to (001) planes, and so on.

## Slide 74: Let us take an example to find the Miller Indices of a given plane(see Fig.):
Intercepts: 2a 1b 1c
Dividing by unit translation vectors: 2a/a 1b/b 1c/c = 2 1 1
Taking the reciprocals: ½ 1/1 1/1
Reducing to whole numbers: 1 2 2
Miller indices: (122)

## Slide 81: INTERPLANER DISTANCE OR SPACING
Interplaner spacing is defined as the perpendicular distance dhkl between corresponding planes. It is also perpendicular distance from the origin to the set of parallel planes (see Fig.)

## Slide 82
For a cubic lattice, a = b = c, therefore, we get
d100 = a, d110 = a/2 and d111 = a/3.
Also, For a cubic lattice,

## Slide 83: Physical Parameters for Crystal Structure
(i) Number of Atoms per Unit Cell
Number of atoms per unit cell determines how closely the solid is packed and is given by
N = Nc/8 + Nf/2 + Ni
here Nc is the number of corner atoms, Nf the number of face centred atoms and Ni the number of body centred atoms(see Fig.).
For SC crystal : In a SC crystal, there are 8 atoms only, each at one corner. Each atom is shared by 8 unit cells. Therefore, we have
N = Nc/8 = 8/8 = 1
For BCC crystal :N = Nc/8 + Nf/2 + Ni = 8/8 + 0 + 1 = 2
For FCC crystal :N = Nc/8 + Nf/2 + Ni = 8/8 + 6/2 + 0 = 4

## Slide 84
(ii) Coordination Number (CN)
In a crystal, the number of nearest neighbours of the same type and at equal distances from the given atom is called coordination number.
For SC : The corner atoms are the nearest neighbours of each other. Here CN = 6 (see Fig.) which is a group of 8 unit cell and atom at the centre has six corner atoms as its nearest neighbours).

## Slide 85
For BCC : In this case all the corner atoms are at equal distances from the body centered atom.
Hence CN = 8.
For FCC : Here the nearest neighbours of any corner atom are the face centered atoms of the surrounding unit cells. Now for any corner atom there are 4 face centered atoms in each plane and there are three such planes. Therefore, CN = 12.

## Slide 86
(iii) Atomic Radius and Nearest Neighbour Distance (NND)
In a crystal the atoms are assumed to be spheres in contact. Now atomic radius is defined as half the distance between the nearest neighbours in a crystal of pure element, i.e., the distance between the centres of neighbouring atoms.
For SC : In a SC structure, corner atoms are the nearest neighbours and are in touch with each other. If the side of the unit cell is ‘a’ and ‘r’ be the radius , then
2r = a or r = a/2
Now Nearest Neighbour Distance(NND) is given by 2r
Therefore, NND = 2r = a

## Slide 87
For FCC : r = 2 a/4
NND = a/2

## Slide 88
For BCC : r = 3 a/4
NND = 3 a/2.

## Slide 89
(iv) Atomic Packing Fraction (or Factor) (APF)
It is defined as the ratio of the volume of the atoms occupying the unit cell to the volume of the unit cell. It is also called relative packing density.
APF = Volume occupied by the atoms in a unit cell / Volume of the unit cell.
SC Crystal : No. of atoms/unit cell = 1
Volume of one atom = 4/3 r3
Side of the unit cell = a = 2r
Volume of the unit cell = a3
APF = = = /6 = 0.52 = 52%.
BCC Crystal : No. of atoms/unit cell = 2
Volume of two atoms = 2x4/3 r3
Side of the unit cell = a = 4r/3
Volume of the unit cell = a3
APF = = = 3/8 = 0.68 = 68%.
FCC Crystal : No. of atoms/unit cell = 4
Volume of four atoms = 4x4/3 r3
Side of the unit cell = a = 4r/2
Volume of the unit cell = a3
APF = = = 2/6 = 0.74 = 74%.

## Slide 90
Closed Packed Structures
In a closed packed structure the constituent atoms are so arranged as to occupy minimum possible volume, reaching the maximum density.
Planar closed packed spheres
2-layers closed packed structure

## Slide 91
Closed Packed Structures
hcp
ccp
Hexagonal Closed Packed
Cubic Closed Packed

## Slide 92
c.c.p. structure
(111) Of a FCC structure

## Slide 93
h.c.p. structure

## Slide 94
h.c.p. structure

## Slide 95
Interstitial sites in Closed Packed Structures

## Slide 96
Interstitial sites in Closed Packed Structures
Stable Bonding Configurations in Ionic solids.
In reality an ideal fit of a cation into the close packed anion arrangement almost never occurs. Now consider what would be the consequence of placing a cation that is (a) larger than the ideal, (b) smaller than the ideal, into the cation sites.
For a stable coordination the bonded cation and anion must be in contact with each other.
If rcation/ranion becomes too big, the close packed structure of anions is converted into a simple cubic structure

## Slide 97
Interstitial sites in Closed Packed Structures

## Slide 98
Cubic structures

## Slide 101
Rock salt structure
rNa = 0.102 nm
rCl = 0.181 nm
rNa/r Cl = 0.564
Octahedral sites preferred

## Slide 102
Zinc blende structure
Zn 2+
S 2-
rZn/rS = 0.074/0.184= 0.402
tetrahedral sites preferred

## Slide 103
Fluorite and antifluorite
Calcium Fluorite (CaF2)
Cations in cubic sites
UO2, ThO2, ZrO2, CeO2
Antifluorite structure –
positions of cations and anions reversed
Fluorite structure

## Slide 104
Perovskite ABO3
Perovskite structure
Ex: complex oxide
BaTiO3

## Slide 105
Perovskite ABO3

## Slide 106
Spinels
Inverse
Normal

## Slide 107
In order to explain the adoption of a particular cation distribution in a spinel structure, one must take into account the crystal field stabilization energies (CFSE) of the transition metals present. Some ions may have a distinct preference for the octahedral site depending on the d-electron count. If the A2+ ions have a strong preference for the octahedral site, they will displace half of the B3+ ions from the octahedral sites to tetrahedral sites. Similarly, if the B3+ ions have a low or zero octahedral site stabilization energy (OSSE), then they will occupy tetrahedral sites, leaving octahedral sites for the A2+ ions.
Spinels
Inverse
Normal

## Slide 121: DEFECTS IN SOLIDS
No real crystal is perfect. Real crystals feature defects or irregularities in their ideal arrangements and it is these defects that critically determine many of the electrical and mechanical properties of real materials.
Ideally a perfect crystal is the one in which atoms are arranged in perfectly regular manner in all directions. The deviations of crystals from their perfect periodicity are called defects or imperfections.
These imperfections can be of different types such as:
point defects (zero–dimensional defects),
line defects (one–dimensional)
defects over a surface or a plane (two–dimensional) and volume defects (three–dimensional).

## Slide 122: Point Defects
A point defect is a very localized imperfection in the regularity of a lattice and it does not spread over more than one or two lattice spacings. These defects are observed in metallic crystals (vacancies, substitutional impurity and interstitials) as well as in ionic crystals (Schottky and Frenkel) and are discussed here in brief.
Vacancies
The absence of an atom or ion from a normally occupied site in a crystal is called a vacancy (see Fig.)
Substitutional Impurity
In this kind of defect, a foreign atom occupy a regular site in the crystal structure (see Fig.), i.e., .substitutional atom replaces the host atom from its position. For example, when a pure semiconductor crystal of Silicon or Germanium is doped with a trivalent or pentavalent impurity, we call it a substitutional impurity.

## Slide 123
Interstitial Impurity
An interstitial is an atom or ion which can be inserted into the voids between the regularly occupied sites. In a closed packed arrangement of atoms the packing fraction is generally less than one. Therefore an extra atom, of smaller size than the parent atom, can enter the interstitial space without disturbing the regularly positioned atoms. Such an extra impure atom is called interstitial impurity while an extra atom in an interstitial position is called self – interstitial atom, as shown in Fig. If the size of the extra atom is not small then it will produce atomic distortion.

## Slide 124
(c) 2003 Brooks/Cole Publishing / Thomson Learning

## Slide 125
Emerald and Ruby:
Cr3+ impurities
Cr2O3: green

## Slide 127
When a divalent cation replaces a monovalent cation, a second monovalent cation must also be removed, creating a vacancy.
Charge compensation: vacancy formation

## Slide 128
When a divalent cation replaces a monovalent cation, an anion must change its oxidation state.
Charge compensation: change in oxidation state

## Slide 129
Schottky Defect
In a metal, a vacancy is created if an atom is missing from its lattice position. In ionic crystals, a cation – anion pair will be missing from the respective lattice sites, as shown in Fig. Creation of such a pair, of one cation vacancy together with one anion vacancy, is called Schottky defect. Thus the interior of the ionic crystals remain electrically neutral.
Frenkel Defect
When an atom or ion leaves its normal position or site and is found to occupy another position in the interstice we get a Frenkel defect. Thus, in this case, two imperfections are created – an interstitial and a vacancy as shown in Fig. Normally anion leaves its parent site and occupy the interstitial space. These defects are dominant in open structures such as silver halides. Also a Frenkel defect does not affect the electrical neutrality of a crystal.

## Slide 130
Shottky defect
n = number of vacancy pairs
N = total number of sites
E = energy required to produce a pair
of vacancies in the interior of a crystal

## Slide 131
n = number of vacancies = number of atoms in interstitial sites
N = total number of sites
Ni = number of interstitial positions in the crystal
Ei = energy required to produce a pair of vacancies in the interior of a crystal
Frenkel defect

## Slide 132
First elementary dislocation type:
edge dislocations
Edge Dislocations
Line Defects: Dislocations

## Slide 133
Domains formation
Stacking faults
Errors in crystals packing

## Slide 134
Electronic properties of materials
Justify:
Electron transport properties
Optical properties

## Slide 135
Metallic bond: LCAO model
Molecular orbital for N atoms:
In the case of Na
(and other metals)
Metallic bond
Overlapping of the energy states deriving for higher occupied and lowest unoccupied atomic orbitals: electrons are allowed to spread around over all the atoms in the “molecule” (= crystal).

## Slide 136
Metallic bond: LCAO model
In the case of Si:
3s
3p

## Slide 137
Free Electron Model
In one dimension:
In 3D (crystal):
Many states with the same energy!!!!

## Slide 138
Free Electron Model
Fermi-Dirac “filling” function
Density of states
EF = Fermi Level
Energy of the highest
occupied state at 0 K

## Slide 139
Band structure model
Electrical properties of a material depend on the filling of bands

## Slide 140
Band structure model: metal

## Slide 141
Band structure model: insulator

## Slide 142
Intrinsic semiconductor
Eg
Band Gap
max 3.2 – 3.3 eV

## Slide 143
Extrinsic semiconductor
n-type
p-type

## Slide 144
Electron-hole formation

## Slide 145
Direct band gap
Indirect band gap

## Slide 146
Tauc plot
n = 1/2 for direct allowed transitions
n = 2 for indirect allowed transitions
 | Material | Colour | Direct Eg (eV) | Indirect Eg (eV)
a | CoWO4 | Blue | 2.68 | 1.80
b | NiWO4 | Ochre | 2.95 | 1.82
c | CuWO4 | Brown-Green | 2.41 | 1.78
d | ZnWO4 | White | 5.85 | 3.14
Direct
Indirect

## Slide 147: Current Flow in n-type Semiconductors
The DC voltage source has a positive terminal that attracts the free electrons in the semiconductor and pulls them away from their atoms leaving the atoms charged positively.
Electrons from the negative terminal of the supply enter the semiconductor material and are attracted by the positive charge of the atoms missing one of their electrons.
Current (electrons) flows from the positive terminal to the negative terminal.

## Slide 148: Current Flow in p-type Semiconductors
Electrons from the negative supply terminal are attracted to the positive holes and fill them.
The positive terminal of the supply pulls the electrons from the holes leaving the holes to attract more electrons.
Current (electrons) flows from the negative terminal to the positive terminal.
Inside the semiconductor current flow is actually by the movement of the holes from positive to negative.

## Slide 149
p-n junction

## Slide 150
Solar cells

## Slide 151
Surfaces
Represent the place in which the solid interacts with the environment.
Atoms on the surface have different chemical environment with respect to those in the bulk.
Vertex
Facet
Corner
Different coordination number
Metal dispersion =
Number of superficial atoms
Total number of atoms

## Slide 152
Surfaces
Surface energy
quantifies the disruption of intermolecular bonds that occur when a surface is created.
represents the difference in energy between a real crystal composed of i molecules with a surface and a similar configuration of i molecules located inside an infinitely large crystal. This quantity is therefore the energy associated with the surface.
The equilibrium shape of the crystal will then be that which minimizes the value of .

## Slide 153
Metal surfaces

## Slide 154
Metal surfaces

## Slide 155
Metal surfaces – High-Miller-Index Stepped Surface
6(111) x (100)
4(111) x (100)
8(111) x (100)

## Slide 156
Metal surfaces - Superlattice
fcc (100) – (2x2)

## Slide 157
Metal surfaces - Superlattice
fcc (111) – (2x2)

## Slide 158
Metal surfaces - Superlattice

## Slide 159
Metal surfaces - Reconstruction
Pd(110)

## Slide 160
Metal surfaces - Reconstruction

## Slide 161
Metal surfaces - Reconstruction
19 dangling bonds of (7x7) reconstructed surface
(12 adatom, 6 rest atom, 1 corner hole)
(7x7) Reconstruction of Si (111)

## Slide 162
Coverage of adsorbate molecules
Definition of coverage: one monolayer corresponds to one adsorbate atom or molecules for each unit cell of the clean, unreconstructed substrate surface.
For example, the surface coverage of atom on fcc(100) is one-half a monolayer.

## Slide 163
Ni (100) – c(2x2) - C
Carbon chemisorption induced restructuring of the Ni (100) surface.
Four Ni atoms surrounding each carbon atom rotate to form reconstructed substrate.
Metal surfaces – Adsorbate induced reconstructuring

## Slide 164
Metal surfaces – Adsorbate induced reconstructuring
Fe (110) – (2x2)-S
S-Fe (110), Sulfur-chemisorption-induced restructuring of the Fe(110) surface.

## Slide 165
Metal surfaces – Adsorbate induced reconstructuring
Sulfur-chemisorption-induced restructuring of the Ir (110) surface
fcc(111) surface restructure more frequently upon chemisorption than do the closer-packed crystal faces.

## Slide 166
Ionic material surfaces
Stable
Not stable
Type 1 is neutral with equal numbers of anions and cations on each plane and type 2 is charged but there is no dipole moment perpendicular to the surface because of the symmetrical stacking sequence. Both these surfaces should have modest surface energies and may be stable with only limited relaxations of the ions in the surface region. The type 3 surface is charged and has a dipole moment in the repeat unit perpendicular to the surface. This surface can only be stabilised by substantial reconstruction.

## Slide 167
Ionic material surfaces

## Slide 168
Ionic material surfaces