## Slide 1
Support
Active phase
Heterogeneous catalyst
Promoter
Reagents
Products
Surface where the reaction takes place
Affects the properties of the active phase

## Slide 2
Bonding to surfaces
When atoms or molecules adsorb on ordered crystal surface, they usually form ordered surface structure over a wide range of temperature and surface coverages.
Two factors which decide the surface ordering of adsorbates are
Adsorbate-adsorbate (AA) interaction and adsorbate-substrate (AS) interaction
Chemisorption – adsorbate-substrate interaction is stronger than adsorbate-adsorbate interaction, so the adsorbate locations are determined by the optimum adsorbate-substrate bonding, while adsorbate-adsorbate interaction decides the long-range ordering of the overlayer.
Physisorption or physical adsorption – AA interaction dominates the AS interaction – the surface could exhibit incommensurate structures.

## Slide 3
Bonding to surfaces
Two classifications distinguished by the magnitude of their enthalpies of adsorption
  Physisorption: long-range but weak van der Waals-type interactions with negligible exchange of electrons and enthalpies ~DHcond (-DHAD<35 kJ/mol)
  Chemisorption: formation of a chemical bond (covalent, ionic, metallic) with exchange of electrons and –DHAD>35 kJ/mol
  Enthalpy of chemisorption depends strongly on surface coverage (interactions)

## Slide 4
If adsorbate collides with the surface and doesn’t stick, it may not simply rebound, but rather form a weak bond (physisorption) and diffuse for a period (losing energy) until a vacant site is located for chemisorption to occur.
For adsorption to proceed, the gas needs to “dump” energy into the solid, if not it will desorb. The longer the gas molecule resides on the surface, the more likely is energy exchange with the surface. Can write an Arrhenius-type relationship between residence time and the enthalpy of adsorption at the precursor adsorption site.
Precursor state

## Slide 5
Lennard-Jones Potential for physisorption
z
potential energy
-DHads < 35 kJmol-1
attractive van der Waals interactions
repulsive Coulombic interactions
Pauli repulsion
DHads
0

## Slide 6
Not activated Activated
Potential energy profiles

## Slide 7
PHYSISORPTION | CHEMISORPTION
WEAK, LONG RANGE BONDING Van der Waals interactions (e.g. London dispersion, dipole-dipole).. | STRONG, SHORT RANGE BONDING Chemical bonding involving orbital overlap and charge transfer.
NOT SURFACE SPECIFIC Physisorption takes place between all molecules on any surface providing the temperature is low enough. | SURFACE SPECIFIC E.g. Chemisorption of hydrogen takes place on transition metals but not on gold or mercury.
DHads = - 5 ….. - 35 kJ mol-1 | DHads = - 35 ….. - 200 kJ mol-1
Non activated with equilibrium achieved relatively quickly. Increasing temperature always reduces surface coverage. | Can be activated, in which case equilibrium can be slow and increasing temperature can favour adsorption.
No surface reactions. | Surface reactions may take place:- Dissociation, reconstruction, catalysis.
MULTILAYER ADSORPTION BET Isotherm used to model adsorption equilibrium. | MONOLAYER ADSORPTION Langmuir Isotherm used to model adsorption equilibrium..
Adsorption and Reaction at Surfaces

## Slide 8: (1) Adsorption of CO on Metal Surfaces.
orientation of the molecule
coordinated to one, two or three metal atoms
interactions between the adsorbed CO molecules at high coverages.
dissociation / temperature
Terminal "Linear" (all surfaces)
Bridging
2f site (all surfaces)
Bridging
3f hollow ( fcc(111) )
Bridging
4f hollow (rare - fcc(100) ?)

## Slide 9: (1) Adsorption of CO on Metal Surfaces.
Dissociative adsorption

## Slide 10: A. Hydrogen molecule approaching the W Surface end-on
A1. When the hydrogen molecule approaches end-on to an atop site (i.e. from directly above a W atom) the potential energy increases rapidly for a molecule/surface separation of less than 2.3 Å. The molecule is therefore repelled from the surface.
When the hydrogen molecule approaches end-on to a bridging site the potential energy increases slowly and although some lengthening of the H-H bond may occur with little corresponding increase in energy, there is no facile dissociation channel and the molecule is weakly repelled from the surface.

## Slide 11: B. Hydrogen molecule approaching the W Surface broadside-on.
B1. When the hydrogen molecule approaches broadside-on to an atop site then the molecule may dissociate with considerable energy gain and there is no activation barrier to this process (i.e. the potential energy surface is strongly attractive). The deep well in the lower right corner corresponds to the hydrogen atoms produced by dissociation entering the bridge sites of the W surface.
B2. When the hydrogen molecule approaches broadside-on to a bridge site then the molecule may again dissociate but the energy gain as the hydrogen atoms enter the atop sites is less marked than in the previous case (B1) and there is an activation barrier of ca. 0.2 eV that must be overcome for dissociation to occur.

## Slide 12: Oxygen on metal surfaces
Generally dissociative adsorption
Molecular adsorption (e.g. Ag, Pt).
Molecular adsorption state the interaction between the molecule and the surface is relatively weak. Molecules aligned such that the internuclear axis is parallel to the surface plane may bond to a single metal atom of the surface via both
s-donor interaction, in which the charge transfer is from the occupied molecular p-bonding molecular orbital of the molecule into vacant orbitals of s-symmetry on the metal (i.e. M  O2 ), and
p-acceptor interaction, in which an occupied metal d-orbital of the correct symmetry overlaps with empty p* orbitals of the molecule and the charge transfer is from the surface to the molecule (i.e. M  O2 ).

## Slide 13
Although the interaction of the molecule with the surface is generally weak, one might expect that there might be a substantial barrier to dissociation due to the high strength (and high dissociation enthalpy) of the O=O bond. Nevertheless on most metal surfaces, dissociation of oxygen is observed to be facile which is related to the manner in which the interaction with the surface can mitigate the high intrinsic bond energy and thereby facilitate dissociation.
Once formed, oxygen atoms are strongly bound to the surface and, as noted previously, will tend to occupy the highest available co-ordination site. The strength of the interaction between adsorbate and substrate is such that the adjacent metal atoms are often seen to undergo significant displacements from the equilibrium positions that they occupy on the clean metal surface. This displacement may simply lead to a distortion of the substrate surface in the immediate vicinity of the adsorbed atom (so that, for example, the adjacent metal atoms are drawn in towards the oxygen and the metal-oxygen bond distance is reduced) or to a more extended surface reconstruction.
Oxygen on metal surfaces

## Slide 14: Chemisorption of Unsaturated Hydrocarbons
Unsaturated hydrocarbons (alkenes, alkynes, aromatic molecules etc.) all tend to interact fairly strongly with metal atom surfaces. At low temperatures (and on less reactive metal surfaces) the adsorption may be molecular, albeit perhaps with some distortion of bond angles around the carbon atom.
Ethene, for example, may bond to give both a p-complex (A) or a di-s adsorption complex (B):
(A) Chemisorbed (B) Ethene

## Slide 15: Models of chemisorbed ethene and ethyne on Cu(111)
Studies of ethylene (ethene) and acetylene (ethyne) chemisorbed on Cu(111), a surface with which they interact relatively weakly, have led to the following proposed structures for the molecular adsorption complexes.
A. Plan view of the Cu(111) surface showing the adsorption geometry of athylene and acetylene molecules at low temperatures.

## Slide 16
B. Perspective view of the Cu(111) surface with an adsorbed acetylene molecule, illustrating the re-hybridisation of the carbon centres to a geometry more closely associated with a C=C double-bond configuration.

## Slide 17
H2 adsorption on oxide surfaces
ACS Appl. Mater. Interfaces
2016, 8, 35298−35307
H2 on TiO2 rutile (002)

## Slide 18
H2 adsorption on oxide surfaces
Zr
O
H
H
Zr
O
H
H
HOMO
LUMO
e-
+
-
Zr
O
HOMO
H
H
e-
LUMO
+
-
DFT calculations:
Nakatsuij et al., J. Phys. Chem. 98 (1994), 11840
FT-IR spectroscopy:
Kondo et al., J. Chem. Soc. Farad. Trans.
84 (1988), 511-519.

## Slide 19
H2 adsorption on oxide surfaces
Bernal et al., J. Phys. Chem. 99 (1995) 11794
H2
H
H
1)
H
H
2)
H2O
3)
4)
CeIV
CeIII
O=
Vacanza anionica
H
H
H
H
Mechanism of reduction of CeO2

## Slide 20
O2 is physisorbed on clean surfaces while is chemisorbed on oxygen vacancies (defects on surfaces).
O2 adsorption on oxide surfaces
ChemPhysChem 7 (2006), 1957 – 1963

## Slide 21
Amine adsorption on oxide surfaces
Amine are adsorbed on acid sites: both Bronsted/Lowry and Lewis acids
Colloids and Surfaces A: Physicochem. Eng. Aspects 190 (2001), 261–274
Configuration and IR characteristics of pyridine adosrbed species on metal oxide surfaces at ≥300 K

## Slide 22
CO2 adsorption on oxide surfaces
CO2 is adsorbed on basic sites
Progress in Surface Science 89 (2014), 161–217
Many different types of carbonates and bicarbonates are formed, depending on coordination on the surface

## Slide 23
Alcohols adsorption on oxide surfaces
Alcohols adsorb on oxide surfaces in a dissociative way
Phys. Chem. Chem. Phys., 1 (1999), 5717-5724

## Slide 24
Alcohols adsorption on oxide surfaces
Alcohols adsorb on oxide surfaces in a dissociative way
Phys. Chem. Chem. Phys., 1 (1999), 5717-5724
Simple method for analysis of surface composition

## Slide 25
Measurement of Porosity and Specific Surface Area by Gas Adsorption

## Slide 26: What are Porous Materials?
F. Rouquerol, J. Rouquerol, K. S. W. Sing, Adsorption by Powders and Porous Solids, Academic Press, 1-25, 1999
Non-porous solid
Low specific surface area
Low specific pore volume
Porous solid
High specific surface area
High specific pore volume
Porous materials have highly developed internal surface area that can be used to perform specific function.
Almost all solids are porous except for ceramics fired at extremely high temperatures
Notes: All solids can be classified in to two categories; porous and non-porous solids. Porous solids are those that have high surface area and high pore volume where as non-porous solids are those that have low surface area and low pore volume. In general, all solids to some extend are porous except ceramics fired at high temperatures.

## Slide 27: Measure of Porosity
Pore size and
its distribution
Specific Surface Area, m2/g =
Porosity
There are three parameters used as a measure of porosity; specific surface area, specific pore volume or porosity, and pore size and its distribution.
Mass of the solid, g
Total surface area, m2
Specific Pore volume, cm3/g
Mass of the solid, g
Total pore volume, cm3
=
Porosity, % =
Volume of solid (including pores)
Volume of pores
X 100
Notes: The three measure of a porous solids are surface area, pore size and its distribution and pore volume.

## Slide 28: Size of Pores (IUPAC Standard)
2 nm
50 nm
Micropores
Mesopores
Macropores
Zeolite,
Activated
carbon,
Metal organic
framework
Mesoporous silica,
Activated carbon
Sintered metals
and ceramics
Porous material are classified according to the size of pores: material with pores less than 2 nm are called micropores, materials with pores between 2 and 50 nm are called mesopores, and material with pores greater than 50 nm are macrospores
Sing, K. S. W. et al. Reporting Physisorption Data for Gas/Solid Systems. Pure & Appl. Chem. 57, 603-619 (1985).
Notes: Pores can be open or closed. Open pores are accessible where as closed pores are inaccessible. Open pores

## Slide 29: Shapes of Pores
Conical
Interstices
Slits
Cylindrical
Spherical or
Ink Bottle
Pore
Shapes
F. Rouquerol, J. Rouquerol, K. S. W. Sing, Adsorption by Powders and Porous Solids, Academic Press, 1-25, 1999

## Slide 30
Isoterme di fisiasorbimento

## Slide 31: Gas Sorption: Isotherm
Va
1
P/Po
Type I
or
Langmuir
S. Lowell & J. E. Shields, Powder Surface Area and Porosity, 3rd Ed.
Chapman & Hall, New York, 1991
Concave to the P/Po axis
Exhibited by microporous solids ( < 2nm )
1
P/Po
Type II
Exhibited by nonporous or macroporous solids ( > 50nm )
Unrestricted monolayer-multilayer adsorption
Point B indicates the relative pressure at which monolayer coverage is complete
B
Va

## Slide 32: Gas Sorption: Isotherm
Va
1
P/Po
Type III
Convex to the P/Po axis
Exhibited by nonporous solids
Va
1
P/Po
Type IV
Exhibited by mesoporous solids
Initial part of the type IV follows the same path as the type II
S. Lowell & J. E. Shields, Powder Surface Area and Porosity, 3rd Ed.
Chapman & Hall, New York, 1991

## Slide 33: Gas Sorption: Isotherm
Va
1
P/Po
Type V
1
P/Po
Type VI
Highly uncommon
Exhibited by mesoporous solids
Exhibited by nonporous solids with an almost completely uniform surface
S. Lowell & J. E. Shields, Powder Surface Area and Porosity, 3rd Ed.
Chapman & Hall, New York, 1991
Va

## Slide 34
Gas Sorption: Hysteresis
Hysteresis indicates the presence of mesopores.
Hysteresis gives information regarding pore shapes .
Types I, II and III isotherms are generally reversible but type I can have a hysteresis. Types IV and V exhibit hysteresis.
1
P/Po
Hysteresis
Va
S. Lowell & J. E. Shields, Powder Surface Area and Porosity, 3rd Ed.
Chapman & Hall, New York, 1991

## Slide 35
Gas Sorption: Hysteresis
Va
1
P/Po
Type A
Cylindrical
Slits
Type B
1
P/Po
1
P/Po
Type C
Type D
1
P/Po
Type E
1
P/Po
Conical
Bottle neck

## Slide 36
Physisorption
Brunauer, Emmett and Teller – BET Theory
* Multilayer adsorption
* Dynamic equilibrium
Second layer
First layer
1.
2.
3.
4.
qo Fraction of surface unoccupied
A1 condensation coefficient (adsorption probability)
Nm n° of molecules in a monolayer
E1 Energy of adsorption
n1 adsorbate’s vibrational frequency

## Slide 37
nth layer
Assuming n, E and A constant for 2nd, 3rd,…nth layer (liquid state)
L heat of liquefaction
5.
6.
7.

## Slide 38
7.
8.
9.
10.
11.
12.
13.
14.

## Slide 39
The total number of molecules adsorbed at equilibrium is
Substituting for q1, q2 , …
Since a and b are constant
15.
from 11-14.
16.
17.
18.
from 7-10.

## Slide 40
Substituting in 16.
19.
20.
1 = q0 + q1 + q2 +.....qn
21.
22.
Substituting 22 into 20
23.

## Slide 41
Replacing qn in 23. with abn-1qo from 14.
24.
Replacing a in 24. with Cb from 17.
Since
25.
26.
27.

## Slide 42
From 20.
Substituting 28 in 27.
28.
29.
30.
Introducing qo from 30. into 20
31.
= 1 when
N/Nm = infinite
Condensation on the surface or P/P0 = 1

## Slide 43
Considering Eq. 10 for P/P0 = 1 , b= 1 when
32.
33.
Introducing b into 31.
34.
Recalling that N/Nm = n/nm

## Slide 44: Adsorption Theories: BET
Modification of Langmuir isotherm
Both monolayer and multilayer adsorption
Assumptions:
gas molecules physically adsorb on a solid in layers infinitely;
there is no interaction between each adsorption layer;
the Langmuir theory can be applied to each layer.
Adsorbate
Adsorbent
S.Brunauer, P.Emmett, E.Teller Adsorption of Gases in Multimolecular Layers, J. Am. Chem. Soc., 1938, 60 (2), pp 309–319

## Slide 45: Specific Surface Area Calculation
P/Po
1
V[(Po/P)-1]
0-1
0-2
0-3
At least three data points in the relative pressure range 0.05 to 0.30

## Slide 46: Pore Size Distribution
Va
Pore diameter, d
Narrow pore size distribution
Broad pore size distribution
Unimodal pore size distribution
Pore diameter, d
Multimodal pore size distribution
The distribution of pore volume with respect to pore size is called a pore size distribution.
Va

## Slide 47: Pore Size Distribution
Gads = RT(lnPads - lnP0)
Gdes = RT(lnPdes - lnP0)
Gdes < Gads
1
P/Po
(P/Po)des
(P/Po)ads
Adsorption or desorption isotherm.
The desorption isotherm is preferred over adsorption isotherm.
Va

## Slide 48: Pore Size: Kelvin Equation
Multilayer formation occurs in parallel to capillary condensation.
Capillary condensation is described by the Kelvin equation.

## Slide 49: Pore Size: Kelvin Equation
Actual radius of the pore
Kelvin radius of the pore
Thickness of the adsorbed layer
Prior to condensation, some adsorption has taken place on the walls of the pore, rk does not represent the actual pore radius.
Adsorbed layer

## Slide 50
ADSORPTION PLOT for Ce0.5Zr0.5O2

## Slide 51
Zona di saturazione
Pressione
Volume Gas adsorbito

## Slide 54: 1.1% Pt/g-Al2O3
Adsorbimento a 573 K di H2. Curva (a) adsorbimento su 2.031 g di catalizzatore, (c) adsorbimento su 1.00 g di Al2O3, (d) adsorbimento su quantità di supporto corrispondente a quella del campione (2.00 g) ed espressa nella stessa scala della curva (a), (b) differenza tra la curva a e d.

## Slide 55
Dispersione metallica
numero di atomi superficiali di metallo
numero totale di atomi di metallo.
Diametro medio delle particelle metalliche ( geometria sferica)
= 6 V/A
l'area media occupata da un atomo di metallo
è il volume di un atomo di metallo nel "bulk".
peso atomico del metallo,  la sua densità numero di Avogadro.

## Slide 56
Spillover
Pt/CeO2
H
2
H
H
H
H
H
H
Adsorbimento
Dissociazione
Spillover
Metallo
supportato
CeO2
O
H
O
H
O
H
O
H
O
H
O
H
O
H
H
H
2
Ce
III
O
H
O
H
O
H
O
H
O
H
O
H
O
H
2
H
H
Ce
IV
Riduzione
reversibile
CeO2
CeO2-x + x/2 O2

## Slide 57
Spillover
J. Mater. Chem. A, 5 (2017), 20024–20034

## Slide 58
TCSM
(Tethered Complex
on Supported Metal)
Trasferimento di idrogeno attivato
Supporto
Pd
O
H
H
SiO2 Al2O3
CexZr1-xO2 (CZ) elevata capacità di “spillover” di H

## Slide 59
Formazione di idruri metallici
Pd (2%)/Al2O3
PdHx
Pd-H
PdHx
Stable above 20 mmHg
Stable up to 80°C
Stoichiometry x depends on H2 pressure and size of Pd nanoparticles

## Slide 60
PdHx
Stable above 20 mmHg
Stable up to 80°C
Stoichiometry x depends on H2 pressure and size of Pd nanoparticles
J. Catal. 39 (1975), 44-52
35°C
100°C

## Slide 61
Probability of molecule being associatively adsorbed may defined in terms of a sticking probability, S.
Adsorption kinetics
Macroscopic
Microscopic

## Slide 62
Desorption kinetics
COads
CO(g)
2 Oads
O2 (g)
n = 1
n = 2

## Slide 63
Langmuir isotherm
At the equilibrium:
If:
does not depend from θ
gas flow described by ideal gas law

## Slide 64
Langmuir isotherm
S
(s)
+ A(g)
S A(s)
Molecular chemisorption
2 S
(s)
+ A2 (g)
2 S A(s)
Dissociative chemisorption
General equation

## Slide 65
Co-adsorption
S
(s)
+ A(g)
S A(s)
Molecular chemisorption
S
(s)
+ B(g)
S B(s)

## Slide 66
Langmuir-Hinshelwood
I: unimolecular surface reactions
pA
QA
fast
fast
RDS
khet
A
B
QA = 1
pA
rate
Limit
High pressure (p)
high enthalpy of adsorption (b)
bApA >> 1
rate = khet …….. zero order
kexp
Limit
Low pressure (p)
low enthalpy of adsorption (b)
bApA << 1
rate = khet bA pA …….. first order
kexp

## Slide 67
pA
A
fast
fast
RDS
khet
A
AB
B
pB
QB
Langmuir-Hinshelwood
II: bimolecular surface reactions

## Slide 68
pA
A
fast
fast
RDS
khet
A
AB
B
pB
QB
pA
rate
For constant PB
B >> A
Rate limited by
surface concentration of A
B << A
Rate limited by
surface concentration of B
Langmuir-Hinshelwood
II: bimolecular surface reactions

## Slide 69
pA
A
fast
fast
RDS
khet
A
AB
B
pB
QB
Langmuir-Hinshelwood
II: bimolecular surface reactions
O2 needs 2 sites to dissociate and react.
As pCO increases, the number of adjacent sites decreases, reducing the rate of the reaction.

## Slide 70
Langmuir-Hinshelwood
II: bimolecular surface reactions
pA
A
fast
fast
RDS
khet
A
AB
B
pB
QB
B has a negative reaction order.
B acts as a POISON of the reaction

## Slide 71: Eley-Rideal
An adsorbed molecule may react directly with an impinging gas molecule by a collisional mechanism
pA
A
fast
RDS
khet
A
AB
B
pB
Limit
Low pressure (p)
low enthalpy of adsorption (b)
bApA << 1
rate = khet bA pA pB …….. first order in A
kexp
Limit
High pressure (p)
high enthalpy of adsorption (b)
bApA >> 1
rate = khet pB …….. zero order in A
kexp
Note: For constant pA, the rate is always first order wrt pB
Eley-Rideal
bimolecular surface reactions
QA = 1
pA
rate

## Slide 72
Transition State Model and Catalyst Activity
The Volcano Plot
There is often a relationship between CATALYTIC ACTIVITY ( DEhet ) and strength of chemisorption of reactants DHads.

## Slide 73
Rootsaert & Sachtler: Z.Phys.Chem. 26 (1960) 16
The Volcano Plot
When -DHads is small
bp << 1
= bp a exp ( -DGads/RT ) a exp ( -DHads/RT )
Increasing –DHads will increase Q and hence rate.
DEhet remains unchanged.
When -DHads is large
bp >> 1, and Q = 1
Increasing –DHads starts to increase DEhet
and rate decreases (adsorbates too stable to react.
HCCOH CO2 + H2

## Slide 74
Transition State Model and Catalyst Activity
The Volcano Plot