## Slide 1
Catalyst characterization
Evolution of the catalyst: bulk techniques
Evolution of adsorbates: surface techniques
XRD
XANES/EXAFS
Mössbauer
FT-IR of adsorbates
XPS

## Slide 2
X-ray ray tubes
0.02
0.04
0.06
0.08
0.10
Wavelength (nm)
Intensity (a. u.)
Kb
Ka
min
Characteristic
radiation
Bremsstrahlung
radiation
The spectrum from an X-ray tube has discrete fluorescent lines superimposed on
the continuous bremsstrahlung radiation
Anode
Vacuum tube
Cathode
Electrons
HV
Filament supply
X-rays

## Slide 3: Energy Dissipation

## Slide 4
Radiation angular distribution (a) electrons travelling at low speed and
(b) electrons travelling at relativistic speed (g = (1-v2/c2)-1/2  10000 at ESRF)
Synchrotron radiation angular distribution
Electron orbit
Acceleration
v << c
v  c
Electron orbit
Acceleration
e-
e-
Q  m0c2/E
= 1/g rad
m0 = electron mass
v = electron velocity
E = electron energy
c = velocity of light
v
v

## Slide 5: How a Storage Ring Works
Booster
Electron source
LINAC
Front-end
Optical hutch
Experimental
hutch

## Slide 6
= raggio di curvatura

## Slide 7
Time structure
t
I
1ms
100 ps
e-
e-
e-
e-
Time pulsed emission is interesting for studying rapid reactions
Light pulses

## Slide 8
Detector
Sample
X-rays
Absorption
X-rays
Sample
I
wavelength
Imaging
Detector
X-rays
Elemental analysis
8800
0.0
8800
9000
9200
9400
9600
9800
10000
1.0
2.0
E (eV)
9000
9200
9400
9600
9800
10000
Energy
m
Detector
Fluorescence

## Slide 9
sample
x-rays
I0
I1
transmission experiment
XANES
X-ray Absorption Near Edge Structure
EXAFS Extended X-ray Absorption Fine Structure
measured at Alba/CLÆSS
XAFS: X-ray Absorption Fine Structure

## Slide 10
Monochromator
Beamline structure
Optical hutch
Monochromator:
Si single crystals
(111)
(220)
(311)

## Slide 11
Experimental hutch
Ionization chamber
Fluo detector

## Slide 12
Ex-ray
Qualitative Picture of XAFS
x-ray
Ex-ray
E photoelectron
K 1s
L2 2p1/2
L3 2p3/2
L1 2s
M1–M5
continuum
EF
X
Isolated atom
The outgoing wave is scattered by neighbors
X
Single
Scattering

## Slide 13
Qualitative Picture of XAFS
constructive interference –
absorption maximum
destructive interference –
absorption minimum
Here is where the interference is important!
X
Multiple
Scattering

## Slide 14
A. Di Cicco, A. Filipponi, J. P. Itié and A. Polian, Phys. Rev. B 54 (1996) 9086-9098
High-pressure EXAFS of solid and liquid Kr
Liquid
Solid
Gas

## Slide 15
XANES vs EXAFS
Inelastic mean free path

## Slide 16
EXAFS standard formula

## Slide 17
EXAFS standard formula
  absorber-scatterer distance: Ri
  coordination numbers: Ni
disorder along the absorber – scatterer distance: s2
passive electron relaxation: S02
finite photo-electron mean free path: l(k)
function of scattering amplitude: fi(k)
  phase function: i(k)
A
Sj
Ri
Notes: mettere colori secondo che si voglia conoscere o si conoscano i parametri

## Slide 18
E0
m0
Dm
FT[
]
Outline of EXAFS analysis
2
1
Background subtraction
2
Fourier Transform
Ni K-edge
1

## Slide 19: What we can learn from EXAFS
2.3
2.55 (real RCu-Cu)
Unpleasant thing about EXAFS: FT positions are shifted towards small distances. More unpleasant: Each FT peak has its own shift.
Because of the phase shifts, extracting the
structural information from EXAFS requires curve fitting with assumed (calculated) phase shifts.

## Slide 20
What we can learn from XANES: a) Pre-edge Peak
Dipole selection rule (only in central-symmetric case!): l = ±1
Consider K-absorption for transition metals:
initial state = 1s (l=0)
states near EF are formed by nd electrons (l=2)
central-symmetry | non-central symmetry
no resonance | resonance (pre-edge peak)
from [F. Farges, G. E. Brown, J. J. Rehr,
Phys. Rev. B 56 (1997) 1809]
T. Ressler et al. J. Phys. Chem. B 104, 27 (2000) 6360-6370

## Slide 21: What we can learn from XANES: b) Edge Shift
T. Ressler, R. E. Jentoft, J. Wienold, M. M. Günter and O. Timpe:
J. Phys. Chem. B 104, 27 (2000) 6360-6370
I. Arčon, B. Mirtič, A. Kodre, J. Am. Ceram. Soc. 81 (1998) 222–224
Why does it shift?
1) Electrostatic: it is harder for the photoelectron to leave a positive (oxidized) atom
2) Shorter bonds at higher oxidation states  Fermi energy is higher

## Slide 22
a) Pt3 triangle (dashes), Pt4 tetrahedron (solid), Pt5 triangular bipyramid (dash-dot), and Pt6 octahedron (dash-dot-dot);
(b) Pt7 and Pt4 clusters of different shape: planar ‘‘honeycomb,(dashes), D5h bipyramid (solid) , single-capped
octahedron (long dashdot), Pt4 tetrahedron (dots), and Pt4 planar rhombus (dash-dot).
from A. L. Ankudinov, J. J. Rehr, J. J. Low, and S. R. Bare, J. Chem. Phys. 116 (2002) 1911
What we can learn from XANES: c) White Line
G. Meitzner, G. H. Via, F. W. Lytle, and J. H. Sinfelt, J. Phys. Chem. 96 (1992) 4960
L3 absorption edges for 5d metals:
(transition 2p3/2  5d)
Intensity is proportional to the number of free 5d states and also depends on valence state. But…
…white line also depends on particle size and morphology:

## Slide 23: XAS and small objects: coordination numbers
Infinite lattice
A common subject: bulk metal versus metal clusters.
All atoms are both absorber and scattering centers.
Bulk: any atom is equivalent to the others;
Cluster: surface atoms have a diminished coordination number.
The average first coordination number depends on the size, i.e. surface to bulk ratio.
Small cluster
The EXAFS coordination number
is the weighted average
of the coordination numbers of all absorbers.

## Slide 24
Example: Ag/CeO2

## Slide 25
Reduction treatment: in 5%H2/He atmosphere, stepwise with T=50°C.
Measurements at LN2 temperature in order not to have interference of two effects: (i) due to different temperature vibrations and (ii) due to different particle sizes.
Example: Application of EXAFS to Pd,Pt/C Catalysts (b)

## Slide 26
Reference compound: metallic Pd foil
The difference between a simply reduced Pd/C sample (hydrided) and one subsequently blown out by He flow (dehydrided)
Example: Application of EXAFS to Pd,Pt/C Catalysts (c)
Checking your amplitudes and phases with reference spectra must be always the first step in every EXAFS study!

## Slide 27
CeO2
ZrO2
O
M = Ce or Zr
CeO2 - ZrO2

## Slide 29
Applications:
  catalyst composition
  chemical nature of active phase
  dispersion of active phase
Standard technique in catalyst characterisation
Recently developed Near Ambient Pressure techniques (quasi operando conditions).
X-Ray Electron Spectroscopy (XPS)

## Slide 30
X-Ray Electron Spectroscopy (XPS)

## Slide 31
Binding Energy
Conservation of energy
EB depends on chemical environment:
element
valence state
coordination (type of ligands, number, tetrahedral, octahedral. …)
h = EB + Ekin + Ecorr
corrects for potential difference between sample and analyser
kinetic energy of emitted electron
binding energy of emitted electron
energy of photons

## Slide 32
XPS Equipment
Number of emitted electrons measured as function of their kinetic energy

## Slide 33
NAP-XPS Equipment

## Slide 34: Where do Electrons come from?
Intensity of a peak depends on:
composition
position where electrons are emitted
Electrons interact with the solid
only a fraction of the emitted electrons reach detector with original kinetic energy
the longer the distance, the higher the number of “lost” electrons
z = distance travelled by electrons
 = escape depth

## Slide 35: Inelastic Mean Free Path
2 5 10 50 100 500 1000 2000
Electron energy (eV)
Inelastic Mean Free Path (nm)
10.0
5.0
1.0
0.5
0.3
Au
Au
Au
Au
Ag
Au
Ag
Ag
Au
Au
Ag
Ag
Mo
Be
Ag
W
Ag
Be
Be
Fe
Be
C
Ag
Mo
Ag
Ag
Be
Au
Au
C
C
Be
Mo
W

## Slide 36: Is XPS a Bulk or a Surface Technique?
XPS is a surface-sensitive technique
0
1000
2000
3000
4000
5000
0
2
4
6
8
10
12
Thickness of absorbing layer z (nm)
XPS yield
2 nm
0.5 nm

## Slide 37: XPS Survey of Al2O3
N(E)
E
EB
O(KVV)
O 1s
O 2s
Al 2s
Al 2p
Ar 2p3/2
Ar 2s
C 1s
Satellite
O(KVV)
Auger transitions
AUGER
1253 eV
1000 900 800 700 600 500 400 300 200 100 0
Al2O3 Mg K
780.6
766.7
745.3
805 765 725

## Slide 38: Effect of Valence on Chemical Shift - Al and Al2O3
2p 74.7
2p 72.85
Peak position determined by element and valence
Chemical information on elements
Al2O3
Al
‘Binding energy’ (eV)
86 76 66

## Slide 39: XPS spectrum of a Rh/Al2O3
Element specificity of binding energies (calibration of BE)
Linear relation between intensity of the peaks and atomic concentration

## Slide 40: Xe 3d 5/2 Chemical shift versus oxidation state
E (Xe 3d 5/2)

## Slide 41: Morphological Information
Dispersion of particles over a support from peak intensity ratio
XPS spectra of ZrO2/SiO2

## Slide 42: Application of XPS. 1
XPS spectra of MoO3/SiO2/Si(100) after sulfidation in H2S+H2. (From De Jong et al. J. Phys. Chem (1993)