## Slide 1
Fischer-Tropsch process
Syn-gas
Hydrocarbons
Germany: World War II
USA: 1950s
South Africa: SASOL I (1)955) & SASOL II (1980)
South African Synthetic Oil Ltd.
All exothermic reactions

## Slide 2
Fischer-Tropsch process
The process can be considered as a polymerazion of –CH2– units, even if they are not present initially.

## Slide 3
Fischer-Tropsch process: suggested mechanisms
Hydroxymethylene intermediate
CO insertion mechanism

## Slide 4
Fischer-Tropsch process: suggested mechanisms
Hydroxymethylene intermediate
CO insertion mechanism
Never detected by experimental techniques

## Slide 5
Fischer-Tropsch process: first step requires CO dissociation
All the metals that promotes FT synthesis also dissociates CO easily to its elemental components. In FT process, it is later converted into CHads and CH2ads (confirmed by 13C NMR and HREELS).
Mechanicistic studies using diazomethane CH2N2
CH2N2 in inter gas flow
It forms adsorbed CH2 immediately when in contact with metal surface
Dimerization & desorption
No polymerization
Notes: Co, Ni, Fe, Pd, Ru

## Slide 6
Fischer-Tropsch process: first step requires CO dissociation
CH2N2 + H2 vs CO + H2
Mechanicistic studies using diazomethane CH2N2
Notes: Cu non è in grado di dissociare H2: quindi formazione di H è fondamentale per la produzione di idrocarburi.

## Slide 7
Fischer-Tropsch process: first step requires CO dissociation
CH2N2 + H2 vs CO + H2
Mechanicistic studies using diazomethane CH2N2

## Slide 8
Fischer-Tropsch process: first step requires CO dissociation
CH2N2 + H2 vs CO + H2
Mechanicistic studies using diazomethane CH2N2

## Slide 9
Fischer-Tropsch process
Schultz – Flory distribution
Propagation
Termination
(b-hydride elimination + terminal reduction)
Notes: Rn = frammento alchilico di lunghezza n
Pn = prodotto di lunghezza n
kp e kt siano indipendenti da n

## Slide 10
Fischer-Tropsch process
Schultz – Flory distribution
The distribution of products concentrations is governed by:
A succession of i steps will occur with probability . The chance to obtain the product Pi is proportional to or, in other words,
Notes: Rn = frammento alchilico di lunghezza n
Pn = prodotto di lunghezza n
kp e kt siano indipendenti da n

## Slide 11
Fischer-Tropsch process

## Slide 12
Fischer-Tropsch process
Notes: CO si adsorbe e si dissocia.
H2 si adsorbe e si dissocia.
O adsorbito viene rimosso come H2O o CO2, liberando i siti per adsorbimento di altro CO.
CHx formati polimerizzano per dare i prodotti

## Slide 13
Fischer-Tropsch process
The real mechanism is more complicated, considering that a complex mixture of products is obtained, comprising alkanes, alkenes, alcohols and aldehydes.

## Slide 14
Fischer-Tropsch process
The catalyst composition must be tuned to manipulate
Active phase with high : long C chains
Active phase with high : short C Chains
Catalyst:
Fe2O3 + CuO + K2SiO3
SASOL Process:
Fe + Cu + K2O + SiO2
Catalyst:
Oxygenated synthesis
Rh-based material
Main products: Alcohols, mainly ethanol
Catalyst for FT
Promoter for Fe2O3 reduction
Stabilizer for texture

## Slide 15
Fischer-Tropsch process
The catalyst composition must be tuned to manipulate
Active phase with high : long C chains
Active phase with high : short C Chains
Catalyst:
Fe2O3 + CuO + K2SiO3
SASOL Process:
Fe + Cu + K2O + SiO2
Catalyst:
Oxygenated synthesis
Rh-based material
Main products: Alcohols, mainly ethanol
Catalyst for FT
Promoter for Fe2O3 reduction
Stabilizer for texture
Promoter for CO dissociation

## Slide 16
Fischer-Tropsch process: SASOL I & II
Fixed bed reactor
220-350°C, 30bar
Low space velocity
Products: C1-C35 (waxes 45%, diesel & gasoline 32%)
Fluidized bed reactor
320-360°C, 25bar
High space velocity
Products: C5-C11 (gasoline)
FEED
H2 43%, CO 43%, CH4 12%, CO2 1%, N2 balance

## Slide 17
Purification of H2 from Syn-Gas
basso contenuto di CO (<10ppm)
basse temperature per reforming
PEMFC

## Slide 18
Water - Gas Shift Reaction
Cu, Ni, Fe, Co, Pd, Pt su CeO2
Au / CeO2
CO + H2O
CO2 + H2
HTS: Fe2O3 / Cr2O3
LTS: Cu/ZnO/Al2O3
PReferential OXidation
of CO in excess H2
Pt / CeO2 / Al2O3
Au / CeO2
CuO / CeO2
CO + 1/2 O2
CO2
Processes for CO removal
Notes: PROX è selettivo se il metallo adsorbe preferenzialmente CO e non H2.

## Slide 19
WGSR
“Redox” mechanism
“Associative formate with –OH regeneration” mechanism
The factor governing WGSR is the extension of the metal-promoter interface, as a result of a good contact between the two components.

## Slide 20
WGSR
J. Mater. Chem. A, 5 (2017), 20024–20034

## Slide 21
J. Mater. Chem. A, 5 (2017), 20024–20034
WGSR
Deposition-precipitation on SBA-16
Impregnation of SBA-16 with Pt-DT and Ce(OR)4
Impregnation of hydrophobic SBA-16 with Pt-DT and Ce(OR)4
Deactivation by sintering (irreversible)
Deactivation by deposition of intermediates and/or electronic effects (reversible)