## Slide 12
Position of the redox potentials of various metallic couples related to the energy levels of the conduction and valence bands of TiO2 Degussa P25 at pH=0

## Slide 15
Mineralization of organic pollutants
Organic pollutant + O2
CO2 + H2O + minerals
semiconductor
hn> Ebg
The reaction is non-selective and pratically all organic pollutants can be degraded under selected conditions

## Slide 20
Band-gap energies and relative band position of different semiconductors relative to the water oxidation/reduction potential (vs. NHE)
-2.0
-1.0
0
1.0
2.0
3.0
4.0
V vs NHE (pH=0)
H+/H2
ZrO2
TiO2
MoS2
KTaO3
SrTiO3
WO3
Fe2O3
ZnS
CdS
CdSe
GaP
SiC
Si
5.0
3.4
3.2
3.6
2.4
3.0
1.7
2.25
3.0
1.1
1.75
2.8
2.3 eV
O2/H2O

## Slide 21
Metal / TiO2
Conduction Band
Valence band
2H+
H2
e-
h+
hν
TiO2
H2O
2H++½O2
Thechnological solution: separation of red and Ox reactions
Chemical solution: use of sacrifical agents
Inorganic compounds: S2-/SO32-, Ce4+/Ce3+, IO3-/I-
Organic compounds: EDTA, methanol, ethanol, glycerol, etc.
Metal
H2O
+ ½ O2
cat

## Slide 23
Pt/TiO2 photocatalysts were prepared through photodeposition procedure

## Slide 24
Cu/TiO2 photocatalysts were prepared through wet impregnation procedure
675 mmol h-1 g-1

## Slide 25
Pt/TiO2 photocatalyst was prepared through impregnation procedure
Unknown amount of Pt deposited on TiO2 films
Max H2 production in EtOH/water:
Approx. 11000 mmol h-1 g-1

## Slide 26
H2 production from ethanol
Possible pathway
Accumulated
in solution
ChemCatChem 3 (2011), 574-577

## Slide 27
TUNING TiO2 COMPOSITION
Rutile
Anatase
Brookite
R + A
A + B
A + B
160°C x 24h
+ Urea
TiO2
Appl. Catal. A-Gen. 518 (2016), 167-175

## Slide 28
TUNING TiO2 COMPOSITION
Ethanol/water solution
Simulated sunlight
Brookite:
Favorable electronic properties
Well defined morphology and exposed facets
Appl. Catal. A-Gen. 518 (2016), 167-175
Per mass
Per surface area
Pt 0.2 wt% added as co-catalysts

## Slide 29
Pt/TiO2 photocatalysts were prepared through wet impregnation procedure

## Slide 30
Accumulated
in solution
H2 production from glycerol
Possible pathway
ChemCatChem 3 (2011), 574-577

## Slide 31
W.-D. Zhang, B. Xu, L.-C. Jiang, J. Mater. Chem. 20 (2010), 6383.
CNTs as electron sink
CNTs as sensitizer
TiO2/CARBON NANOMATERIALS
Formation of hybrid materials

## Slide 32
500 nm
20 nm
After calcination
Pd@TiO2/CARBON NANOTUBES
Green Chem. doi: 10.1039/C6GC01979J
EF-TEM
Porous Pd@TiO2 shell around CNT
Anatase phase

## Slide 33
Ethanol/water solution
Glycerol/water solution
Pd@TiO2/CARBON NANOTUBES
Green Chem. doi: 10.1039/C6GC01979J
H2 production under
UV-vis irradiation

## Slide 34
Photocatalytic oxidation of naphtalene in aqueous and organic solvents

## Slide 35
J. Catal. 2002, 211, 434-444
Selective oxidation of alcohols in gas phase using light activated TiO2

## Slide 36
QUANTUM YIELD
Eur. J. Inorg. Chem. 2011, 4309–4323

## Slide 37
BEST PRACTICE IN PHOTOCATALYSIS
OPTIMAL
Limited by light absorption
Limited by mass transfer and/or light scattering
J. Phys. Chem. Lett. 2015, 6, 1907−1910