## Slide 1
Polymers
One primary advantage of polymeric materials is that their macromolecular structure provides many structural properties that can be utilized in the body. The elastic modulus and strength of a polymer can be tailored through chemistry and processing to provide values that are bounded by those of hard and soft biological materials. This feature enables polymers to be utilized in a way that optimizes compliance match with many tissues and enables appropriate load transfer between the implant and the adjacent tissue. Further, polymers, like ceramics, offer a range of bioreactivity that spans from inert to fully resorbable.

## Slide 2
Polymeric materials utilize covalent bonds and secondary interactions to establish their basic structures. Polymers consist of repeated units termed “mers.” Homopolymers are created when one mer or monomer (A) reacts with itself to yield a chain comprising mers (-A-A-A-A-A-A-).
Co-polymers utilize two monomers (A and B) and these monomers many react with themselves or with each other (-A-B-A-B-A-B- or -A-A-B-B-A-A-B-B-). The way in which molecules pack together in a polymer is as important in dictating its properties as is its chemical constitution. Polymers differ primarily from metals and ceramics in that these repeated “mers” are typically in the form of chains or macro-molecules rather than lattice structures. The macromolecules tend to utilize covalent bonds along the backbone of the chain but only use weak secondary forces such as hydrogen bonds or van der Waals forces for cohesion between chains. The foundation element in most polymers is carbon that utilizes sp3 hybridization to facilitate four bonds and serves as the basis for covalent bonding along the backbone structure

## Slide 3
The covalent bonding along the backbone provides strength to the molecules, while the secondary van der Waals attractive forces between molecules contribute to the basic structural properties but also facilitate low melting points and ease of processing.
Polymer chains can be folded into ordered structures or they may be randomly grouped together. If the chains are sufficiently long, they may become entangled and the mechanical drag or friction in moving these chains past each other (owing to the secondary forces) can offer further structural integrity to the polymer system.
The structural properties of polymers depend on many variables, including how their chains are organized in space. The chains can order themselves in three dimensions (network), two dimensions (planar), or in one dimension (chains).

## Slide 5
Most three-dimensional polymer networks are highly crosslinked (covalently bonded between chains) but have no long-range order or lattice structure. Such materials have little or no crystallinity and offer relatively high hardness, strength, and modulus but provide little ductility or strain to failure.
Two-dimensional systems have covalent bonding and ordering in the planar layer but only weak van der Waals forces between layers. The two-dimensional structure provides a lower hardness and low shear strength that facilitates molecular transfer under shear loading (such attributes are necessary when writing with a pencil or in the generation of solid lubricants).
One-dimensional systems (chains) are the most prevalent architectural group in polymers. These systems utilize covalent bonding on the backbone of polymer chains but weak van der Waals interactions between chains and achieve structural integrity through packing and entanglements of chains. These systems may be crystalline or amorphous.

## Slide 6
The ability to pack into crystalline domains is usually the consequence of the chain architecture, backbone chemistry, or molecular weight. If the long chains pack regularly, side-by- side, they tend to form crystalline domains. If the long chain molecules have large side groups or extensive chain length, they may become irregularly tangled and they will tend to be amorphous (no long-range order).
The semi-crystalline polymer comprises uniform stacking of crystalline domains,. In the crystalline lamellae the chains are folded back and forth with order and symmetry, while in the adjacent amorphous regions the chains are entangled but have no order.
Another structural factor contributing to the mechanical properties of a polymer is crystallinity. It is extremely difficult to achieve full crystallinity in a polymer, and there- fore polymers are generally classified as semi-crystalline or amorphous.

## Slide 7
Molecular characteristics such as branching of the backbone, bulky side groups, chain length, and crosslinking (covalent bonds between chains) can limit the ability of a polymer to form crystalline structures. For example, chain branching prevents regular organization of the backbone chain and generally limits crystallinity to less than 30% in the polymer, as is the case with low-density polyethylene (LDPE). Similarly, bulky side groups can prevent packing of chains with any long-range order and may result in fully amorphous structures, as is the case with polystyrene (PS). Another factor that may impede long-range ordering is molecular weight or chain length. If chains become extremely long, as in very high molecular weight polymers, they may become more prone to entanglement rather than crystallization. An interesting result of such factors is that polymers with the same chemistry can vary greatly in molecular weight, crystallinity, and density along with concomitant mechanical properties
Linear chains facilitate efficient packing of molecules and thus the system has higher crystallinity (up to 90%) and density.

## Slide 8
The crystallinity is facilitated through chain folding during chain growth. The linear chains can minimize their energy with appropriate fold lengths. In many highly linear systems, the crystalline domains tend to grow from a nucleation site and form crystalline domains termed spherulites
Spherulites are structurally similar to grains in that they represent the limit of a specific orientation of crystal growth and serve as a boundary that can resist deformation and contribute to the strength of the polymer.

## Slide 9
If the polymerization is allowed to continue so that the linear chains get very long, the molecular weights can become very large. The very high molecular weight has an interesting effect on the structure, and due to the greater propensity for entanglement of very long chains, the ability to crystallize is much more limited. The chains can fold back and forth regularly or irregularly. The latter is characterized as the switchboard model

## Slide 10
The crystallinity of a polymer system directly affects its mechanical properties and hence it is important to understand the nature of crystallite development in polymer systems. There are several factors that indicate whether a polymer will be likely to have a high degree of crystallinity. These include linear and symmetric chains, small side groups, lower molecular weight (smaller chain lengths pack more efficiently), and slow cooling from the melt (enables crystal formation).
In contrast to semi-crystalline polymers, an amorphous polymer comprises randomly ordered or entangled chains throughout its structure. A large side group (-R) on the vinyl polymers (-CH2-CH-R-) or other steric hindrance on the backbone chain can prevent crystallization. In a case such as polystyrene, where R is a benzene ring, the result is a fully amorphous (randomly organized) polymer structure.

## Slide 11
The characterizing feature of an amorphous polymer or the amorphous phase of a semi-crystalline polymer is the glass transition temperature, Tg.
This is the temperature where the polymer transitions from glassy behavior to rubbery behavior and represents the transition between large chain motions and small chain motions in a polymer so that above Tg large chain mobility and sliding are readily available, whereas below Tg chain mobility and sliding are quite limited.
If polymers have a high degree of chain branching, entanglements, or large side groups, then the mobility of chains is limited or restricted, and Tg will be much higher than for other polymer systems.
Polymers with high glass transition temperature (on the order of 100 C or greater) are known as glassy polymers.
If the polymer chains are linear and without large side groups, then chain mobility is easier and Tg is typically quite low.

## Slide 12
Below Tg, amorphous polymers exhibit little deformation. This is useful in applications where the component needs to have a high elastic modulus and little deformability, such as polymethylmethacrylates in acrylic bone cements.
Glassy polymers tend to offer high strength, elastic modulus, and optical clarity (in the absence of additives or scattering particles) but offer limited toughness or strain to failure. Such materials may be used in certain applications where a high degree of resilience or toughness is not required but where optical clarity is needed, such as in their use in ophthalmologic implants
Rubbery polymers, on the other hand, exhibit large recoverable deformations and tend to have very low glass transition temperatures. A classic rubber material is a lightly crosslinked long chain polymer structure that is well above its Tg. Large motions are available to the chains at elevated temperatures and this facilitates large recoverable deformation as the crosslinks (and equivalently hard phases below Tg) provide an intrinsic memory throughout the chain extension.

## Slide 13
The degree of crosslinking has an interesting effect on glass transition temperature of a polymer.
At low levels of crosslinking, the covalent ties between backbone chains facilitate recoverable deformation under large extension and the Tg of the system is low as chain coiling and uncoiling is not hindered.
However, with extensive crosslinking, the extensive deformation is prevented by the covalent bonds between molecular chains and the system behaves like a glassy polymer with a high Tg.
The molecular weight, like crosslinking, affects the glass transition of a polymer system. This effect can be predicted from the Fox and Flory equation
where Tg∞ is the glass transition temperature at infinite molecular weight, K is a material constant for the polymer, and Mn is the molecular weight of the polymer.
The equation predicts that increasing molecular weight increases the glass transition temperature of the polymer.

## Slide 15
The result of basic polymer synthesis is that the polymer structure contains many chains and hence there is a distribution of chain lengths depending on individual termination sequences in polymerization.
Because of this variability in chain size, the molecular weight is typically averaged and can be done on a number or weight basis. The number average molecular weight, Mn, is an average over the number of molecules of given size:
where ni is the number of moles and Mi is the molecular weight of mer-i and is known as the first moment of molecular weight.
Similarly, the weight average molecular weight, Mw, is based on the weight distribution of chains:
where wi is the weight fraction and Mi is the molecular weight of mer-i. The weight average molecular weight is always greater than or equal to Mn.
Molecular weight distribution in polymers

## Slide 16
The distribution of molecular weight and molecule size for a given chemistry makes polymers vastly different than metals and ceramics; while this limits the ability to generally classify properties based solely on chemistry of the polymer, it enables a wide range of properties to be tailored through processing.
The increased length of polymer chains improves strength but reduces the mobility of the chains and can limit the methods by which a polymer is processed. For example, a very high molecular weight polymer may not be able to be injection molded if the melt viscosity is too high and will be limited to a sintering type process coupled with molding, machining, or extrusion.
The chain length or molecular weight also affects the chain entanglement density. As the molecules become larger, they have a greater likelihood for entanglement of chains. These entanglements can act as physical crosslinks but are different in that the entanglements will dissipate at elevated temperatures or sufficient length scales of loading

## Slide 17
crosslinks, on the other hand, are often created with energetic or chemical means and result in permanent covalent bonds between chains.
With sufficient crosslink density, the molecular weight between crosslinks is decreased and the nonlinear elastic deformation (rubber elasticity) or time-dependent strain (viscoelasticity) is severely limited.

## Slide 18
Determination of molecular weight
Consider two linear polymers, such as MDPE and HDPE, which are combined to create one polymer. Assume both polymers are monodisperse, that is, PDI = 1, and that the molecular weight of the MDPE is 100,000 g/mol and that of the HDPE is 400,000 g/mol.
Consider a mixture that is one part by weight MDPE and two parts by weight HDPE.
Determine the weight and number average molecular weight and PDI for this polymer mixture.
The polydisperity index (PDI) is the ratio of Mw/Mn, and is always greater than or equal to one.

## Slide 20
Mechanical behavior of polymers
The deformation of polymers is complicated by the role of various molecular variables such as backbone chemistry, molecular weight, crystallinity, crosslinking, and chain entanglement density.
The mechanical behavior is also strongly affected by both temperature and strain rate. Polymers deform elastically under small stresses. This is similar to an elastic deformation of a crystalline metal or ceramic, except that in addition to bond stretching there is also elastic deformation that is accommodated by angular changes and rotational changes of the polymer chains.
This results in elastic strains being much greater for semi-crystalline polymers and amorphous polymers above their glass transition temperatures than for other crystalline materials. Typical limits of elastic strains are as high as 2% for polymers but are limited to 0.2% for metals and less than 0.1% for ceramics.

## Slide 21
In the rubbery state, the full coiling and uncoiling effect can be activated much like the deformation of an elastic band. This enables large amounts of elastic deformation to occur (up to several hundred percent strain in some elastomers) and elastic strain energy to be stored when the polymer is above its glass transition temperature.

## Slide 22
as the molecular weight, crystallinity, and crosslinking density increase, the polymer becomes more solid-like and less susceptible to viscous mechanisms. Specifically, as a polymer becomes fully crosslinked, it behaves like an elastic solid with an elastic modulus that is not time dependent and a yield strength that is independent of strain rate. A lightly crosslinked system will behave like a rubber system and will demonstrate an upper bound modulus (glassy) below its glass transition temperature or over very short length scales and a lower bound modulus (rubbery) above its glass transition or over very long length scales. The molecular weight affects the onset of flow and at infinitely high values the system behaves like a fully crosslinked structure.

## Slide 23
Polymers in medical implants
Polyethylenes
Polyethylenes are commonly employed as biomaterials and depending on their prop- erties can be employed as catheter tubes, facial implants, artificial tendons, or bearing components in total joint replacements. The polyethylene polymer is made through an addition polymerization reaction that utilizes an ethylene monomer (-C2H4-) repeated along the chain and is generally a semi-crystalline polymer with a Tg of −80 C and a Tm of 125–135◦C.

## Slide 24
The branched, low molecular weight form of polyethylene is known as low-density polyethylene (LDPE). If the chains of this low molecular weight polyethylene are linearly maintained with catalysts during polymerization, the result is a linear low-density polyethylene (LLDPE). High-density polyethylene (HDPE) is a linear polyethylene with chains that have little or no branching along extended lengths of chain.
For this reason, polyethylene is generally subcategorized as low-density polyethylene (LDPE), medium-density polyethylene (MDPE), high-density polyethylene (HDPE), or ultra-high molecular weight polyethylene (UHMWPE).
molecular weight of polyethylene can vary from 30,000–6,000,000 g/mol, density can range from 0.91–0.98 g/cc, and crystallinity can span 30–90%.

## Slide 25
The most widely used and studied polyethylene material is medical grade ultra-high molecular weight polyethylene (UHMWPE) and typically has a molecular weight of about 4–6 million g/mol, an elastic modulus on the order of 1 GPa, and crystallinities of about 50–60%.
In UHMWPE, the polymer chains fold themselves into crystalline lamellae (plate-like structures) dispersed within amorphous phases. Within the crystalline lamellae, UHMWPE has exceptional energetic toughness (ability to absorb energy) owing to its very high molecular weight, crystallinity, and chain entanglement density.
Additionally, its low surface energy and coefficient of friction enable the polymer to perform well as a bearing material against CoCr and ceramic counter bearings in hips, knees, shoulders, and other joint replacements.
A typical total hip replacement utilizing an UHMWPE acetabular cup that articulates against a CoCr femoral head Such implant designs can have survivorship rates of up to 90% after two decades of in vivo service.

## Slide 26
Polymethylmethacrylates
The polymer is generally amorphous with a Tg on the order of 100◦C. In general, this polymer is resilient but it has a limited amount of ductility. PMMA has an elastic modulus on the order of 3–4 GPa and its molecular weight can vary between 200,000–700,000 g/mol depending on processing conditions.
PMMA in general it is known as a glassy polymer. Without any additives this material is known to have excellent transparency. For this reason PMMA is used in ocular implants, although it is best known for its application as a dental or bone cement. An example of PMMA as an orthopedic bone cement providing load transfer between the stem and the adjacent bone in a cemented total hip replacement.

## Slide 27
Fluorocarbon polymers
Fluorocarbon polymers are flexible polyolefin polymers that are commonly employed as vascular grafts, facial implants, or artificial tendons. The fluorocarbon polymer is made through an addition polymerization reaction that utilizes a fluoroethylene monomer (-C2F4-) repeated along the chain and is generally a semi-crystalline polymer with a Tg of −70 C and a Tm on the order of 300–340◦C.
These polymers provide excep- tional properties such as chemical inertness, mechanical integrity, and lubricity that are owed to the highly electronegative fluorine sheath that protects the carbon backbone from chemical attack and results in a hydrophobic polymer with low surface energy. The primary fluoropolymer used in biomedical applications is predominantly based on expanded polytetrafluoroethylene (e-PTFE). The success of this biomaterial results from its microporous structure that allows bio-integration for fixation and provides structural integrity. The predominant success of e-PTFE as a biomaterial is owed to its microporous structure that allows bio-integration for fixation and long-term stability in vivo

## Slide 28
Polypropylenes
Polypropylenes (PP) are commonly used in finger joint prostheses, grafts, and sutures
These polyolefins are generated through addition polymerization and have a repeat mer of the form -(CH2CH CH3)-. The methyl side group can affect the crystallinity of the polymer depending on its arrangement on the backbone.
The melting temperature spans 125–167◦C and its glass transition temperature is on the order of −10 C. Typically, the molecular weight ranges between 200,000–700,000 g/mol and the density is generally bounded between 0.85–0.98 g/cc.
This polymer material has an exceptional fatigue life in flexion and it is for this reason that PP is used in small joint reconstruction. The high tensile strength of this polymer also serves as a good material choice for non-resorbable sutures
Polipropilene isotattico (in alto) e sindiotattico (in basso).

## Slide 29
Polyesters
PET
The annual world wide production of PET is approximately 40 million tonnes and is growing at ca 7% per year. Of this, about 65% is used to make fibres, 5% for film and 30% for packaging.
Polyesters are utilized in non-resorbable sutures and are also employed as vascular graft materials owing to their non-thrombogenic properties. Polyesters have a characteristic ester linkage, -(RC=OOR′)-, in their backbone chain and include materials such as polyethylene terephthalate (PET) and Dacron⃝ fibers. These systems are generally semi-crystalline. The melting temperature spans 250–260 C and its glass transition temperature is on the order of 50–70◦C. These materials are highly flexible and the fabric form enables good tissue integration.
ESTER GROUP

## Slide 30
Another group of condensation polymers includes the polyamides or nylons. These materials have a repeat mer with the form -(NHCO(CH2)4CONH(CH2)6)-. Nylons can be amorphous or semi-crystalline depending on process conditions. Polyamides typically have a glass transition temperature on the order of 50 C and a melting range between 200–300 C. Nylons are susceptible to swelling in aqueous solutions but are often employed in short-term medical device applications such as the outer layer of cardiovascular catheters and as the balloon used for deployment of a stent or the expansion of an occluded artery. Nylons offer strength and stiffness to balloon angioplasty systems
Polyamides
Amide group

## Slide 31
Polyurethanes
Polyurethanes are the broadest classification of polymers and are generated through a step-growth polymerization that combines a monomer comprising at least two isocyanate functional groups with another mer containing at least two hydroxyl (alcohol) groups. The urethane links that build the polymer chains have the chemical formulation (R1-O- C=ONR2R3). Polyurethanes can be processed to have hard and soft segments of varying glass transition temperatures and can span a full range of structural properties ranging from elastomeric to glassy (the glass transition temperature can range between −80 C and 140 C). As a biomaterial, polyurethanes can be used for a wide range of applications, including bearing materials and soft tissue reconstruction.
Isocyanate group
alcohol groups

## Slide 32
Silicones
Silicones are a broad class of polymers also known as siloxanes. These amorphous polymers are composed of -(OSiR2)- on their backbones, have a glass transition on the order of −127 C, and a melting temperature in the range of 300 C. Silicones are known best for their elastomeric-viscoelastic properties. A well-known subclassification of silicone is polydimethylsiloxane (PDMS) that was once used as the fluid filler in silicone breast implants, but this technology was terminated due to concerns of leaking Modern silicone breast implants utilize a crosslinked form of silicone that is a soft solid and elastomeric in nature.

## Slide 33
PEEK
PEEK is a semicrystalline thermoplastic with excellent mechanical and chemical resistance properties that are retained to high temperatures. Its Young's modulus is 3.6 GPa and its tensile strength is 90 to 100 MPa. PEEK has a glass transition temperature of around 143 C and melts around 343 C. Some grades have a useful operating temperature of up to 250 C. It is highly resistant to thermal degradation, as well as to attack by both organic and aqueous environments Polyetheretherketone (PEEK) is used in spinal cages and is also used in suture anchors in soft tissue repair. The backbone structure of PEEK is (-C6H4-O-C6H4-O-C6H4-CO-)n and this semi-crystalline macromolecule provides strength and resistance to deformation. Suture anchors must maintain an anchoring point in bone to securely fasten a suture and are often employed in shoulder arthroplasty

## Slide 34
Poly(lactic) acids
Poly(lactic acid) (PLA) and its derivatives are bioresorbable polyesters that are designed to break down in the body. These materials are used as bioresorbable sutures, tissue engineering meshes, and temporary fracture fixation components. PLA has a glass transition on the order of 50–80 C and a melting temperature of 165–175◦C. The chemical formulation of PLA is (-O-CH (CH3)–C(=O)-)n and it can be found in amorphous or semi-crystalline form depending on its conformation.
The polymers can be blended or co-polymerized to achieve a tailored resorption rate that is controlled primarily through its molecular weight and crystallinity.
PLA degradation is due to 3 mechanisms:
Hydrolysis: The ester groups of the main chain are cleaved, dividing the molecule in two parts, thus reducing molecular weight.
Thermal degradation: A complex phenomenon leading to the appearance of different compounds such as lighter molecules and linear and cyclic oligomers with different Mw, and lactide.
Photodegradation: Sunlight induces degradation due to low-wavelength and high-energy UV radiation.