## Slide 1: SINTERING PROCESS Silvia Dalla Marta (dal corso di Scienza e tecnologia dei materiali ceramici prof. V. Sergo)

## Slide 2
ceramic matherial with porosity:
before sintering
It is a thermal process of microstructural rearrangement in which the particles of powder are compacted and the porosity decreases to form a dense piece of ceramic.
monodisperse powder fcc or hcp: PF=74.5%

## Slide 3: WHY DO YOU HAVE TO SINTER A PIECE OF CERAMIC AFTER FORMATURE?
K: the parameter for the determination of the stress at the tip of the crack.
y: dimensionless constant that depends on defect’s geometry and load
c: length of defect (m)
For the polycrystalline alumina:
In ceramics materials these values are very low compared to metals.
A very small defect or porosity lead to failure during an application of stress.
The absence of defects and porosity is very important for the
mechanical properties:

## Slide 5: Considering two particles of ceramic material in contact with each other:
concave zone
convex zone
The atoms in a convex zone tend to migrate in a concave zone in according to a diffusion process actived by temperature.
BEFORE SINTERING:
powder compact united by weaks Van der Waals forces
individual grains separated by 25-60% of volume porosity

## Slide 6: DIFFUSION PROCESS
Thermodinamically favored
kinetically slow
FICK’S LAW (1D):
Diffusion coefficient:
In order of kinetics to be fast enough for microstructural rearrangment to occur in short time, the sintering temperature must be:

## Slide 7: SINTERING MECHANISMS
SURFACE DIFFUSION
VAPOR TRANSPORT
densification
decrease of the distance between particle centres
NO densification
thinning of the particles
BULK DIFFUSION
GRAIN BOUNDARY DIFFUSION

## Slide 8: Thinning due to vapor phase matherial transfer:

## Slide 9: DENSIFICATION:
atoms migration in the neck zone
pores disappearence
obtaining straight grain boundaries
same chemical potential
thermodynamically stable

## Slide 10: Monodispersed powder: rare and expensive!
More frequent:
Grain size distribution!

## Slide 11: Since grain boundaries migrate toward their centre of curvature, grains with more than 6 sides tend to incorporate grains with less than 6 sides.
SECONDARY ABNORMAL OF BOUNDARY

## Slide 12
Polycrystalline flurite CaF2
illustrating normal grain growth
Growth of a large Al2O3 crystal into a matrix of uniformly sized grain.

## Slide 13
PROGRESSIVE DEVELOPMENT OF MICROSTRUCTURE
IN LUCALOX ALUMINA
a) SEM of initial particles befor sintering (5000x)

## Slide 14
b) SEM of particles after1minute at 1700°C (5000x)
c) SEM of particles after 2 minutes at 1700°C (5000x)

## Slide 15
d) SEM of particles after 6 minutes at 1700°C (5000x)
e) SEM of the final microstructure that is nearly porefree, with only a few pores located within grains (500x)

## Slide 16: PRESSURE DIFFERENCE ACROSS A CURVED SURFACE
The differences in the curvature of surface, causes a pressure difference in the various part of system, that leads to atoms transport.
At the surface of the particle there is a positive radius of curvature, so that the vapour pressure is larger than would be observed in a flat surface.
At the junction between particles there is a NECK whith a small negative radius of curvatures and a vapour pressure lower than that for the particle itself.

## Slide 17
P : Supplementary pressure to create the bubble.
: surface tension
SPHERICAL MODEL:
GENERICALLY:

## Slide 18
in equilibrium condition
vapour pressure of water
in a flat liquid-vapour interface
If the liquid-vapour interface is not flat, as in a small drops, the water has a vapour pressure that is larger than that in a flat surface:
: standard vapour pression

## Slide 19: ENERGY SURFACE in a densification process in which the only energy is given by radius of curvature:
: molecular volume
: density
: particle radius
: number of particles in a mole of powder
: surface area
:surface energy
: surface tension
: molecular weight

## Slide 20
Energy available without added pressure in a sintering pocess of alumina:
Energy available whith added pressure in the same sintering:
Image from Kingery

## Slide 21: DIFFUSION AND MOBILITY:
true in the absence of friction:
otherwise:
Einstein’s generalized equation of mobility:
: friction coefficient
: mobility
: diffusion coefficient

## Slide 22: KINETIC MODELING OF SINTERING PROCESS
define a DRIVING FORCE
define the GEOMETRY
define the MECHANISM OF TRANSPORT
PARAMETERS TO DEFINE THE MODEL:
STAGES OF THE SINTERING:
INITIAL STAGE : from 50-55% to 75% of TD
INTERMEDIATE STAGE : from 75% to 92% of TD
FINAL STAGE : from 92% to 100% of TD
MODELING

## Slide 23
: radius of the neck’s curvature
: radius of particle
: parameter indicated the progress of the sintering
GEOMETRY

## Slide 24
FLUX
The material transfer is linked to the flux.
Considering the area through which the transport takes (the neck area):
d : density
MW : molecoular weight
J : flux
Variation of the neck volume based on the increase of the ‘x’ parameter:

## Slide 25
FLUX expressed as a DRIVING RORCE
c : concentration
M : mobility of bulk and grain boundary atoms
F : force
Variation of the free energy during the diffusion on the neck area:

## Slide 26
integration between 0 and x
t=0, x=0
t: sintering time

## Slide 27
Variation of the volume of the particles in the sintering process during the time:
The increase of a few degrees in temperature has much more influence on the grain size than the increase of a one order of magnitude of the time
Variation of the relative density variatung time and temperature:
t
T

## Slide 30
pore
grain boundary
v
v pore > v grain boundary
GS
E.G. :
ALUMINA ‘LUCALOX‘:
polycrystalline Al2O3 - 1% MgO
During the growth, the larger grain leaves behind a lot of pores and the piece can not achive the 100% of theoretical density (DT).
To avoid the pore incorporation inside the grain, the speed of grain boudaries must be lower than that of the pores.
Some impurities can segregate on grain boundary (GRAIN BOUNDARY PINNING) slowing the growth and so it’s possible to achive the 100% of DT.

## Slide 35
WETTABILITY
Is the ability of a drop of liquid to recline on a solid surface.
Varying the pressur is changed the wettability.
: contact angle
: liquid-vapour interfacial energy
: liquid-solid interfacial energy
: solid-vapour interfacial energy

## Slide 36
possible cases:
The contact angle specifies the condition for minimum energy, according to the relation:
non-wettability
wettability
spreading

## Slide 37
It is the process of adding an additive to the powder which will melt before the ceramic grains.
The metal added, at high temperatures, melt and WET the grains. The intergranulary spaces are such as to have a capillary forces which attract the grain one another.
( By lowering the temperature, the amorphous phase does not wet the grains anymore and ritires in triple junctions.)
(This gives good mechanical proprieties.)
E.G. : WIDIA ( 93% WC in a Co matrix).
LIQUID PHASE SINTERING

## Slide 38: Liquid phase sintered SiC

## Slide 39: Liquid phase sintered Si3N4

## Slide 40: Lquid phase sintered SiAlON

## Slide 46: PROCEDURE FOR THE SINTERING PROCESS
Determination of the Tm Tsintering = 2/3 Tm E.G. : Al2O3 Tm =2400°C Tsintering = 1600°C
CALCINATION (200°C-300°C under the sintering temperature) E.G. : ZrO2 stabilized by CaO, Y2O3, CeO2
FORMING the ceramic parts
SINTERING

## Slide 47: DENSITY DETERMINATION BY ARCHIMEDE’S PRINCIPLE
D = dry weight
boil the piece for 5 hours
W = wet weight in air
S = wet weight in water suspended
V = external volume of the piece: V = W - S
BULK DENSITY B = D/V
P = apparent porosity P = (W-D)/V

## Slide 48: TYPICAL SINTERING TIME-TEMPERATURE PROFILE
1400°C
500°C
T
t
1 h
1-10 h
2-5 K/min
1-5 K/min
10 K/min

## Slide 52
AlN
SiC

## Slide 53: Undistinct features: brittle fracture (SiC)

## Slide 57: Fracture of glass

## Slide 58: Fracture surface of silicon nitride with steel impurity

## Slide 59: Fracture surface of lathe machined Silicon nitride

## Slide 60: Roadmap for fractography

## Slide 61: Roadmap for correcting failure

## Slide 62: Toughening by whiskers and fibers

## Slide 63: Glass theory
Glasses lack the periodic (long range) order of a crystal
•
Infinite unit cell (no repeating large scale structures)
•
3D network lacking symmetry and periodicity
•
ISOTROPIC: same average packing and properties in all directions
•
Crystals in different directions(see above):
•
different atom packing and so different properties

## Slide 66: Pair distribution function of SiO2 glass

## Slide 67: Radial distribution function for Si02
Si-O
1.62
O-O
2.65
Si-Si
3.12
Si-O 2nd
4.15

## Slide 68: Glass structure: SiO2 quartz compared to SiO2 glass

## Slide 70: Zachariasen rules for glass AmOn
An oxygen atom is linked to no more than two glass-forming atoms A.
2) The number of oxygen atoms around each glass-forming atom A is small, perhaps 3 or 4.
3) Among the oxygen-containing polyhedra, a polyhedron cation A shares corners, but no sides or faces.
4) For three-dimensional networks of oxygen-containing polyhedra, at least three corners must be shared.
In general, all four rules should be satisfied for glass formation to occur.
Low coordination numbers, corner-sharing rules imply that glass formation is more likely
with open, low density polyhedral structures.

## Slide 74: Elements for glass formation
Formers Modifiers Intermediate
B Sc Ti
Si La Zr
Ge Na Pb
Al K Al
V Rb Th
As Cs

## Slide 76: Glass Viscosity and Workability
104 Poise
107 Poise

## Slide 77: Pilkington process

## Slide 79: Glass bending

## Slide 80
Bottle production line
://www.youtube.com/watch?v=k8MmEuvugG4

## Slide 81: Dielectrics

## Slide 83: Non destructive testing Techniques
Visual inspection
Penetrant dyes
Ultrasonic testing
Radiographic testing
Magnetoscopic testing
Eddy currents

## Slide 84: Proof testing: 1) load configuration as similar as possible to service condiction 2) one single test slightly above load/stress values in service

## Slide 85: Liquid penetrant dyes

## Slide 86
Fluorescent penetrant dye revealed with a Wood lamp

## Slide 87: Ultrasonic testing

## Slide 90: Radiographic testing

## Slide 91: Radiographic testing of two chips

## Slide 92
X ray image of C inclusions in Si3N4
X ray image of WC inclusions in Si3N4

## Slide 93: Magnetoscopic testing

## Slide 94: Eddy current testing

## Slide 96: SiC Heat exchanger

## Slide 97: Ceramic seal for taps

## Slide 98: Sandblast nozzles

## Slide 99: Rado watches

## Slide 100: SEM fundamentals

## Slide 102: E-beam sample intercation

## Slide 105: Compositional contrast

## Slide 106: Topographycal contrast