## Slide 1: Air pollution
MOBILE SOURCES
EXHAUST
HYDROCARBONS (HC)
CARBON MONOXIDE (CO)
NITROGEN OXIDES (NOX)
SULFUR COMPOUNDS
PM10

## Slide 2: Possible solutions
Hydrogen car
Fuel cell
Electric car
Technical problem - batteries
Hybrid car
Catalytic converters – TWC
Cycling - walking

## Slide 3: Properties of a suitable Three Way Catalyst
Highly active: Conversion > 98%.
50-100 liters of exhaust to be converted in
1 sec per liter of catalyst.
Highly selective: H2O, CO2 and N2 as products.
Thermally stable: working temperature 350-1100°C.
Long life: 200.000 Km.

## Slide 4: Exhaust emissions vary as a function of air-to-fuel ratio (A/F)
Air to fuel ratio, by weight
STOICHIOMETRIC COMBUSTION
(A/F = 14.6 - 14.7)
C8H18 + 12.5 O2 + 12.5 * 3.76 N2
9 H2O + 8 CO2 + 12.5 * 3.76 N2
Engine power NO X 5
Hydrocarbons CO

## Slide 5
TWC: How is the exhaust converted?
CO oxidation:
CO + ½ O2  CO2
HC oxidation:
HC + O2  CO2 + H2O
NO reduction:
NO + ½ CO  ½ N2 + CO2
HC + 2 NO  CO2 + N2 + H2O
Catalyst: Pt (Pd) / Rh / Al2O3 / Cex Zr1-xO2
3 way catalyst

## Slide 7
Support
Metal
Gas phase diffusion
Dissociative adsorption
Molecular adsorption
Surface diffusion
Product desorption
Adsorbed product
Surface reaction
CO
CO2
NO

## Slide 8: Three-way catalysts
Rh for NO reduction
Pt and Pd for CO and
HC oxidation
e-
2 p*
1 s
1 p
NO
Rh Pd Pt
nuclear charge
4 d 4d 5d
Fermi Level
Ms, p
Md
R. Hoffmann et al., J.Phys. Chem., 97 (1993) 7691.

## Slide 9: Temperature dependence of conversions
NO
CO
Temperature / K
Conversion / %
100
50
0
HC
473 573 673 773

## Slide 10: Three-way catalyst
Rich
Lean
NOx
CO
HC

## Slide 11: Drawbacks of current TWCs
Low activity below 300 - 400 °C
Solutions:
Active catalyst at low temperature
Close Coupled Converter (high thermal stability)

## Slide 12
Need A/F close to the stoichiometric value
2CeO2  CeO2-x + x/2 O2
Oxygen buffer in TWCs
CeO2 is an oxygen buffer

## Slide 13: Why CeO2-ZrO2 solid solutions ?
  High thermal stability (ceramic materials)
  incorporation of CeO2 in the solid solution
  may prevent the undesirable fixation of
  ceria in the 3+ state such as in CeAlO3 or
  Ce2(CO3)3.

## Slide 14: CeO2-ZrO2 structure
Ce Zr O
CeO2 CeO2-ZrO2 ZrO2

## Slide 15
Temperature / K
Hydrogen Consumption / a.u.
Rh2O3
Ce4+  Ce3+
10
20
30
40
50
50
60
70
80
90
100
% CeO2
Temperature programmed reduction of 0.5% Rh/CeO2-ZrO2
Surface area < 1 m2/ g
Bulk effects
Tetragonal
Cubic
300 500 700 900 1100 1300
P. Fornasiero et al., J.Catal., 151 (1995) 168.

## Slide 16: Dynamic Oxygen Storage Capacity
How the dynamic-OSC is affected by the nature of the reducing agent ?
What is the importance of surface area in the NM/CeO2-ZrO2 system?
Both H2 and CO are present
in the exhaust

## Slide 17
Room temperature dynamic H2 - OSC on Pt/Ce0.68Zr0.32O2
OSC: H2 and O2 pulses are buffered using Pt/Ce0.68Zr0.32O2
Partial Pressure / torr x 108
Time /s
Pt/Al2O3
Pt/Ce0.68Zr0.32O2

## Slide 18
2 q
CeAlO3
CeO2/Al2O3
CZ20/Al2O3
Samples calcined at 1100°C and after redox ageing
XRD of CeO2/Al2O3 and Ce0.2Zr0.8O2/Al2O3
ZrO2 prevents CeAlO3 formation

## Slide 19: Dynamic CO-OSC at 600°C over the CexZr1-xO2/Al2O3 system
CZ20/Al2O3
CZ60/Al2O3
CZ60
R. Di Monte et. al., Chem.Comm., (2000) 2167.

## Slide 20: Thermal stability: effect of the interaction between CexZr1-xO2 and Al2O3
CZ20
CZ20/Al2O3
CZ60/Al2O3
CZ100/Al2O3

## Slide 21: HREM of Ce0.2Zr0.8O2 (13%)/ Al2O3
30 nm
10 nm
t-Ce0.2Zr0.8O2
In collaboration with S. Bernal and J.M. Gatica, Univesity of Cadiz, Spain
Digital Diffraction Pattern
Calcined at 1100°C 5h

## Slide 22: Role of Ce3+ sites: NO + CO Reaction
Rh/Ce0.6Zr0.4O2-x
Rh/Al2O3
P. Fornasiero et al., J. Catal., 175 (1998) 269

## Slide 23: NO reduction over ceria-based systems
T < 500 K T > 500 K
CO, H2
Ce3+
Ce4+- O
NO
N2O, N2
CO2
H2O
M
M - CO
M - H
CO2, H2O
CO, HC
M - O
M
NO
N2O, N2
M = Rh, Pt, Pd

## Slide 24
CH4 & GREENHOUSE EFFECT
EPA, Emission Overview 2015
Source Identification
and Quantification
Lifetime in the atmosphere is much shorter than CO2
More efficient at trapping radiation than CO2
Impact of CH4 on climate change is more than 25 times greater than CO2
Anthropogenic sources
NEEDS FOR
CATALYTIC ABATEMENT

## Slide 25
Pd-based CH4 combustion catalysts
CH4 + 2O2 CO2 + 2H2O
2 active phases: PdO and Pd
PdO
Pd
High T
Low T
Al2O3
Al2O3
High specific activity
Lower specific activity
Noble metal-based catalysts (Pd, Pt, Au)
Pd(5%)/La-Al2O3
P. Gélin, M. Primet, Appl. Catal. B-Environ. 39 (2002), 1–37

## Slide 26
Pd-based CH4 combustion catalysts
Pd
Pd
PdO
Catalyze re-oxidation
O2 from the gas phase
Al2O3
Pd
O2
Al2O3
Pd
CeO2
O2
O
Ce III
Ce III
O2 from a PROMOTER
REDUCIBLE OXIDES
Maximize PdO - CeO2
interaction

## Slide 27
Pd@CeO2 SUPRAMOLECULAR STRUCTURES
Montini et al. J. Am. Chem. Soc. 132 (2010), 1402-1409.
Hydrolysis conditions:
THF + 30 eq H2O (120 mol vs Ce) in 4 h
THF
MUA: 11-Mercapto Undecanoic Acid
Dispersible in CH2Cl2, toluene, hexane
Pd core size: 1.8 ± 0.2 nm
MUA-Pd NPs
Ce(IV) tetrakis(decyloxide)
Controlled Hydrolysis

## Slide 28
Pd@CeO2 FOR CH4 combustion
Montini et al. Science 337 (2012), 713-717.
HAADF-STEM

## Slide 29
Pd@CeO2 FOR CH4 combustion
Montini et al. Science 337 (2012), 713-717.

## Slide 30
Pd@CeO2 FOR CH4 combustion
R. Farrauto, Science 337 (2012), 659
Water vapor
SO2
Phosphates
PdO DEACTIVATION

## Slide 31
Pd@CeO2 FOR CH4 combustion
0.5% CH4, 2.0% O2, 15% H2O (if present), Ar balance, O2/O2(stoich)=2, GHSV = 200000 mL g-1 h-1
Montini et al. ChemCatChem 7 (2015), 2038-2046
Light Off
Steady State
Effect of water
Dry
Wet
Dry
Wet

## Slide 32
Pd@CeO2 FOR CH4 combustion
IR
Chemisorption
EXAFS
Montini et al. ChemCatChem 7 (2015), 2038-2046
Dry
Wet
Dry-aged
Wet-aged
Fresh

## Slide 33
Pd@CeO2 FOR CH4 combustion
Reduction of PdO to Pd
Increase in population of OH
Wet aging reduces Pd accessibility
Montini et al. ChemCatChem 7 (2015), 2038-2046

## Slide 34
Ce4
ITO/quartz
Al2O3/ITO/quartz
Pd@MOx/Al2O3/ITO/quartz
850°C calcination
ALD
Surface study: SO2 POISONING
Montini et al. Appl. Catal. B-Environ. 202 (2017), 72-83

## Slide 35
Ce4
ITO/quartz
Al2O3/ITO/quartz
Pd@MOx/Al2O3/ITO/quartz
Choose layer composition
Change thickness
General applicability
850°C calcination
ALD
Surface study: SO2 POISONING
Montini et al. Appl. Catal. B-Environ. 202 (2017), 72-83
Model materials comparable to real catalysts

## Slide 36
Ce4
Surface study: SO2 POISONING
Surface area 90-100 m2g-1
Pd accessible area 3 m2 g-1 (~ 60% D)
Similar activity in light off experiments
XRD
CeO2
80:20
60:40
40:60
20:80
ZrO2
PdO
Montini et al. Appl. Catal. B-Environ. 202 (2017), 72-83

## Slide 37
Ce4
Surface study: SO2 POISONING
Low T
0.5% CH4, 2.0% O2, SO2 50 ppm (if present), Ar balance, O2/O2(stoich)=2, GHSV = 200000 mL g-1 h-1
Pd@CZ
Pd@ZrO2
Pd@CeO2
Pd
Similar performances
complete deactivation
Fresh
SO2 350°C Aged
Pd (0)
Pd-SO4
SO2 + PdO → SO3 + Pd
SO3 + PdO → PdSO4
Montini et al. Appl. Catal. B-Environ. 202 (2017), 72-83

## Slide 38
Sulfates formation/desorption
CeO2
CZ
ZrO2
Ce4
Catalytic Activity
0.5% CH4, 2.0% O2, SO2 50 ppm(if present), Ar balance, O2/O2(stoich)=2, GHSV = 200000 mL g-1 h-1
Pd@ZrO2 more resistant
Less sulfates formed and partial desorption
Surface study: SO2 POISONING
S 2p region
Pd@CZ
Pd@ZrO2
Pd@CeO2
Pd
Montini et al. Appl. Catal. B-Environ. 202 (2017), 72-83

## Slide 39
Surface study: SO2 POISONING
Single Cations Sulfates
At 600°C: no deactivation observed
Modification of Ce and Zr spectra
Zr signal not affected in CZ
In CZ, sulfates are mostly formed on Ce
Zr 3d
Ce 3d
CeO2
ZrO2
CZ
CZ
Pristine
500°C SO2/dry
600°C SO2/dry
XPS
Montini et al. Appl. Catal. B-Environ. 202 (2017), 72-83

## Slide 40: Advantages of Lean technology
Lean technology (Excess of air: A/F > 14.6)
fuel economy (15-35%)
decreased CO2 emissions
low HC and CO emissions
Drawback of Lean technology
The reduction of NOx is very
difficult in the presence of a large excess of O2
4 NH3 + 4NO + O2  4 N2 + 6 H2O
C. Cohn et al., 1961, US Patent 2, 975, 025.

## Slide 41: Selective Catalytic Reduction of NOx with NH3
4 NH3 + 4NO + O2  4 N2 + 6 H2O
4 NH3 + 2NO2 + O2  3 N2 + 6 H2O
Stationary applications but NOT (yet) for car :
Separate and additional supply system
Slip of ammonia
and on board NH3 production ?
2NO + 5 H2  2 NH3 + 2 H2

## Slide 42
Scheme of the converter
HC Oxidation
NH3-SCR
Urea

## Slide 43
Catalysts
Catalysts 2017, 7, 199

## Slide 44
Mechanism

## Slide 45: Lean burn catalysts: zeolite-based materials
NO decomposition on Cu-ZSM5
NO  N2 + O2
High temperatures favours NO desorption
H2O slightly effects the activity
NO decomposition is inhibited by O2
Selective catalytic reduction of NO with hydrocarbons
HC + NOx + O2  N2 + H2O + CO2

## Slide 46
0
20
40
60
80
100
100
200
300
400
500
600
Temperature (°C)
2
Conversion on NO to N
(%)
Mn2O3 / Ce-ZSM-5
Ce-ZSM-5
C. Yokoyama and M. Miosnoi, Catal. Lett., 29 (1994) 1.
NO
O2
NO2
X
N2 (+ COx, H2O)
C3H6
NO2/O2
i
iii
ii
Bifunctional DeNOx catalyst
X = organic nitro/nitroso compound

## Slide 47: Silver DeNOx catalysts
DeNOx: NO + HC N2 + CO2
HC combustion: O2 + HC H2O + CO2
Pt and Pd good oxidation catalyst
Growing interest in the use of Ag-based catalysts as possible alternatives
Ag/Al2O3 has been widely studied

## Slide 48
F.C. Meunier et al. J. Catal. 187 (1999) 493.
Silver DeNOX catalyst:
Particle size effect on activity
10% Ag/  - Al2O3
1.2% Ag/  - Al2O3
C3H6 and NO Conversion (%)
Increasing the silver loading shifts the activity to lower temperature

## Slide 49
N2O
NO2
N2
NH3
200
300
400
500
600
Temperature (°C)
0
10
20
30
40
50
60
Yield (%)
10% Ag/  -Al2O3
200
300
400
500
600
Temperature (°C)
0
10
20
30
40
50
60
Yield (%)
1.2% Ag/  - Al2O3
F.C. Meunier et al. J. Catal. 187 (1999) 493.
Silver DeNOX catalyst:
Particle size effect on selectivity

## Slide 50
Ag 0
N
N
O
O
CxHy
NO / O2
C3H6
N2O + N2
H2O
COx
NO + O2
C3H6
Ag+
NOx-
R-ONO
R-NO2
R-NH2
R-NCO
NH3
NO2
N2
O2
Al2O3
Silver DeNOx catalyst: Different roles of Ag during the C3H6-SCR over Ag/  - Al2O3

## Slide 51: Silver DeNOx catalysts
There is a support effect on the De-NOx activity of Ag:
Both using ZrO2 and Ce0.16Zr0.84O2 as support results in a much lower activity range in comparison with Al2O3.
Ag/ZrO2 deactivates completely in the presence of SO2 but it can be easily regenerated.
Ag/Al2O3 deactivates partially in the presence of SO2 and it is not easily regenerated.
Ag/Ce0.16Zr0.84O2 deactivates partially in the presence of SO2 and it can be easily regenerated.

## Slide 52: “ The Toyota” concept
None of the studied system show acceptable activity, hydrothermal stability or resistance to sulphur.
So, perhaps it is not possible to achieve the goal of efficiently reducing NOx in the car exhaust under oxidising condition.

## Slide 53
BaCO3
Ba(NO3)2
Pt
NO + 1/2 O2
Al2O3
CO2
NO2
Rh
NOX storage catalyst: lean conditions

## Slide 54
BaCO3
Ba(NO3)2
Pt
CO + HC + H2
Al2O3
NOx
Rh
CO
N2 + CO2
NOX storage catalyst: rich conditions

## Slide 55
350
325
300
300
200
100
0
0
0.5
2.5
1.5
1.0
2.0
Time / min
NOx / ppm
Temperature / °C
NOx inlet
NOx outlet
Rich pulse
Toyota catalyst: time profiling