## Slide 1
Density Functional Theory Formalism and Applications
Mauro Stener
Dipartimento di Scienze Chimiche e Farmaceutiche
Università degli Studi di Trieste
Via L. Giorgieri 1, 34127 TRIESTE
E-mail: stener@units.it
XIII-EM-TCCM-European Master in Theoretical Chemistry and Computational Modelling 13th International Intensive Course, Perugia (I), 3rd – 28th September 2018

## Slide 2
Summary
THEORY - DFT Review of DFT basic theory and equations
THEORY - TDDFT with the aim to underline what is general from Linear Response formalism.
COMPUTATIONAL - Some numerical aspects of the implementation in the ADF code, most important computational choices, how to assign spectral features. New TDDFT algorithm.
APPLICATIONS:
4.a. Plasmons in metal clusters.
4.b. Core electron excitations (NEXAFS).

## Slide 3
Objectives
Design of a DFT/TDDFT computational scheme to describe photoabsorption of alloyed nanoclusters
Validation with respect to experimental data
Identification of trends in alloys (composition, chemical ordering, cluster shape)
Rationalization of trends in terms of electronic structure

## Slide 4
Computational scheme: geometry
Cluster geometry: DFT geometry optimization or experimental bulk interatomic distances (2.88 Å for Au)
Standard DFT-KS method: LDA (VWN), DZ basis
Scalar Relativistic (SR) effects: ZORA
Code: ADF parallel (MPI) IBM SP6

## Slide 5
Computational scheme: geometry
O. Häberlen, S.-C. Chung, M. Stener and N. Rösch, J. Chem. Phys. 106 (1997) 5189.
LDA  2.89 Å
GGA  2.97 Å
Exp. Bulk: 2.88 Å
For Au, LDA is the best choice for geometry optimization

## Slide 6
orbitals () and eigenvalues () obtained with:
DZ basis set
LB94 (correct asymptotic –1/r behavior) or LDA (VWN)
More stringent SCF convergence: |FP-PF|<10-8
Closed shell electronic structure (charged clusters)
Davidson iterative diagonalization, extraction of the lowest n eigenvalues (n = 300 in our calculations)
LB94: R. van Leeuwen and E. J. Baerends, PRA 49 (1994) 2421
TDDFT electronic excitations
Common VXC choices (LDA and GGA) do not obey to correct asymptotic –1/r behavior, this feature is important to obtain accurate excitation energies and intensities: LB94 is asymptotically correct.

## Slide 7
Conventional chemical synthesis
Structural characterization
at electron microscopy (TEM)
Gold nanoparticles whose size and shape distributions are well defined
Gold nanoparticles TEM images with SPR at:
(a) 700, (b) 760, (c) 880, (e) 1130, e (f) 1250 nm.
Bar scale 50 nm.
Nikoobakht, B.; El-Sayed, M. A. Chem. Mater. 2003, 15, 1957-1962.
Gold and silver clusters

## Slide 8
Samples of large large nanoparticle exhibit an absorption band in visible region
Abs. spectrum of a sample of gold nanoparticles with aspect ratio di 2.6, 3.3, e 5.4 ( = 480 nm).
Burda, C.; Chen, X.; Narayanan, R.; El-Sayed, M. A. Chem. Rev. 2005, 105, 1025-1102
SPR
(Surface Plasmon Resonance)
Collective excitations of conduction band electrons
Important optical property
Theoretical models: classical
electrodynamics for large size
Small size: quantum confinement effects: TDDFT
Gold and silver clusters: optical properties

## Slide 9
How to identify SPR with TDDFT?
H. E. Johnson and C. M. Aikens, JPCA 113 (2009) 4445
TDDFT, SAOP XC potential, DZ basis set, ADF code

## Slide 10
Plasmon resonance: contributed by many 1h1p configurations, with “constructive” interference of z-component of transition dipole moment
Typical “collective” behaviour!

## Slide 11
How to identify SPR with TDDFT?
The “Collective” nature of plasmon resonance is reflected in the “many configurations” which contribute to the excited states, properly described by TDDFT.
Comparison with Single Electron calculation: excited state described by only one Slater determinant, spectrum calculated from dipole moments between KS molecular orbitals.
KS
TDDFT
Peak shifted at higher energy
In TDDFT one transition (plasmon) carries most of the intensity
The Plasmon is contributed by many configurations

## Slide 12
Emerging of SPR along a series of Au nanowires
Au14 Su >> Pu lenghth: 3.744 nm
Au20 Su >> Pu lenghth: 5.472 nm
Au30 Su >> Pu lenghth: 8.352 nm
Gold nanowires (chains):
strong HOMO -> LUMO transition in both KS and TDDFT
It is not plasmonic (dominated by only 1 configuration)
Its energis goes to zero as length increases

## Slide 13
“Thick” Au nanowires
Peak shifted at higher energy
In TDDFT one transition (plasmon) carries most of the intensity
The Plasmon is contributed by many configurations
Typical plasmon size effect
TDDFT
Au122 3.744 nm
Au86 3.168 nm
Au68 2.016 nm

## Slide 14
Structures of four gold clusters
N. Durante, A. Fortunelli, M. Broyer, and M. Stener, JPCC 115 (2011) 6277
[Au147]- Icosahedral
[Au172]4+ Cubic
[Au147]5+ Cube-octahedral
[Au146]2+ Octahedral

## Slide 15
Geometry: bulk (2.88 Å)
Structural relaxation:
[Au146]2+ octahedral

## Slide 16
Structural relaxation:
[Au146]2+ octahedral
Geometry: relaxed

## Slide 17
system | peak position (eV) | peak centre (eV) | peak height (f)
147-CO LB94 | 3.2 | 3.25 | 1.20
146-Oh LB94 | 3.4 | 3.25 | 1.80
172-CU LB94 | 2.95 | 3.00 | 1.20
147-Ih LB94 | 2.95 | 2.95 | 0.65
147-CO LDA | 2.3 | 2.55 | 0.47
146-Oh LDA | 2.6 | 2.50 | 0.55
172-CU LDA | 2.1 | 2.35 | 0.30
147-Ih LDA | 2.5 | 2.35 | 0.35
Estimate peak energy from exp.:
2.9 – 3.0 eV
Cottancin, E.; Celep, G.; Lermé, J.; Pellarin, M.; Huntzinger, J. R.; Vialle, J. L.; Broyer, M. Theor. Chem. Acc. 2006, 116, 514
LB94 better than LDA
Peak maximum more sensitive than peak center
Peak shape dependence

## Slide 18
Charge effect
[Au147]Z+ Cube-octahedral TDDFT (LDA)
relaxed geometry

## Slide 19
Structural relaxation effect
[Au146]Z+ Octahedral TDDFT (LB94)
relaxed and bulk (2.88 Å) geometry

## Slide 20
Alloys: nanoclusters
Built by chemical substitution of [Au147]5+ Cubo-Octahedral, keeping Oh symmetry
Two chemical compositions: [Ag55Au92]5+ and [Au55Ag92]5+
Three chemical ordering: core-shell, multi-shell and maximum mixing.
[Ag55Au92]5+
core-shell
[Ag55Au92]5+
multi-shell
[Ag55Au92]5+
Max mixing
[Ag68Au79]5+
Max mixing
G. Barcaro, M. Broyer, N. Durante, A. Fortunelli, and M. Stener, JPCC 115 (2011) 24085

## Slide 21
Alloys, chemical compositon effect:
[Au147]5+ Cubo-Octahedral shape, core-shell chemical ordering
TDDFT (LB94) relaxed geometry
As Ag concentration increases:
blue shift + intensity enhancement  consistent with experiment
M. Gaudry, J. Lermé, E. Cottancin, M. Pellarin, J. -L. Vialle, M. Broyer, B. Prével, M. Treilleux, and P. Mélinon, PRB 64 (2001) 085407

## Slide 22
Alloys, chemical ordering effect:
[Ag55Au92]5+ and [Au55Ag92]5+ [Ag68Au79]5+ [Au68Ag79]5+ Cubo-Octahedral shape
core-shell (CS), multi-shell (MS) , maximum mixing (MM) chemical ordering
TDDFT (LB94) relaxed geometry
MM
Mixed bonds 55:92
CS 33.9 %
MS 54.6 %
MM 59.2 %
68:79 MM 64.0 %
Double feature
core-shell and multi shell resemble each other
maximum mixing looks different
Ag68Au79 double feature is less evident

## Slide 23
Shape effect:
[M147]5+ and M120 M=Au, Ag Cubo-Octahedral and Td shapes
TDDFT (LB94) relaxed geometry
Shape effect is important for Au and dramatic for Ag, needs more investigation!

## Slide 24
Rationalization in terms of electronic structure
Preliminar results on [Ag55Au92]5+ and [Au55Ag92]5+ core-shell
Analysis of transitions in terms of initial and final states
A: Au(6s)  Au (6p), Ag (5p)
B: Au(6s,5d)  Au (6s,6p)
C: Au(5d)  Au (6p)
D: Au(6s), Ag(5s)  Ag (5p)
E: Au(5d)  Au (6s,6p), Ag(5s,5p)
F: Au(5d)  Au (6s,6p), Ag(5s,5p)
Increasing Ag concentration, Ag contributions start to populate final states.

## Slide 25
Validation of the method, Au86
Au86 nanowire, E longitudinal polarization along (Z).
Scalar Relativistic ZORA, DZ basis set, LB94 XC, energy cutoff at 7 eV, fitting: as in Au2, intense plasmon at 2.35 eV
TCM analysis at 2.35 eV:
Strong intraband 6s  6s 6p transitions, cutoff at 7 eV justified a posteriori
Induced density analysis:
Simple dipolar shape

## Slide 26
Validation of the method, [Au147]-
[Au147]- D5d cluster, E polarization along C5 axis (Z).
Scalar Relativistic ZORA, DZ basis set, LB94 XC, energy cutoff at 7 eV, fitting: as in Au2, weak plasmon at 3.45 eV, accurate transition energy, but the intensity is overestimated
TCM analysis at 3.45 eV:
Strong interband 5d  6s 6p transitions, Plasmon is quenched by screening!
cutoff at 7 eV justified a posteriori
Induced density analysis:
Simple dipolar shape

## Slide 27
Plasmon analysis by scaling factor 
K(r,r’) (kernel)
Scaling method: “Plasmons in molecules” S. Bernadotte F. Evers and C. R. Jacob JPCC 117 (2013) 1863.
E = 0.6 eV
E = 0.4 eV

## Slide 28
Applications: ‘green gold’Au30(S-t-But)18
D. Crasto and A. Dass, JPCC 117 (2013) 22094
D. Crasto, S. Malola, G. Brosofsky, A. Dass and H. Häkkinen, JACS, 136 (2014) 5000
TDDFT ADF with first X-ray structure from A. Dass (private communication)

## Slide 29
Applications: ‘green gold’Au30(S-t-But)18

## Slide 30
Applications: ‘green gold’Au30(S-t-But)18
HOMO-5
HOMO-4
HOMO-3
HOMO

## Slide 31
Applications: ‘green gold’Au30(S-t-But)18
LUMO+4
LUMO+2
LUMO

## Slide 32
Applications: plasmon re-birth Au30(SX)18 X = t-Butyl, Phenyl and Phenyl-NO2
New complex polarizability algorithm
Re-birth with TDDFT in Au23/Au25 clusters:
L. Sementa, G. Barcaro, A. Dass, M. Stener, and A. Fortunelli
Chem. Comm. 51 (2015) 7935 – 7938.
Going from t-But to PhenylNO2:
Red shift
Enhanced absorption
Rising of a new structure at 3.5 - 3.1 - 2.8 eV!
Further analysis is under consideration

## Slide 33
Conclusions:
The density-matrix Casida approach is not practical to treat plasmons in big metal clusters, since many roots (lowest eigenvalues) are necessary.
A complex polarizability TDDFT algorithm is suggested too treat large systems
Implementation of the complex polarizability algorithm is completed in ADF code and published in JCP
Pros: efficiency, low memory, analysis of the transitions
Cons: some approximation (imaginary energy, energy grid), density depenedent kernel.
Applications to large and low symmetric systems, higher energy
Specific applications: re-birth, big clusters (>1000 metal atoms), chiral clusters.