## Slide 1
Solid state chemistry

## Slide 2: Difference Between Amorphous and Crystalline Solids
Amorphous
Amorphous solids (means without form) are the solids which lacks the regular arrangement of atoms or molecules and hence they have a short range order or no order in their structure : ABCBBACBCACCB...
Do not have sharp melting point (because all bonds are not equally strong)
Isotropic (Physical properties are same in different directions)
Examples: glass, wax, plastics, etc.
Crystalline
A crystalline solid is the one in which there is a regular repeating pattern in the structure, or in other words, there is long-range order : ABCABCABCABC…
Have sharp melting point (because all bond are equally strong)
Anisotropic (Physical properties are different in different directions)
Examples: diamond, table salt, ice, methanol, sodium chloride, etc.

## Slide 3: CRYSTAL SYSTEMS AND BRAVAIS LATTICES
Crystals of different substances have similar shapes and hence the crystals are classified into the so called crystal systems depending upon their axial ratio and the interfacial angles ,  and . In three-dimension, there are 7 crystal systems. Bravais showed that throughout the seven crystal systems there are fourteen unique lattice types possible. These are known as Bravais or space lattices. These seven crystal systems with examples are :
Cubic(CsCl, NaCl, Cu)
Tetragonal(SnO2)
Orthorhombic(PbSO4, MgSO4)
Monoclinic(FeSO4, LiSO4  H2O)
Triclinic(FeSO4  5H2O, K2Cr2O7)
Trigonal (Rhombohedral)(Sb, As, CaCO3)
Hexagonal(Zn, Cd, Ni, As, SiO2)
The characteristics features of these crystal systems and the corresponding Bravais lattices are as follows:

## Slide 4
No. | Crystal class | Intercepts on Axes | Angles between Axes | Bravais space lattice
1 | Cubic | a  b  c |       900 | Simple, body-centred, face-centred
2 | Tetragonal | a  b  c |       900 | Simple, body-centred
3 | Orthorhombic | a  b  c |       900 | Simple, body-centred, face-centred, Base(side)-centred
4 | Trigonal | a  b  c |       900 | Simple
5 | Hexagonal | a  b  c |    900,   1200 | Simple
6 | Monoclinic | a  b  c |     900   | Simple, base-centred
7 | Triclinic | a  b  c |      | Simple

## Slide 5
Closed Packed Structures
In a closed packed structure the constituent atoms are so arranged as to occupy minimum possible volume, reaching the maximum density.
Planar closed packed spheres
2-layers closed packed structure

## Slide 6
Closed Packed Structures
hcp
ccp
Hexagonal Closed Packed
Cubic Closed Packed

## Slide 7
Closed Packed Structures
hcp
ccp
Hexagonal Closed Packed
Cubic Closed Packed

## Slide 8
c.c.p. structure
(111) Of a FCC structure

## Slide 9
h.c.p. structure

## Slide 10: MILLER INDICES
The crystal structure may be regarded as made up of an aggregate of a set of parallel equidistant planes passing through at least one lattice point or a number of lattice points. These planes are known as Lattice Planes. For a given crystal, lattice planes can be chosen in different ways as shown in Fig.
Miller Indices are the three smallest possible integers, which have the same ratio as the reciprocals of intercepts of the plane concerned on the three axis.

## Slide 17: INTERPLANER DISTANCE OR SPACING
Interplaner spacing is defined as the perpendicular distance dhkl between corresponding planes. It is also perpendicular distance from the origin to the set of parallel planes (see Fig.)

## Slide 18
For a cubic lattice, a = b = c, therefore, we get
d100 = a d110 = a/2 d111 = a/3.
Also, For a cubic lattice,

## Slide 19: Physical Parameters for Crystal Structure
(i) Number of Atoms per Unit Cell
Number of atoms per unit cell determines how closely the solid is packed and is given by
N = Nc/8 + Nf/2 + Ni
here Nc is the number of corner atoms, Nf the number of face centred atoms and Ni the number of body centred atoms(see Fig.).
For SC crystal : In a SC crystal, there are 8 atoms only, each at one corner. Each atom is shared by 8 unit cells. Therefore, we have
N = Nc/8 = 8/8 = 1
For BCC crystal :N = Nc/8 + Nf/2 + Ni = 8/8 + 0 + 1 = 2
For FCC crystal :N = Nc/8 + Nf/2 + Ni = 8/8 + 6/2 + 0 = 4

## Slide 20
(ii) Coordination Number (CN)
In a crystal, the number of nearest neighbours of the same type and at equal distances from the given atom is called coordination number.
For SC : The corner atoms are the nearest neighbours of each other. Here CN = 6 (see Fig.) which is a group of 8 unit cell and atom at the centre has six corner atoms as its nearest neighbours).

## Slide 21
For BCC : In this case all the corner atoms are at equal distances from the body centered atom.
Hence CN = 8.
For FCC : Here the nearest neighbours of any corner atom are the face centered atoms of the surrounding unit cells. Now for any corner atom there are 4 face centered atoms in each plane and there are three such planes. Therefore, CN = 12.

## Slide 22
(iii) Atomic Radius and Nearest Neighbour Distance (NND)
In a crystal the atoms are assumed to be spheres in contact. Now atomic radius is defined as half the distance between the nearest neighbours in a crystal of pure element, i.e., the distance between the centres of neighbouring atoms.
For SC : In a SC structure, corner atoms are the nearest neighbours and are in touch with each other. If the side of the unit cell is ‘a’ and ‘r’ be the radius , then
2r = a or r = a/2
Now Nearest Neighbour Distance(NND) is given by 2r
Therefore, NND = 2r = a

## Slide 23
For FCC : r = 2 a/4
NND = a/2

## Slide 24
For BCC : r = 3 a/4
NND = 3 a/2.

## Slide 25
(iv) Atomic Packing Fraction (or Factor) (APF)
It is defined as the ratio of the volume of the atoms occupying the unit cell to the volume of the unit cell. It is also called relative packing density.
APF = Volume occupied by the atoms in a unit cell / Volume of the unit cell.
SC Crystal : No. of atoms/unit cell = 1
Volume of one atom = 4/3 r3
Side of the unit cell = a = 2r
Volume of the unit cell = a3
APF = = = /6 = 0.52 = 52%.
BCC Crystal : No. of atoms/unit cell = 2
Volume of two atoms = 2x4/3 r3
Side of the unit cell = a = 4r/3
Volume of the unit cell = a3
APF = = = 3/8 = 0.68 = 68%.
FCC Crystal : No. of atoms/unit cell = 4
Volume of four atoms = 4x4/3 r3
Side of the unit cell = a = 4r/2
Volume of the unit cell = a3
APF = = = 2/6 = 0.74 = 74%.

## Slide 26
Interstitial sites in Closed Packed Structures

## Slide 27
Interstitial sites in Closed Packed Structures
Having determined what types of interstitial sites are available, we must now decide:
(a) Which sites are occupied by a given cation: this determined by the radius ratio (= rcation/ranion)
(b) How many sites are occupied: this is determined by the stoichiometry.
For an octahedral site:
For a tetrahedral site, rcation/ranion = 0.225.
For these two values, the close packed structure of anions is maintained.

## Slide 28
Interstitial sites in Closed Packed Structures
Stable Bonding Configurations in Ionic solids.
In reality an ideal fit of a cation into the close packed anion arrangement almost never occurs. Now consider what would be the consequence of placing a cation that is (a) larger than the ideal, (b) smaller than the ideal, into the cation sites.
For a stable coordination the bonded cation and anion must be in contact with each other.
If rcation/ranion becomes too big, the close packed structure of anions is converted into a simple cubic structure

## Slide 29
Interstitial sites in Closed Packed Structures

## Slide 30
Cubic structures

## Slide 31
Rock salt structure
rNa = 0.102 nm
rCl = 0.181 nm
rNa/rCl = 0.564
Octahedral sites preferred

## Slide 32
Zinc blende structure
Zn 2+
S 2-
rZn/rS = 0.40
tetrahedral sites preferred

## Slide 33
Fluorite and antifluorite
Calcium Fluorite (CaF2)
Cations in cubic sites
UO2, ThO2, ZrO2, CeO2
Antifluorite structure –
positions of cations and anions reversed
Fluorite structure
rCa/rF = 0.958
cubic sites preferred

## Slide 34
Perovskite ABO3
Perovskite structure
Ex: complex oxide
BaTiO3

## Slide 35
Perovskite ABO3

## Slide 36
Spinels
Inverse
Normal

## Slide 37
In order to explain the adoption of a particular cation distribution in a spinel structure, one must take into account the crystal field stabilization energies (CFSE) of the transition metals present. Some ions may have a distinct preference for the octahedral site depending on the d-electron count. If the A2+ ions have a strong preference for the octahedral site, they will displace half of the B3+ ions from the octahedral sites to tetrahedral sites. Similarly, if the B3+ ions have a low or zero octahedral site stabilization energy (OSSE), then they will occupy tetrahedral sites, leaving octahedral sites for the A2+ ions.
Spinels
Inverse
Normal

## Slide 38: DEFECTS IN SOLIDS
No real crystal is perfect. Real crystals feature defects or irregularities in their ideal arrangements and it is these defects that critically determine many of the electrical and mechanical properties of real materials.
Ideally a perfect crystal is the one in which atoms are arranged in perfectly regular manner in all directions. The deviations of crystals from their perfect periodicity are called defects or imperfections.
These imperfections can be of different types such as:
point defects (zero–dimensional defects),
line defects (one–dimensional)
defects over a surface or a plane (two–dimensional) and volume defects (three–dimensional).

## Slide 39
(c) 2003 Brooks/Cole Publishing / Thomson Learning

## Slide 40: Point Defects
A point defect is a very localized imperfection in the regularity of a lattice and it does not spread over more than one or two lattice spacings. These defects are observed in metallic crystals (vacancies, substitutional impurity and interstitials) as well as in ionic crystals (Schottky and Frenkel) and are discussed here in brief.
Vacancies
The absence of an atom or ion from a normally occupied site in a crystal is called a vacancy (see Fig.)
Substitutional Impurity
In this kind of defect, a foreign atom occupy a regular site in the crystal structure (see Fig.), i.e., .substitutional atom replaces the host atom from its position. For example, when a pure semiconductor crystal of Silicon or Germanium is doped with a trivalent or pentavalent impurity, we call it a substitutional impurity.

## Slide 41
Interstitial Impurity
An interstitial is an atom or ion which can be inserted into the voids between the regularly occupied sites. In a closed packed arrangement of atoms the packing fraction is generally less than one. Therefore an extra atom, of smaller size than the parent atom, can enter the interstitial space without disturbing the regularly positioned atoms. Such an extra impure atom is called interstitial impurity while an extra atom in an interstitial position is called self – interstitial atom, as shown in Fig. If the size of the extra atom is not small then it will produce atomic distortion.

## Slide 42
Schottky Defect
In a metal, a vacancy is created if an atom is missing from its lattice position. In ionic crystals, a cation – anion pair will be missing from the respective lattice sites, as shown in Fig. Creation of such a pair, of one cation vacancy together with one anion vacancy, is called Schottky defect. Thus the interior of the ionic crystals remain electrically neutral.
Frenkel Defect
When an atom or ion leaves its normal position or site and is found to occupy another position in the interstice we get a Frenkel defect. Thus, in this case, two imperfections are created – an interstitial and a vacancy as shown in Fig. Normally anion leaves its parent site and occupy the interstitial space. These defects are dominant in open structures such as silver halides. Also a Frenkel defect does not affect the electrical neutrality of a crystal.

## Slide 43
Shottky defect
n = number of vacancy pairs
N = total number of sites
E = energy required to produce a pair
of vacancies in the interior of a crystal

## Slide 44
n = number of vacancies = number of atoms in interstitial sites
N = total number of sites
Ni = number of interstitial positions in the crystal
Ei = energy required to produce a pair of vacancies in the interior of a crystal
Frenkel defect

## Slide 45
Emerald and Ruby:
Cr3+ impurities
Cr2O3: green

## Slide 47
Cr-O distance in Be3Al2(SiO3)6 is larger than in Al2O3
DO1 < DO2
DO1
DO2

## Slide 48
When a divalent cation replaces a monovalent cation, a second monovalent cation must also be removed, creating a vacancy.
Charge compensation: vacancy formation

## Slide 49
When a divalent cation replaces a monovalent cation, an anion must change its oxidation state.
Charge compensation: change in oxidation state

## Slide 50
Electronic properties of materials
Justify:
Electron transport properties
Optical properties

## Slide 51
Metallic bond: LCAO model
Molecular orbital for N atoms:
In the case of Na
(and other metals)
Metallic bond
Overlapping of the energy states deriving for higher occupied and lowest unoccupied atomic orbitals: electrons are allowed to spread around over all the atoms in the “molecule” (= crystal).

## Slide 52
Metallic bond: LCAO model
In the case of Si:
3s
3p

## Slide 53
Free Electron Model
In one dimension:
In 3D (crystal):
Many states with the same energy!!!!

## Slide 54
Free Electron Model
Fermi-Dirac “filling” function
Density of states
EF = Fermi Level
Energy of the highest
occupied state at 0 K

## Slide 55
Band structure model
Electrical properties of a material depend on the filling of bands

## Slide 56
Band structure model: metal

## Slide 57
Band structure model: insulator

## Slide 58
Intrinsic semiconductor
Eg
Band Gap
max 3.2 – 3.3 eV

## Slide 59
Extrinsic semiconductor
n-type
p-type

## Slide 60
Electron-hole formation

## Slide 61
Direct band gap
Indirect band gap

## Slide 62
Tauc plot
n = 1/2 for direct allowed transitions
n = 2 for indirect allowed transitions
 | Material | Colour | Direct Eg (eV) | Indirect Eg (eV)
a | CoWO4 | Blue | 2.68 | 1.80
b | NiWO4 | Ochre | 2.95 | 1.82
c | CuWO4 | Brown-Green | 2.41 | 1.78
d | ZnWO4 | White | 5.85 | 3.14
Direct
Indirect

## Slide 63
Surfaces
Represent the place in which the solid interacts with the environment.
Atoms on the surface have different chemical environment with respect to those in the bulk.
Vertex
Facet
Corner
Different coordination number
Metal dispersion =
Number of superficial atoms
Total number of atoms

## Slide 64
Surfaces
Surface energy
quantifies the disruption of intermolecular bonds that occur when a surface is created.
represents the difference in energy between a real crystal composed of i molecules with a surface and a similar configuration of i molecules located inside an infinitely large crystal. This quantity is therefore the energy associated with the surface.
The equilibrium shape of the crystal will then be that which minimizes the value of .

## Slide 65
Metal surfaces
FCC metals

## Slide 66
Metal surfaces
BCC metals

## Slide 67
Metal surfaces - Superlattice
fcc (100) – (2x2)

## Slide 68
Metal surfaces - Superlattice
fcc (111) – (2x2)

## Slide 69
Metal surfaces - Superlattice

## Slide 70
Metal surfaces - Reconstruction
Pd(110)

## Slide 71
Metal surfaces - Reconstruction

## Slide 72
Metal surfaces - Reconstruction
19 dangling bonds of (7x7) reconstructed surface
(12 adatom, 6 rest atom, 1 corner hole)
(7x7) Reconstruction of Si (111)

## Slide 73
Metal surfaces – High-Miller-Index Stepped Surface
6(111) x (100)
4(111) x (100)
8(111) x (100)

## Slide 74
Coverage of adsorbate molecules
Definition of coverage: one monolayer corresponds to one adsorbate atom or molecules for each unit cell of the clean, unreconstructed substrate surface.
For example, the surface coverage of atom on fcc(100) is one-half a monolayer.

## Slide 75
Ni (100) – c(2x2) – C
Carbon chemisorption induced restructuring of the Ni (100) surface.
Four Ni atoms surrounding each carbon atom rotate to form reconstructed substrate.
Metal surfaces – Adsorbate induced reconstructuring

## Slide 76
Metal surfaces – Adsorbate induced reconstructuring
Fe (110) – (2x2)-S
S-Fe (110), Sulfur-chemisorption-induced restructuring of the Fe(110) surface.

## Slide 77
Metal surfaces – Adsorbate induced reconstructuring
Sulfur-chemisorption-induced restructuring of the Ir (110) surface
fcc(110) surface restructures more frequently upon chemisorption than do the closer-packed crystal faces.

## Slide 78
Ionic material surfaces
Stable
Not stable
Type 1 is neutral with equal numbers of anions and cations on each plane and type 2 is charged but there is no dipole moment perpendicular to the surface because of the symmetrical stacking sequence. Both these surfaces should have modest surface energies and may be stable with only limited relaxations of the ions in the surface region. The type 3 surface is charged and has a dipole moment in the repeat unit perpendicular to the surface. This surface can only be stabilized by substantial reconstruction.

## Slide 79
Ionic material surfaces

## Slide 80
Ionic material surfaces

## Slide 81: Microscopia a scansione ad effetto tunnel
Punta
CORRENTE
COS’È?
Se sulla superficie ci sono delle asperità anche piccolissime la corrente di tunneling cambia intensità

## Slide 82
COME SI USA?
Percorso seguito dalla punta

## Slide 83
COSA VEDO?
Superficie (111) di Pt

## Slide 84
STM: Scanning Tunneling Microscopy
Developed by Binning and Rohrer at the IBM Zürich research laboratory in the early 1982 (Noble Prize in 1986)
Based on a new concept:
To examine a surface at very close range (near field) with a scanning probe, the position of which can be perfectly controlled in three dimensions to within ± 0.1 nm. The signal generated on each point by the interaction between the probe and the surface atoms is translated electronically into an image of the surface.
Technique for “topografical” investigation of surfaces

## Slide 85
Principle of the technique
“The principle of STM in straightforward. It consists essentially in scanning a metal tip over the surface at constant tunnel current. The displacements of the metal tip given by the voltage applied to the piezodrives then yield a topographic picture of the surface. The very high resolution of STM rests on the strong dependence of the tunnel current on the distance between the two electrodes, i.e., the metal tip and the scanned surface.”
G. Binning et al. Phys. Rev. Lett. 49 (1), 57-61 (1982)
Surface
Tip
Tunnel
Current
<1nm

## Slide 86
Tunnel effect
In classical physics, an electron cannot penetrate into or across a potential barrier if its energy E is smaller than the potential  within the barrier.
The quantum mechanics treatment predicts that an electron have a finite probability to exist behind the potential barrier.
This is called TUNNEL EFFECT

## Slide 87
Theoretical basis of tunnel effect
A quantum mechanic treatment predicts an exponential decaying solution for the electron wave function in the barrier. For a rectangular barrier of width d:
where

## Slide 88
Theoretical basis of tunnel effect
A quantum mechanic treatment predicts an exponential decaying solution for the electron wave function in the barrier. For a rectangular barrier of width d:
where
The probability of finding an electron behind the barrier of the width d is:
When a little bias potenzial V is applied between 2 electrodes (sample and tip, in this case), the tunneling of electrons results in a tunneling current I.
The tunneling current is proportional to propability of electrons to tunnel through the barrier:
It is necessary that the tip is very close to the surface to have a measureable current!

## Slide 89
Theoretical basis of tunnel effect – Bardeen Approach
In case of a negative potential on the sample the occupied states generate the current, whereas in case of a positive bias the unoccupied states of the sample are of importance. It should finally be mentioned that the probability of tunneling is larger for electrons which are close to the fermi edge due to the lower barrier.
The current is given by a combination of the local densities of states of the sample and the tip.

## Slide 90
Theoretical basis of tunnel effect – Bardeen Approach
Examples:
Imaging the occupied states of SiC() 3x3
Imaging the unoccupied states of SiC() 3x3

## Slide 91
Lateral resolution
Calculations and experiments showed that there is often a dz2 like state near the Fermi edge present at the apex atom which also predominantely contributes to the tunneling current. It is understood that this state (and also the pz like state) is advantageous for a «sharp» tip.
It is possible to obtain ATOMIC RESOLUTION of the surfaces investigated.

## Slide 92
Schematic rappresentation of an STM apparatus

## Slide 93
Modes of operation
1. Constant Current Mode
By using a feedback loop the tip is vertically adjusted in such a way that the current always stays constant.
A kind of a topographic image of the surface is generated by recording the vertical position of the tip.

## Slide 94
Modes of operation
1. Constant Current Mode
By using a feedback loop the tip is vertically adjusted in such a way that the current always stays constant.
A kind of a topographic image of the surface is generated by recording the vertical position of the tip.
2. Constant Height Mode
In this mode the vertical position of the tip is not changed. The current as a function of lateral position represents the surface image. This mode is only appropriate for atomically flat surfaces as otherwise a tip crash would be inevitable.

## Slide 95
COME È FATTO LO STRUMENTO?
0.38 mm

## Slide 96
Molecole di NH3 su una superficie Pt (111)

## Slide 97: Applicazioni alla catalisi
Struttura intermedia nella formazione di un ossido sul rodio
4030 nm2
5353 Å2
Distanza lungo il profilo
Altezza
3.0 Å invece di 2.7 Å

## Slide 98
L’STM COME UNA VIDEOCAMERA
Catalizzatore di rodio ricoperto di ossigeno esposto ad idrogeno
Superficie iniziale
1515 nm2
I step: l’onda
1 min
II step: la reazione continua
3 min
Superficie pulita
11 min
Un’onda chimica spazza il catalizzatore

## Slide 100
Superficie iniziale
5050 nm2
Coppie di ossigeni
1 min
Specie intermedia
3 min
Fase finale
7 min
Si formano dei prodotti intermedi

## Slide 101
Superficie iniziale
6060 nm2
Reazione
4 min
Superficie pulita
10 min
Superficie finale
2h 39 min
Gli atomi di superficie si riarrangiano

## Slide 102
L’STM PER MISURE STATICHE
NO
NH3
NH3 + NO
Ammoniaca (NH3) + monossido di azoto (NO) sul platino (Pt)

## Slide 103
Example: CeO2 (111)
Surface of the crystal
200nm x 200nm
Flat
Terraces
Large enough for topographical study of the surface
Crystal of CeO2 provided by Commercial Crystal Inc., grown with (111) orientation

## Slide 105
Example: CeO2 (111)
10nm x 5 nm
M.A. Henderson et al.
Surface Science 526 (1-2), 1-18 (2003)
Cleaned surface
The main contribution to the STM image contrast originates from the oxygen 2p states.
H. Nöremberg et al. Physical Review Letters 79 (21), 4222-4225 (1997)

## Slide 106
Example: CeO2 (111)
20nm x 20nm
After cleaning:
sputtering with Ar+ + annealing in O2 up to 1000°C

## Slide 107
20nm x 20nm
Example: CeO2 (111)
After 3h H2 1x10-8 mbar 400°C
Single vacancy
Line
defect

## Slide 108
Example: CeO2 (111)
After 3h H2 1x10-8 mbar 400°C
Oxygen atoms around the vacancies are brighter.
Oxygen vacancies corrisponds to a CeIII in the first sub-layer.
For the explanation of the enhanced brightness of oxygen atoms one has to consider the possibility of a small charge transfer from vacancies to these oxygen atoms.
20nm x 20nm

## Slide 109
Difetti superficiali su CeO2 (111)
F. Esch, S. Fabris, L. Zhou, T. Montini, C. Africh, P. Fornasiero, G. Comelli, R. Rosei Science 309 (2005), 752
Annealing a 900°C
1 min
5 min

## Slide 110: Difetti singoli su CeO2 (111)
F. Esch, S. Fabris, L. Zhou, T. Montini, C. Africh, P. Fornasiero, G. Comelli, R. Rosei Science 309 (2005), 752

## Slide 111: Difetti multipli sotto superficiali su CeO2 (111)
Difetti superficiali di CeO2:
Siti di attivazione di piccole molecole
Stabilizzazione di cluster di Au attraverso interazione con difetti superficiali / sotto superficiali
F. Esch, S. Fabris, L. Zhou, T. Montini, C. Africh, P. Fornasiero, G. Comelli, R. Rosei Science 309 (2005), 752