## Slide 1: Scienza e tecnologia dei materiali ceramici
Prof. Valter Sergo
Università degli Studi di Trieste
Dipartimento di Ingegneria ed Architettura
Contributi di:
Federico Antonelli
Elisa Favero
Silvia Dalla marta

## Slide 3: Packing of atoms determines structures

## Slide 6
Rock Salt: MgO, CaO, NiO

## Slide 7: ROCKSALT (NaCl)

## Slide 8
Zinc Blend and wurtzite: ZnO, SiC, BeO

## Slide 9: WURTZITE [(Zn,Fe)S]

## Slide 10: SPHALERITE [(Zn,Fe)s]

## Slide 11
Fluoride struture: ZrO2, CeO2, UO2

## Slide 12: FLUORITE (CaF2)

## Slide 13: CORUNDUM (Al2O3 - )

## Slide 14
Perovskite

## Slide 16: Cubic Body Centered

## Slide 17: PEROVSKITE (CaTiO3)

## Slide 19: Kröger – Vink Notation

## Slide 20
Proposed in 1956 by F.A. Kröger and H.J. Vink in the journal Solid State Physics (F.A. Kröger, H.J. Vink, Relations between the Concentrations of Imperfections in Crystalline Solids, Solid State Physics, Volume 3, 1956, 307-435)
Set of conventions used to describe lattice position and electric charge for point defects in crystalline structures
The key concept is the crystal lattice to consist of POSITIONS and ATOMS

## Slide 21: Vacancy
There can be unoccupied positions :
these empty positions are called VACANCIES
In the picture, there is a Na vacancy, which is symbolized by:
Notes: Na = sodium
Cl = chlorine

## Slide 22: Vacancy & Charge
However, like ions, also vacancies have charge:
e.g. proceeding with the previous example, the absence of a ion Na+ leads to a lack of positive charge, meaning a negative charge concentration!
Vacancies have always OPPOSITE CHARGE to the missing ion

## Slide 23: Charge
 negative charge e.g.
 positive charge e.g.
 neutrality e.g.
(neutrality may be unexpressed)
[Oxygen vacancy
with 2 (+) charges]

## Slide 24: Substitutional defect
An atom or a ion can be replaced by another:
The Ca ion took the place of the Na ion, which is symbolized by:
As Ca ion has 2 (+) charges, while Na ion has only 1 (+) charge, there is a total 1 (+) charge, so:
Notes: Ca = calcium
Na = sodium
Cl = chlorine

## Slide 25: Interstitial defect
An atom or a ion can be present on any site that would be unoccupied in a perfect crystal, as is typical for H+ ions in metallic lattice:
Interstitial H+ ion in Fe lattice is symbolized by:
Notes: H = hydrogen
Fe = iron

## Slide 26: Pure electric charge
pure electric charges
electrons
“holes"
electron:
hole:

## Slide 27: Quasi – Chemical Approach to defect formation

## Slide 28
Apply Chemical Equilibrium concepts to solid dissolutions of a substance into another
In order to be able to describe (hence with predictive purposes also) defects formation “reactions”

## Slide 29: RULES for defect formation “reactions”
SITE BALANCE,
MASS BALANCE,
CHARGE BALANCE.

## Slide 30
Given a generic compound MAXB:
SITE BALANCE: at equilibrium the ratio of #M SITES (NOT actual atoms) to #X SITES must always be preserved
  So, creating anionic sites must lead to the creation of cationic sites as well (and vice versa) IN THE RIGHT RATIO
MASS BALANCE: defect formation reactions can’t create nor destroy mass
CHARGE BALANCE (Electro Neutrality Condition): preservation of crystal global neutrality
  So, there can’t be reactions which leave the crystal charged
  So, the total sum of negative electric charges must be equal to total sum of positive charges

## Slide 31: Defects

## Slide 32: Perfect Crystal
Crystal which has a completely ordered structure with atoms at rest and electrons distributed in the lowest possible energy states.
But REAL crystals contain a variety of imperfections, or defects.
In crystalline ceramics the structure and chemistry of the material will be determined by the kinetics of defect movement.

## Slide 33: Defects
What is special about ceramic defects is that they can be charged, while metals cannot.
DEFECT HIERARCHY: defects are often classified in terms of a dimensionality: 0D, 1D, 2D, or 3D.
NB: In spite of the classification, ALL these defects are three-dimensional!
“Dimension” | Defect
0 | Point defects
1 | Line defects
2 | Surfaces Grain boundaries Phase boundaries
3 | Volume defects

## Slide 34: Point defects
Point defects are particularly important in ceramics because of the role they can play in determining the properties of a material.
e.g. the entire semiconductor industry is possible because of minute concentrations of point defects that are added to Si (dopants determine the whole material electrical properties: if it’s n-type, p-type, or semi-insulating).

## Slide 35: Point defects
Types of point defects:
  Misplaced atoms & Solute atoms (substitutional defects: atoms or ions are replaced by others),
  Vacancies (empty positions),
  Interstitials (atoms or ions present on any site that would be unoccupied in a perfect crystal),
  Electronic defects (electrons and holes),
  Associated centers (two point defects which interact so that they can be considered as a single defect; if more atoms are involved, they would be called a defect cluster or a defect complex).

## Slide 36: Solid Solutions
If a material crystallizes in the presence of foreign atoms, their inclusion in the main crystalline structure could:
  Increase significantly system’s energy  foreign atoms would be almost completely excluded from forming crystalline structure
  Decrease considerably system’s energy  there would be the development of a new crystalline form
  In intermediate cases, foreign atoms would fit in a random way in the forming crystalline structure  SS
SS are stable, of course, when the mixed crystal has a lower ∆Gformation than the other 2 alternatives.

## Slide 37
Let’s try to apply Quasi – Chemical Approach rules to 2 real instances:
SS of calcium chloride (CaCl2) in sodium chloride (NaCl), which we would assume as a perfect crystal:
First of all, SS of CaCl2 in NaCl is indicated as follows:
MASS BALANCE:
Notes: CaCl2 = cloruro di calcio

## Slide 38
CHARGE BALANCE: being Ca++ the cation, it would probably substitute host Na+ cations, leading to an exceeding (+) charge  adding charges to previous equation:
but this equation doesn’t balance charges!! So…
SITE BALANCE: in this example the right ratio anionic/cationic sites is 1:1: our equation doesn’t balance lattice sites neither! So...

## Slide 39
REMARKS:
All balances are related to a perfect, neutral crystal.
Having charge separation, we expect the new crystal to be a better conductor…
The equation we wrote gives us a better knowledge of the system in an atomic scale:
e.g. we could represent it as:
[*] close enough to balance charges!
Notes: !!!

## Slide 40
SS of titania (TiO2) in magnesia (MgO), which we would still assume a perfect crystal
Mg has a double valence, while Ti has 4 (+) charges…
Notes: TiO2 = biossido di Ti

## Slide 41: Schottky Disorder
Simultaneous anionic and cationic vacancies.
Total stoichiometry of the solid isn’t compromised by Schottky disorders, because the number of empty M and X sites is balanced as to preserve local electro neutrality.
Opposite charged vacancies tend to associate (they carry an effective charge), so they’d never be too far-away from one another.
Schottky disorder formation “reaction”:

## Slide 42: Schottky Disorder
This is a common defect in alkali halides at high T.
In oxides vacancies ∆Gformation is 2x-3x ∆Gformation(alkali halides), so at equilibrium the number of S. disorders in not relevant until very high T.
Notes: alkali halides = alogenuri alchilici

## Slide 43: Frenkel Disorder
Auto-interstitial defect: there is the same number of reticular vacancies and interstitial atoms, cause reticular atoms migrate in interstitial positions.
e.g. halide: AgBr
e.g. oxide: Y2O3

## Slide 44: Frenkel Disorder
This is a common defect in:
  Crystals with fluorite structure, which has large interstitial sites.
  Crystals with high polarizable ions, which can in an easier way set up in interstitial sites.
The energy change for F. disorder formation depends strongly on reticular structure and ion characteristics.

## Slide 45: Some more examples

## Slide 46: SS of Ti02 in MgO
We wrote
for substitutional SS, but it could be also an interstitial SS:
Which one is better?
Evaluate ∆G° and choose the favorite!
Usually it is ∆Gi >> ∆GV  easier formation of vacancies than interstitials.

## Slide 47: SS of Ti02 in MgO
This specific instance follows that general rule, too, as the passage of atoms to interstitial positions requires quite high energies:
∆Hi >> ∆HV
 almost the entire part of defects will be substitutional:


## Slide 48: Zirconia doped with calcia
There are, again, 2 possibilities:
Zirconia has a Fluorite structure  lots of empty space inside  interstitials are not automatically privileged…
So??
1
2

## Slide 49: Zirconia doped with calcia
Let’s consider the profiles of density in function of mole % of CaO in ZrO2 (at Tamb):
Experimentally, reaction  is the favourite.

## Slide 50: Lambda sensor (or oxygen sensor)
Notes: NOTA: con la zirconia drogata con calcia ci fanno le sonde lambda

## Slide 51: Zirconia doped with yttria
Applications of pure zirconia are restricted because it shows polymorphism:
  It is monoclinic at room temperature
  Changes to the denser tetragonal phase from circa 1000 °C.
The phase change t-ZrO2  m-ZrO2 shows a large change in volume (∆V=5%) which causes extensive cracking.
The addition of some oxides (like CaO, Y2O3) results in (meta)stabilizing the t-phase (or c-phase) at room temperature.
Notes: Note (zirconia):
si hanno meno vacanze che con il drogaggio di CaO, x qsto x le sonde lambda si usa la CaO, mentre l’yttria si usa cm stabilizzante
extensive cracking = rottura estensiva, ampia, grande

## Slide 52: Yttria-stabilized Zirconia
Cubic zirconia (or CZ) : hard, optically flawless and usually colorless (but may be made in a variety of different colors).
Single crystals of the cubic phase of zirconia are commonly used as diamond simulant in jewellery.
Notes: Nota:
This state of zirconia is commonly called "cubic zirconia," "CZ," or "zircon" by jewellers, but the last name is not chemically accurate. Zircon is actually the mineral name for naturally occurring zirconium silicate (ZrSiO4).

## Slide 53: Magnesia doped with lithium fluoride
Magnesia doped with alumina

## Slide 54: Quasi – Chemical Approach Constant of Reaction

## Slide 55
There’s a need of a more immediate way to estimate defect concentration in crystals.
Applying:
  Kröger – Vink notation
  Quasi – Chemical approach
to equations that represent defect formation’s processes
A “constant of reaction” for those equation can be defined.

## Slide 56
With e.g. :
Defining:

Notes: NB: n(O) = n°siti di O
n(Mg) = n°siti di O
n(MgO) = n°siti di O

## Slide 57
So:
(where activity of solute specie is at the denominator)
And, going on with the “Quasi – Chemical” approach:
Where ∆G° is energy change associated with the dissolution process of TiO2 in MgO
 (1)

## Slide 58
ENC (Electro Neutrality Condition):
 
Finally, the (1) becomes:
(2)
which permit to ESTIMATE DEFECTS CONCENTRATION
NOTE:
Notes: Nota: n(Mg) = n°siti di O

## Slide 59: Phase Diagram
In the phase diagram:
From equation [2] we can also obtain an expression for the SOLVUS LINE (remembering that, for solids, at equilibrium activity is 1).
Notes: All’equil (=> sulla linea di solvus) attività =1
Nota: => lungo una linea di composizione se e.g. aumento la T allora l’attività, com’è logico, dv cambiare!

## Slide 60: Phase Diagram
So, when you come down on a composition line:
activity changes till when you reach the solvus line  then in the microstructure you’ll have precipitation of TiO2.
Notes: Nota: => lungo una linea di composizione se e.g. aumento la T allora l’attività, com’è logico, dv cambiare!

## Slide 61: Some examples

## Slide 62: Schottky Disorder in magnesia
With:
Notes: Note:
Mg si estrae dal mare cm MgO  (1g Mg)/(m3 H2O mare) xké è la soluzione energeticam + conveniente (risp all’estrazione dai silicati di Mg)
7.5 eV/mol vac è molto alta

## Slide 63: Schottky Disorder in magnesia
So, at T = 2,000 K  [V] ≈ 10-9
 in 1 mol there’ll be ≈ 10+14 defects.
NB: in a real crystal, there’ll be, in any case, AT LEAST 1016 – 1017 defects/mol
 [V] ≈ 10-6 – 10-7
Notes: NB:
nO = n°siti di O, nMg = n°siti di Mg, nMgO = n°siti di MgO
2) n V(Mg)=n V(O) =nV
[VMg]=[VO] =[V] =>
nMg=nO =nMgO

## Slide 64: Schottky Disorder in alumina
With:

## Slide 65: Schottky Disorder in alumina

## Slide 66: Schottky Disorder in alumina
So:
  1 Schottky disorder in alumina disarranges 5 points in crystal structure (3 VO and 2 VAl)
  1 Schottky disorder in magnesia (previous example) disarranges 2 points in crystal structure (1 VO and 1 VMg)

## Slide 67: Schottky disorder’s energy of formation
SPECIE | ∆HS [eV]  E/defect [eV] | 
Al2O3 | 25 | 5
MgO | 7.5 | 3.75
CaO | 6.1 | 3.05
NaCl | 2.30 | 1.65
KCl | 2.26 | 1.1
LiF | 2.34 | 1.17
LiCl | 2.12 | 1.1
LiBr | 1.80 | 0.9
LiI | 1.30 | 0.7
more stable

## Slide 68: Frenkel Disorder in urania
NB: thank to the low defect concentration, [UU] is SUBSTANTIALLY 1.

## Slide 69: Frenkel Disorder in urania
As urania has a fluorite structure it is:

## Slide 70: Fuel rods for nuclear reactors
Notes: Barre combustibili x reattori a fissione nucleare

## Slide 71: Frenkel disorder’s energy of formation
STRUCTURE | MATERIAL – interstitial | ΔG [eV]
Rocksalt str. | MgO – Mg | 13.5
 | MgO – O | 17.6
Corundum | Al2O3 – Al | 14
 | Al2O3 – O | 16.5
Fluorite str. | UO2 – U | 3.4
Fluorite | CaF2 – Ca | 2.8
till 147 °C: wurtzite (over 147 °C: CBC and there is also a metastable form, with sphalerite str.) | AgI – Ag | 0.75
Oxygen has also a bigger steric effect

## Slide 72: Concentrations of charge carriers (electrons and holes)

## Slide 73
Consider a regular periodic arrangement of atoms in which each atom contains more than one electron (eg Si).
Suppose the atom in this imaginary crystal contains e- up through the n=3 energy level.
If the atoms are initially very far apart , the e- in adjacent atoms will not interact and will occupy the discrete energy levels.
Schematic of an isolated Si atom

## Slide 74
If these atoms are brought closer together, somehow (quantum mechanics), their quantized energy levels split and turn into many states grouped in “energy bands” (see diagrams)
Conduction only happens if electrons have empty “states” available at nearby energy
Splitting of the s and p states of Si into the allowed and forbidden energy bands

## Slide 75
Considering an intrinsic semiconductor we have:
When an e- springs from VB to CB, it leaves a hole in VB
Notes: S.C. intrinseco = senza difetti, quindi un cristallo perfetto, per cui il livello di Fermi è esattamente a metà tra il limite sup della BV e il limite inf della BC

## Slide 76
According to Quasi – Chemical approach it’s possible to represent this process as:
where:

## Slide 77
We have that
This is a number little lower than the number of atoms in 1 CC
So almost every atom contributes with one state

## Slide 78
If, as supposed, the S.C. is intrinsic, we can obtain the concentrations of charge carriers equation:

## Slide 79
Some EGAP values for ceramics:
(Ceramics Science and Technology: Properties; Volume 2; Ralf Riedel, I-Wei Chen)
Pay attention!! There are direct and indirect S.C.s, which means they may have respectively a direct or indirect transition…
Ceramic | Energy gap [eV]
Al2O3 | 7
Si | 1.1
Single crystal ZnO | 3.2
Cd doped ZnO | ~3.0
Mg doped ZnO | ~4.0
Single crystal TiO2 | 3.23

## Slide 80
Direct transition
Indirect transition
Notes: Slides 15-16 lez 24-26 fisica
Gamma = punto di max in BV

## Slide 81
Why did we evaluate ∆H (instead of ∆G)?
Usually ∆G° is due mostly to system’s free energy, as:

## Slide 82
qualitatively:
If it is:

## Slide 83
[UU] is SUBSTANTIALLY 1:
Given a generic compound MAXB ,
With, e.g. 109 atoms of M:
Notes: Sistemare animazioni

## Slide 84: Non-stoichiometry in Kroger Vink Notation
Cd1-xO is non-stoichiometric (and this is due to the fact that more than one oxidation state is available for Cd)
+
+
Nc density of states in the conduction band
Nv density of states in the valency band
NA Avogadro’s number
PM molecular weight of CdO

## Slide 85: Kroeger-Vink diagram for metal oxide semiconductor MO
Schottki defects dominate Electronic defects dominate

## Slide 86: Famous case of non-stoichiometric compounds: ceramic superconductors
YBa2Cu3O7-x

## Slide 87: Properties of Ceramics

## Slide 89: Melting temperatures

## Slide 91: Heat capacity
Notes: Substantially independent on crystal structure. Energy is absorbed by 1) rotation or vibration of atoms and group pf atoms, 2) by electronic transitions and 3) change in atom positions during formation of defects. No matter how these contribution is partitioned, the overall sum is substantially constant for materials.
The effect is important for mass: easier to heat porous materials than bulk ones -> furnaces are lined, when possible, with porous or fibrous materials.

## Slide 92
Notes: Thermal conductivity k is proportional to heat capacity, number of carriers (electrons or phonons) and mean free path.
Metals have large number of electrons and large mean free path so usually they have large conductivities. Alloying reduces conductivity.
Single element ceramic (diamond and graphite) have high conductivities, as well as compounds with similar atomic weight because phonons are not disturbed and have large mean free path.
Solid solutions decrease the thermal conductivity of ceramics.

## Slide 93: AlN contains always some Al2O3. Industrially some CaO or Y2O3 is added, which reacts with Al2O3 but then it remains isolated in triple junctions
Notes: Reason why commercial AlN has lower thermal conductivity than expected is the ubiquitous presence of Al2O3.

## Slide 94: Thermal condutivity for binary systems

## Slide 95
Notes: Thermal diffusivity is thermal conductivity divided by density and by heat capacity at constant pressure.

## Slide 96
Thermal expansion
Definition of
Thermal Expansion Coefficient

## Slide 97: Thermal expansion

## Slide 98
If grains are too large, fractures due to thermal expansion mismatch can occur also in pure compunds if they have thermal expansion anysostropy.

## Slide 100: Preparazione di uno specchio telescopico in vetroceramica ZERODUR della Schott: CTE 0,02x 10-7 k-1 (0° - 50° C)

## Slide 101: Young’s modulus

## Slide 102: Poisson’modulus: it is the ration of the transverse strain (x) to the axial strain (y)

## Slide 103: Rigidity modulus: it is the ratio of the shear stress to the shear strain
L

## Slide 104: Bulk modulus: it is the ratio of the isostatic stress (pressure) to the volumetric strain
K

## Slide 105: Relations among elastic constants
E , Young modulus
n , Poisson modulus
G, Rigidity (shear) modulus
K, bulk modulus
n ) E=3K(1-2 n )
E=9KG/(3K-G) n =(3K-2G)/(6K+2G)

## Slide 106: Importance of TEC: Stress build-up
Material 1
Material 2
T0 ,
compression
Tension
If materials are joined together there must be displacement compatibility,
which generates stresses

## Slide 107: Asby map Young modulus/density

## Slide 111: Strength
Tensile tests with and without luders behaviour
https://www.youtube.com/watch?v=D8U4G5kcpcM

## Slide 112: Ashby map strength/density

## Slide 113: Ashby map strength/density

## Slide 123: Accurate determinations of KlC

## Slide 127: ISB determination of Klc

## Slide 131: Creep tests
https://www.youtube.com/watch?v=k8Py4-SdjyU

## Slide 134: Flow mechanism in creep

## Slide 135: Typical exponents for GS and stress

## Slide 136: Nabarro Herring Deformation maps

## Slide 137: Ashby map Therm. Expan./therm Conduc

## Slide 138: Thermal shock resistance
Thermal shock testing of Schott glasses

## Slide 139: Stress data for Weibull plot

## Slide 140: Data from SKF