## Slide 1
Weimarn’s law
D x C0 = constant
C0 = initial concentration
D = particle dimention
Cs = solubility
L1’ > L1” > L1”’ = solubility
When C0 is high = the precipitation is controlled by nuclei formation
When C0 is small = the precipitation is controlled by the rate of nuclei growth
Precipitation/coprecipitation

## Slide 2: Factors influencing precipitate formations

## Slide 3: Precipitation/coprecipitation
Effect of Temperature and Concentration on the precipitation of CaCO3
(a) Calcite (T<25°C)
Ca(HCO3)2 (aq)  CaCO3  + H2O + CO2
(b)Aragonite (70-80°C)
(c) Vaterite (T> 40°C high concentration)

## Slide 4: Precipitation/coprecipitation
Ca(OH)2
CaCl2 (aq)+2 NaOH (aq)  Ca(OH)2 (s) + 2 NaCl (aq)

## Slide 5: Precipitation/coprecipitation
Addition of NaOH to a CaCl2/H2O/methanol solution
Adsorption of •OCH3 on the 001 facets with the suppression /inhibition of their growth

## Slide 6: Precipitation by increasing pH
:
  increasing the pH (one element to precipitate)
  at constant pH (the most used case)
  at constant pH in a continuous flow

## Slide 7: Colloidal Chemical Methods
Examples: Gold
  A common method for preparing colloidal gold nanoparticles involves combining hydrogen tetrachloroaurate (HAuCl4) and sodium citrate (Na3C6H5O7) in a dilute solution.
  Upon dissociation, the citrate ions (C6H5O73-) reduce Au3+ to yield 30-40 nm gold particles.

## Slide 8: Formation of Gold Nanoparticles
Heat a solution of chloroauric acid (HAuCl4) up to reflux (boiling). HAuCl4 is a water soluble gold salt.
Add trisodium citrate, which is a reducing agent.
Continue stirring and heating for about 10 minutes.
  During this time, the sodium citrate reduces the gold salt (Au3+) to metallic gold (Au0).
  The neutral gold atoms aggregate into seed crystals.
  The seed crystals continue to grow and eventually form gold nanoparticles.
HAuCl4
Gold
NP
HAuCl4
Sodium
Citrate
Heat
Red Color = Gold NP
J. Chem. Ed. 2004, 81, 544A.

## Slide 9: Formation of Gold Nanoparticles
Reduction of gold ions: Au(III) + 3e- → Au(0)
Nucleation of Au(0) seed crystals:
Seed Crystal
10’s to 100’s of Atoms
Nanorods
Spherical
Nanoparticles
Isotropic
Growth
Anisotropic
Growth
Surface capped
with citrate anions
Adding surfactant to growth solution
caps certain crystal faces and promotes
growth only in selected directions.
Growth of nanoparticles:
Seed

## Slide 10: Colloidal Gold Nanorod Clusters
A seed solution of gold nanoparticles was prepared by borohydride (30 mM, 0.3 mL) reduction of HAuCl4 (0.25 mM, 5 mL) in aqueous cetyltrimethylammonium bromide (CTAB) solution (0.1 M).
2. An aliquot of seed solution (24 μL) was added to a growth solution (10 mL) containing CTAB (0.1 M), HAuCl4 (0.5 mM), ascorbic acid (0.8 mM), …... Mixtures were left undisturbed for 4 h at 27 °C.
Langmuir 2012, 28, 24, 8826-8833

## Slide 11: Colloidal methods : Molybdenum
  1-5 nm molybdenum nanoparticles can be created at room temperature by reducing MoCl3 in a toluene solution in the presence of sodium triethylborohydride (NaBEt3H).
  MoCl3 + 3NaBEt3H  Mo + 3NaCl + 3BEt3 + (3/2) H2
The main applications of molybdenum nanoparticles are as additives in alloys for hi-tech applications, such as high-vacuum or corrosive environments.
Some of these areas are as follows:
- High-temperature lubrication;
- Hard alloys, cutting tools, textiles;
- Microelectronics films;
- Sintering additives, coatings, plastics, nanowire and nanofiber;
- High-power vacuum valve, heater tube and X-ray tube.

## Slide 12: Colloidal methods: Iron
  3 nm Fe nanoparticles produced by reducing FeCl2 with sodium borohydride (NaBH4) in xylene.
  Trioctylphosphine oxide (TOPO) was introduced as a capping agent to prevent oxidation and aggregation.
Phys. Chem. Chem. Phys., 2001, 3, 1661-1665
TEM image of Fe nanoparticles

## Slide 13: Colloidal methods : Iron
Nano zero-valent iron for groundwater cleanup, have been deployed at full-scale cleanup sites
NaBH4 (0.2 M) is added into FeCl3•6H2O (0.05 M) solution (~1:1 volume ratio). Ferric iron is reduced via the following reaction:
4 Fe3+ + 3BH4 − + 9H2O → 4Fe0 + 3H2BO3− + 12H+ + 6H2
https://nanoiron.cz/en/

## Slide 16: Colloidal methods : M/Fe core-shell nanoparticles
Palladized Fe particles are prepared by soaking the nanoscale iron particles with an ethanol solution of 1wt% of palladium acetate ([Pd(C2H3O2)2]3). This causes the reduction and deposition of Pd on the Fe surface:
Pd2+ + Fe 0 → Pd0 + Fe2+
Similar methods may be used to prepared Fe/Pt, Fe/Ag, Fe/Ni, Fe/Co, and Fe/Cu bimetallic particles. With the above methods, nanoparticles of diameter 50-70 nm may be produced. The average specific surface area of Pd/Fe particles is about 35 m2/g.