## Slide 1: Physisorption, surface area and porosity

## Slide 2
100 Kg H2O
V = 100 L
V = a3 = 100 dm3 a = 4.64 dm
Surface 6 x a2 = 129 dm2
Vi = 1 L
Vi = ai 3 = 1 dm3 a = 1 dm
Total surface 100 x 6 x ai 2
= 600 dm2
100 Kg H2O
1 cube
100 cubes

## Slide 3
Physisorption and chemisorption

## Slide 4
PHYSISORPTION | CHEMISORPTION
WEAK, LONG RANGE BONDING Van der Waals interactions (e.g. London dispersion, dipole-dipole).. | STRONG, SHORT RANGE BONDING Chemical bonding involving orbital overlap and charge transfer.
NOT SURFACE SPECIFIC Physisorption takes place between all molecules on any surface providing the temperature is low enough. | SURFACE SPECIFIC Marked variation between crystal planes E.g. Chemisorption of hydrogen takes place on transition metals but not on gold or mercury.
DHads = 5 ….. 50 kJ mol-1 Related to factors like molecular mass and polarity (i.e. ~ heat of liquefaction) | DHads = 50 ….. 500 kJ mol-1 Wide range (related to the chemical bond strength)
Non activated with equilibrium achieved relatively quickly. Increasing temperature always reduces surface coverage. | Can be activated, in which case equilibrium can be slow and increasing temperature can favour adsorption.
No surface reactions. | Surface reactions may take place:- Dissociation, reconstruction, catalysis.
MULTILAYER ADSORPTION BET Isotherm used to model adsorption equilibrium. | MONOLAYER ADSORPTION Langmuir Isotherm used to model adsorption equilibrium..
Adsorption and Reaction at Surfaces

## Slide 7
Type I Pores are typically microporus with the exposed surface residing almost exclusively inside the microspores, which once filled with adsorbate, leave little or no external surface for further adsorption.
Type II Most frequently found when adsorption occurs on nonporous powders or powders with diameters exceeding micropores. Inflection point occurs near the completion of the first adsorbed monolayer.
Type III Characterised by heats of adsorption less than the adsorbate heat of liquification, adsorption proceeds as the adsorbate interaction with an adsorbed layer is greater than the interaction with the adsorbent surface.
Type IV Occur on porous adsorbents with pores in the range of 1.5 – 100nm. At higher pressures the slope shows increased uptake of adsorbate as pores become filled, inflection point typically occurs near completion of the first monolayer
Type V Are observed where there is small adsorbate-absorbent interaction potentials (similar to type III), and are also associated with pores in the 1.5 –100 nm range.
Type VI The reversible stepwise Type VI isotherm is representative of layer-by-layer adsorption on a highly uniform nonporous surface.

## Slide 12
IUPAC
Classification
Macroporous
> 50nm
Mesoporus
2-50 nm
Microporus
< 2nm

## Slide 13
Where...
Pv = equilibrium vapor pressure
Psat = saturation vapor pressure
H = mean curvature of meniscus
g = liquid/vapor surface tension
Vl = liquid molar volume
R = ideal gas constant
T = temperature

## Slide 14
Hysteresis

## Slide 15
Heterogeneity of pores

## Slide 16
Heterogeneity of pores

## Slide 17
Adsorption
Kinetic behavior of the adsorption process
Rate of arrival of adsorption is equal to the rate of desorption
Heat of adsorption was taken to be constant and unchanging with the degree of coverage, θ

## Slide 18
Langmuir Assumption
Gas molecules behave ideally
Only 1 monolayer forms
All sites on the surface are equal
No adsorbate-adsorbate interaction
Adsorbate molecule is immobile

## Slide 19
Langmuir Isotherm
An isotherm describes the dependence of volume, concentration , or in the case of a surface, coverage q, on pressure p at constant temperature T at equilibrium.
q = [ƒ(p)]T
p
q
In the equilibrium between the gas phase and the adsorbed phase, LeChatelier's Principle predicts that at constant temperature an increase in pressure will increase the number of molecules adsorbed on the surface since the volume occupied by the molecules at the surface (per mole) is smaller.
This can, however, reach a limiting value. The number of molecules adsorbed at any pressure p will also depend on the strength of the adsorbate bond to the surface.

## Slide 20
Langmuir’s “checkerboard” model of adsorption assumes that a surface is composed of a finite number of equivalent adsorption sites.
So the maximum coverage is obtained when all sites are filled. The coverage  is expressed in terms of the number of molecules adsorbed in relation to the number of available sites. i.e. When all sites are filled,  = 1.
Langmuir Isotherm
Consider the equilibrium:
Agas Aadsorbed
p

The Rate of adsorption is proportional to:
The number of surface collisions n from the gas phase
per second, which is proportional to the pressure p .
2) area of bare surface available for adsorption (1 - ).
ie. rate of adsorption = kads P (1 - )
kads

## Slide 21
Langmuir Isotherm
Consider the equilibrium:
Agas Aadsorbed
p

Rate of desorption proportional to:
1) the fraction of surface covered by adsorbate .
i.e rate of desorption = kdes 
kdes

## Slide 22
kads p (1 - ) = kdes 
At equilibrium
Rate of adsorption = Rate of desorption
If we write b = kads / kdes
 = bp / (1+bp) ……….. The Langmuir Isotherm

 = 1
p
b = 10
b = 100
b = 50
Since b = kads / kdes , this is the same as an equilibrium constant K
And since ln K = -DG/RT one can write:
b = exp (-DG/RT ), i.e b reflects the strength of the adsorbate bond to the surface.
Since  = nads / nmax
p / nads = 1 / b nmax + p / nmax

## Slide 23
“finite number of equivalent adsorption sites”
Langmuir Isotherm
Limitations and approximations
different surface adsorbate structures
surface reconstruction

## Slide 24
“finite number of equivalent adsorption sites”
Langmuir Isotherm
Limitations and approximations
lateral interactions between adsorbates
Enthalpy of adsorption DHads
depends on site/coverage

## Slide 25
Langmuir Isotherm
Limitations and approximations
rate of adsorption = kads p (1 - )
X
assumes collision at a vacant site is required for adsorption

rate of adsorption i.e. sticking probability (S)
S a (1 - )
precursor kinetics

## Slide 26
1. gas molecules physically adsorb
on a solid in layers infinitely;
2. gas molecules only interact
with adjacent layers; and
3. the Langmuir theory can be applied to each layer.
4. the enthalpy of adsorption for the first layer is constant and greater than the second (and higher).
5. the enthalpy of adsorption for the second (and higher) layers is the same as the enthalpy of liquefaction.
The concept of the B.E.T. theory is an extension of the Langmuir theory, which is a theory for monolayer molecular adsorption, to multilayer adsorption with the following hypotheses

## Slide 27
Physisorption
Brunauer, Emmett and Teller – BET Theory
* Multilayer adsorption
* Dynamic equilibrium
Second layer
First layer
1.
2.
3.
4.
qo Fraction of surface unoccupied
A1 condensation coefficient (adsorption probability)
Nm n° of molecules in a monolayer
E1 Energy of adsorption
n1 adsorbate’s vibrational frequency

## Slide 28
nth layer
Assuming n, E and A constant for 2nd, 3rd,…nth layer (liquid state)
L heat of liquefaction
5.
6.
7.

## Slide 29
7.
8.
9.
10.
11.
12.
13.
14.

## Slide 30
The total number of molecules adsorbed at equilibrium is
Substituting for q1, q2 , …
Since a and b are constant
15.
from 11-14.
16.
17.
18.
from 7-10.

## Slide 31
Substituting in 16.
19.
20.
1 = q0 + q1 + q2 +.....qn
21.
22.
Substituting 22 into 20
23.

## Slide 32
Replacing qn in 23. with abn-1qo from 14.
24.
Replacing a in 24. with Cb from 17.
Since
25.
26.
27.

## Slide 33
From 20.
Substituting 28 in 27.
28.
29.
30.
Introducing qo from 30. into 20
31.
= 1 when
N/Nm = infinite
Condensation on the surface or P/P0 = 1

## Slide 34
Considering Eq. 10 for P/P0 = 1 , b= 1 when
32.
33.
Introducing b into 31.
34.
Recalling that N/Nm = n/nm

## Slide 35
Brunauer Emmett and Teller (BET equation):
n amount of adsorbate (g) at the pressure P
nm amount of adsorbate corresponding to the formation of a monolayer
C BET constant
P0 saturation pressure
Mw è Molecular weight of the adsorbate Na Avogadro Number am “cross section area” of the adsorbate.