## Slide 1: Chemisorption, surface area and metal dispersion

## Slide 2: 1.1% Pt/g-Al2O3
Adsorbimento a 573 K di H2. Curva (a) adsorbimento su 2.031 g di catalizzatore, (c) adsorbimento su 1.00 g di Al2O3, (d) adsorbimento su quantità di supporto corrispondente a quella del campione (2.00 g) ed espressa nella stessa scala della curva (a), (b) differenza tra la curva a e d.

## Slide 3
Metallic Dispersion (DM)
metal surface atoms
total metal atoms
In the case of a sphere
S / V = (4 p r2 )/ (4/3 p r3) = 3/r
r = 3 V / S d = 2r = 6 V /S
In the case of a cube, the Surface to Volume ratio is
S / V = 6 a2 / a 3 a = 6 V / S
Mean diameter of a metal particle

## Slide 4
Metallic Dispersion (DM)
metal surface atoms
total metal atoms
Mean diameter of metal particles ( spherical geometry)
= 6 V/A
area of a metal atom
volume of a metal atom in the "bulk"
atomic weight,  density Avogadro’s number

## Slide 5
M

## Slide 6
Sample pretreatment and chemisorption
We need metals to get chemisorption!!
Wet Synthesis –exposure to air. Nanoparticles surface oxidation state ? Passivation ?
Pre-reduction: typically diluted hydrogen (flow vs static, Temperature and conditions that do not change nanoparticle size/morphology) based on TPR
Degassing conditions – Removal of gas phase and chemisorbed hydrogen (up to 350-400°C)

## Slide 7
Thermoanalytical techniques
measurement of a physical or chemical property of a solid as the temperature of the solid is varied in a predetermined manner
temperature programmed
Material Characterization by
Temperature Programmed Methods

## Slide 8
Thermoanalytical techniques
Techniques dependent on dimensional changes
Techniques dependent on evolved gases
Techniques dependent on gas analysis from chemical reaction
DILATOMETRY
Techniques dependent on weight changes
Thermogravimetry
Techniques dependent on energy changes
Diff. Thermal analysis
Diff. Scanning calorim.
Temp. prog. desorption
Temp. prog. reaction
Temp. prog. reduction
TPD, TPDE, TPSR
TPRE, TP...
TPR/TPO

## Slide 9
temperature programmed desorption/decomposition
time
coverage
temperature
rate
Pretreatment of the material
Exposure to reactant gas
Desorption of physisorbed fraction
Heating of sample in an inert gas stream
Analysis of desorbed components

## Slide 10
temperature programmed reduction/oxidation
time
Degree of
reduction
temperature
reduction
rate
Pretreatment of the material
Heating of sample in the presence of reducing or oxidizing mixture
Analysis of reductant or oxidant consumption
MO(s) + H2(g) M(s) + H2O(g)
M(s) + O2(g) MO(s)

## Slide 11
temperature programmed reaction
Coadsorption of two gases and heating in inert carrier
Adsorption of one component and heating in reactive carrier gas
Heating in reactive atmosphere containing reagents
Temperature programmed methanation, hydrogenation, sulphidation, combustion…….

## Slide 12
CO
CO
CO
CO
CO
CO
CO2
CO2
CO2
O
O
CO
CO
CO
CO
CO
CO2
CO2
CO2
TPD
TPDE
TPRE
desorption vs decomposition vs reaction

## Slide 13
Characterization of reducibility of materials
Determination of binding energy of adsorbed molecules
Acidity
Characterization of surface carbon deposits
Physical parameters (surface area, dispersion…)
information that can be obtained…

## Slide 14
Experimental:
apparatus for TP studies
introduction of reactants
furnace and reactor
detector
data acquisition
time/temp.
concentration

## Slide 15
Experimental: Detector and data acquisition
Thermal conductivity detector
 Good for TPO/TPR
 Non specific gas analysis
 Concentration can be monitored continuously
Mass spectrometer
 Concentration can be monitored continuously
 Specific gas analysis
 High cost
Micro GC
 Concentration cannot be monitored continuously
(delay 1-2 min.)
 Complex gas analysis
 Accurate quantitative evaluation