## Slide 1: Pyrolysis: Industrial method for many products
Carbon Black
TiO2
SiO2
Tires
Inks
Paints
Makeup
Optical
fibers
Carbon black - 8 million tons $8 billion
TiO2 - 2.5 million tons, $5 billion
SiO2 - 2.0 million tons, $2 billion

## Slide 4
A precursor (liquid or gas) is forced through an orifice at high pressure and burned.
The resulting ash is collected to recover the nanoparticles.
Large volume of gas leads to high rate of material synthesis.
Pyrolysis: popular method for creating nanoparticles, especially oxides
Versatile
Large Variety of precursors
Controllable
Scalable
Aggregation
Condensation
Coagulation
Nucleation
Droplet evaporation
Flame Spray Pyrolysis (FSP)

## Slide 5
Pyrolysis: System Overview

## Slide 6
Aggregates and Agglomerates:
Aggregate – An assemblage of particles rigidly joined together by chemical or sinter-forces.
Agglomerate – A loosely coherent assembly of particles and/or aggregates held together by weak interactions
  Aggregates Agglomerates
Pyrolysis

## Slide 7
TiO2
Monomers
Transient Hard
Agglomerates
Spherical
Particles
Hard Agglomerates
Soft Agglomerates
Pyrolysis: Agglomerate Formation Sequence
Distinction between hard and soft agglomerates is largely empirical.
Controlled agglomeration can minimize post-grinding and other costly separation techniques.

## Slide 8
Impact of oxygen
Aids in combustion
Provides chemistry in the reaction
Acts as a dilutent, cools the flame, prevents agglomeration
All of these variables can be decoupled by burner design. Which is cheaper than increasing oxygen flow.
Excess oxygen makes the flame burn cooler resulting in smaller diameter particles
Pyrolysis: Particle Size Controlled by O2 Flow

## Slide 9
Flame Pyrolysis
Particle Formation and Growth by Gas Phase Chemical Reaction, Coagulation, Sintering and Surface Growth:
O2
TTIP
Molecules
TiO2
Molecules
TiO2
Particles
Ti
C3H7O
C3H7O
OC3H7
OC3H7
Titanium-Tetra-Iso-Propoxide
TiO2
Aggregates
Decreasing Temperature

## Slide 10
Flame Pyrolysis: Jet Design
CH4
CH4
CH4
Air
Air
Air
TiCl4
TiCl4
TiCl4
TiCl4
Air
Air

## Slide 11
Effect of Oxidant Composition on TiO2 Morphology:
CH4
CH4
Oxidant
Oxidant
TiCl4
TiCl4
Flame mixing B
Flame mixing C
Flame Pyrolysis: Jet Design

## Slide 12
Flame Pyrolysis: Nozzle Quenching
Vapor
Flame length is controlled by rapid quenching
Prevents agglomeration by inhibiting growth processes in the early stages of growth.
Provides precise control of particle size
Desired

## Slide 13
Nozzle Quenching controls flame length and particle size.
Flame Pyrolysis: Nozzle Quenching

## Slide 14
Flame Pyrolysis: Nozzle Quenching
TiO2 Particle Size Control by Nozzle Quenching

## Slide 15
Pyrolysis: Electrostatic Charging
Particle size can also be controlled by generating an electric field across the flame.
A large electric field (hundreds of kV/m) is generated between two plate electrodes situated on opposite sides of the flame.
Similar to nozzle quenching, the electric field limits particle growth by reducing the residence time in the high temperature region of the flame.
In addition, the electric field charges the particles. This results in electrostatic repulsion between newly formed particles, preventing coagulation.
S. Vemury, S.E. Pratsinis, L. Kibbey, Electrically-controlled flame synthesis of nanophase TiO2, SiO2, and SnO2 powders. JMR, Vol. 12, 1031-1042. 1997.

## Slide 16
Pyrolysis: Electrostatic Charging

## Slide 17
Pyrolysis is a high yield method that can fulfill the strong demand for nanoparticles.
Can be customized to produce unique nanoparticles.
Broad distribution of particle sizes and morphology.
Flame Pyrolysis: Advantages & Disadvantages

## Slide 18
Spray Pyrolysis
An aerosol process that
atomize a solution and
heats the droplets to
produce solid particles.
Simple and low cost for powder and thin film deposition process
Applicable to large areas;
No need of exotic or expensive precursors;
No need of vacuum.

## Slide 19
Spray Pyrolysis
Metals (Cu, Ni, Co,…) and metal oxides powders
Converting microsized liquid droplets of precursors or precursors mixture into solid particles trough heating
Droplets  evaporation  solute condensation  decomposition & reaction  sintering
e.g. silver particles made from Ag2CO3 or AgNO3 with NH4HCO3 @ 400 °C

## Slide 20
Spray Pyrolysis
The precursor must be dissolved in the liquid, but not react with it.
The product must not dissolve in the liquid, and must not react with the liquid.
There must be a large volume decrease for the reaction of precursor to product.
Transport of the leaching agent in the liquid and the fugitive compounds formed must be sufficiently rapid.

## Slide 21
Spray Pyrolysis Advantages
Spherical morphology
Narrow particle size distribution
Easy preparation of powders with complex formation
Relatively homogeneous composition
Continuously production
Reaction occurs at the microcapsule reactor (droplets)

## Slide 22
Spray Pyrolysis limitations
Technique is quite empirical, with a number of variables that can affect the final product:
- solute concentration
- atomization technique
- temperature, temperature gradient
- residence time in furnace
- carrier gases

## Slide 23
Spray Pyrolysis

## Slide 24
Spray Pyrolysis
Nozzle to substrate distance
Droplet size: relates to size of product
Substrate temperature
Solution concentration
Solution flow rate
Atomization rate – affects scalability of the process
Droplet velocity – affects residence time with the furnaces and ultimately size particle

## Slide 25
Spray Pyrolysis

## Slide 26
Messing et al. J. Am.Ceram.Soc 1993
Spray Pyrolysis

## Slide 27
Droplet to particles conversion process
Spray Pyrolysis

## Slide 28
Heating Time, Heating Temperature

## Slide 29
Spray Pyrolysis

## Slide 30
Low temperature and high initial solute concentrations Dense particles (aggregates of nanocrystals)
High temperature and high solvent evaporation rate Hallow particles
Nanoparticle < 100 nm
Dilute solutions and
very small initial droplet size
Spray Pyrolysis

## Slide 31
Conventional Spray Pyrolysis

## Slide 32
Low Pressure Spray Pyrolysis

## Slide 33
Low Pressure Spray Pyrolysis

## Slide 34
Salt-assisted Spray Pyrolysis

## Slide 35
Conventional vs Salt-assisted Spray Pyrolysis
Conventional Salt-assisted

## Slide 36
Electrospray Pyrolysis
By applying a 3KV electric field to the liquid coming from a cylindrical tube, it becomes conic.

## Slide 37
Electrospray Pyrolysis

## Slide 38
https://www.youtube.com/watch?v=I4w0nlrVU94

## Slide 39
https://www.youtube.com/watch?v=hRDD4l1dzaI

## Slide 40
https://www.youtube.com/watch?v=mmtXFlIQD9E
Spray Process

## Slide 41
Spray Pyrolysis: nanofilm
https://www.youtube.com/watch?v=eJbuY4HJFV0

## Slide 42
Flame Spray Pyrolysis: nanofilm
https://www.youtube.com/watch?v=pAYsH7xnV6s