## Slide 1: Single point BET

## Slide 2: 6 way valve and a loop for gas injection

## Slide 3
ADSORPTION PLOT for Ce0.5Zr0.5O2

## Slide 4: Chemisorption, surface area and metal dispersion

## Slide 5
Chemisorption for probing metal surface areas
Objective
determine number of accessible metal sites
Exploit high reactivity of metal surface atoms
- let them react with small molecules (H2, O2, CO, etc.)
- count the number of molecules that have reacted
- knowing the stoichiometry of the reaction you obtain the number of metal surface atoms
Choice of the probe molecule
- must be selective for reaction with metal vs. support
- must be selective for reaction with surface atoms (not with bulk)
- reaction must be «irreversible»

## Slide 9
n = number of surface metal atoms that are occupied by the chemisorption of a gas molecule.
ex : H2 on Pt : n = 2 because of dissociative adsorption: 1 molecule H2 dissociates to 2 H atoms adsorbed on 2 Pt atoms
v adsorbed gas volume
Vm volume of a mole of metal atom
Na Avogadro’s number
S surface of one metal atom
Metal surface atoms (N(s)M) and metal surface area (SM)

## Slide 10
Chemisorption stoichiometry
Nanoparticle < 1nm  n < 2
corner atoms are usually more active than atoms on the flat surfaces
stoichiometry of chemisorption may also change

## Slide 11
Rh/Al2O3

## Slide 12
Chemisorption and Physisortion: the role of support in nanocomposites
Pressure
Gas adsorption
Physisorption is investigated at 77 K but occurs at higher temperature

## Slide 13
Chemisorption and Physisortion: the role of support in nanocomposites
Pressure
Adsorption

## Slide 14: 1.1% Pt/g-Al2O3
Adsorbimento a 573 K di H2. Curva (a) adsorbimento su 2.031 g di catalizzatore, (c) adsorbimento su 1.00 g di Al2O3, (d) adsorbimento su quantità di supporto corrispondente a quella del campione (2.00 g) ed espressa nella stessa scala della curva (a), (b) differenza tra la curva a e d.