## Slide 1
STRONG METAL/SUPPORT INTERACTION
(SMSI) EFFECT
S.J. Tauster et al; J. Am. Chem. Soc. 100, 170 (1978)
  Typically associated with reducible supports
  At low Tredn (200ºC) the material exhibits a
    “conventional” chemical behaviour
  At high Tredn (500ºC) strong perturbation of the
    chemisorptive and catalytic properties
  Reversibility. Reoxn. + mild Redn. allows to
    regenerate the material
Classic SMSI system: M/TiO2

## Slide 2
H/Rh Catalytic Activity*
Red. 200°C 0.43 17
Red. 500°C 0 0
Red. 500°C
Reox. 400ºC 0.23 7
Red. 200ºC
S. Bernal et al, Appl. Catal. 99, 1 (1993)
Rh(5%)/TiO2
SMSI Effect. Chemical Evidence
* Benzene hydrogenation (25ºC) (cm3 cyclohexane /gRh.s)

## Slide 3
Rh(5%)/TiO2
HREM micrograph
Catalyst reduced at 200ºC
3 nm
TiO2 – A [111]
Rh
High density of clean and well faceted Rh particles

## Slide 4
Rh(5%)/TiO2
HREM Micrograph
Catalyst reduced at 500ºC
3 nm
TiO2 – A [111]
Rh
TiO2-x migrates onto and partly covers the metal microcrystals (DECORATION)

## Slide 5
Rh(5%)/TiO2
At Tred = 500ºC:
A significant fraction of the Rh microcrystals look like clean (Partial Decoration)
Rh
HREM micrograph
Catalyst reduced at 500ºC

## Slide 6
Rh(5%)/TiO2
Reversibility of the SMSI Effect
TiO2 – R [110]
2 nm
Rh [110]
Reoxn. at 400ºC-500ºC followed by a mild reduction allows to recover the catalyst from the SMSI state
Red. 500ºC + Ox. 400ºC
+ Red. 200ºC

## Slide 7
Metal Decoration in Rh/Ce(M)O2-x
700 ºC < Tred < 900º C
Rh/CeO2 Red. 700ºC in H2

## Slide 8
Pt/CeTbOx Tred: 700ºC
Pt
0.34 nm
(111) sop.
soporte[011]
(111) Pt
Monocapa de soporte
8°
Pt [110]
Metal Decoration Effects in Pt/Ce(M)O2-x
700 ºC < Tred < 900º C
Simulated image
0.34 nm

## Slide 9
No evidence of formation of Rh-Ce intermetallics
3 nm
decoración
2.3
2.2
2.2
61°
54°
65°
3 nm
1.9
2.2
2.2
1.9
2.2
Nano-structure of HT (900ºC) reduced Rh
Tred  900º C
Twinned Rh particle.
Metal sintering on HT reduction
decoration

## Slide 10
Pt-Ce Alloying Phenomena
Tred > 900º C
5 nm
Pt/CeO2 Red. 1173 K en H2
4.66
3.02
4.22
90°
42°
[010] CePt5
CePt , CePt2
CePt5 , Ce3Pt2 , Ce7Pt3
Pt

## Slide 11
0 1 2 3 4 5 6
50
40
30
20
10
0
Frequency / %
Particle diameter / nm
TEM
H2 Chemisorption
EXAFS
dm = 2.5 nm
5 wt % Rh /Al2O3
J.Catal, 190, 2001, 182
Effect of the support on metal dispersion: Ce0.6Zr0.4O2 vs Al2O3

## Slide 12
0 1 2 3 4 5 6
50
40
30
20
10
0
Frequency / %
Particle diameter / nm
dm = 2.5 nm
dm = 1.2 nm
5 wt % Rh /Al2O3
5 wt % Rh /Ce0.6Zr0.4O2
J.Catal, 190, 2001, 182
Effect of the support on metal dispersion: Ce0.6Zr0.4O2 vs Al2O3

## Slide 13
J.Phys.Chem. B, 104,2000, 4667
Frequency / %
Particle diameter / nm
0
1
2
3
4
5
6
7
2.4 nm
2.4 nm
Effect of temperature on metal dispersion: Rh/Ce0.68Zr0.32O2
150°C

## Slide 14
Frequency / %
Particle diameter / nm
0
1
2
3
4
5
6
7
2.4 nm
2.4 nm
2.7 nm
J.Phys.Chem. B, 104,2000, 4667
150°C
500°C
Effect of temperature on metal dispersion: Rh/Ce0.68Zr0.32O2

## Slide 15
Frequency / %
Particle diameter / nm
0
1
2
3
4
5
6
7
2.4 nm
2.7 nm
4.2 nm
150°C
500°C
900°C
J.Phys.Chem. B, 104,2000, 4667
Effect of temperature on metal dispersion: Rh/Ce0.68Zr0.32O2

## Slide 16
Metal nanoparticle and chemisorption
Hydrogen spillover is the migration of hydrogen atoms from the metal catalyst onto the nonmetal support or adsorbate
Reducible oxides TiO2, CeO2
Apparent Dispersion >>> 100%
Low Temperature chemisorption (-90° C)
HR-TEM vs Chemisorption data

## Slide 17
Support
Noble metal
H2
Rh/CeO2 Reducibility

## Slide 18
CeO2 Reducibility

## Slide 19
Support
Noble metal
H2
H2 ads. (- 90ºC): DH = H/RhT
HREM: DHREM = RhS/RhT
DH / DHREM = H/RhS
J. Phys. Chem. B, 104, 2000, 4667
Rh/Ce0.68Zr0.32O2 Chemical deactivation

## Slide 20
Pd on Al2O3 and ZrO2 after treatment in 0.2 Torr O2 at 560°C
Rogriguez N.M. et al., J. Catal 157, 676-686 (1995)
PdO
Al2O3
Low Metal Loading
PdO
Al2O3
Pd
High Metal Loading
ZrO2
ZrO2
ZrO2
150°C
350 - 850 °C
> 890°C
PdO
PdO
PdO
Al2O3
Al2O3
Al2O3
150°C
350 - 650°C
> 800°C
PdO
PdO
“PdAlOx”

## Slide 21
Phase: Solid Solution
MHx
(0 < x < 0.1)
b Phase: Hydrides
MHx
( x = 1, 2, 3, ..)
Metal Hydrides and chemisorption
Metal : Al, Mg, Li, Be,….

## Slide 22
Pd nanoparticle and chemisorption
Pd bulk hydrides vs surface at room temperature
decomposes at 80 °C
Pd/Al2O3 H2 Chemisorption at 100 °C, low physisorption
Pd/CeO2 H2 Chemisorption ?? RT very low pressure
α-PdHx phase exists at x < 0.017
β -PdHx phase is realised for x > 0.58
intermediate x values correspond to α-β mixtures

## Slide 23
M/CeO2 based materials reducibility
TPR-MS profiles for fresh Rh/Ce0.68Zr0.32O2 (A), Pt/Ce0.68Zr0.32O2 (B), and Pd/Ce0.68Zr0.32O2 (C): H2 uptake (upper traces) and H2O evolution (lower traces).

## Slide 24
Pd nanoparticle and chemisorption at 25°C
(A) and the same sample oxidized at 427 °C and rereduced at 150 °C (B)