## Slide 1
Production of Syn-gas and Hydrogen

## Slide 2
Steam Reforming
Partial Oxidation
Autothermal Reforming
Aqueous Phase Reforming

## Slide 4
Today: Steam Reforming
Steam at high T
Ni based
Catalyst
Hydrocarbons
e.g. Methane
High metal loading
(Ni/Al2O3 until 15% wt)
High coking deposition
(catalyst deactivation)
High operative temperature
(highly endothermic reaction, 600-900 °C)

## Slide 5: Ni/Al2O3
Steam Reforming Mechanism
TEM picture
I. Alstrup, Haldor Topsøe A/S.
Catalyst deactivation:
C filament formation
Adsorption and dehydrogenation of CnHm on surface catalyst;
Adsorption and dissociation of H2O on surface catalyst;
Reaction of intermediate species to form H2/CO

## Slide 6
Coking
Catalytic reactions involving HC or CO
Formation of carbonaceous residues
Coke
Carbon
or
Coking or condensation
of HC
CHx: 0.5 < x < 1
CO disproportionation
2 CO C + CO2
Coke or
Carbon
Pore blocking
Physically cover the active sites

## Slide 7
Coking
Mechanism of coke formation
Olefin polymerization
Olefin cyclization to substituted benzenes
Formation of polynuclear aromatics from benzenes
via carbonium ions intermediates
Analytical techniques
IR
EPR
TG-DTA
UV-vis
13C-NMR
Evolution of combustion products
(CO2 and H2O)

## Slide 8
Coking
Coke deposition
Preferencially on the exterior of the particles
Resistance to the transport of reactants and products in the pores
Pore blocking

## Slide 9
Preventing Coking
Appropriate combination of process conditions
The gas mixture composition is kept as far as possible from conditions under which carbon formation is thermodynamically favored
High H2 pressure in catalytic reforming
Low HC / H2O ratios in steam reforming over Ni catalysts
Optimal catalyst composition
Promoters or additives that enhance the rate of gasification adsorben carbon or coke precursors and / or depress the carbon - forming reactions.
K in Ni - based steam - reforming catalysts
Pt - Re / Al2O3

## Slide 10
Preventing Coking

## Slide 11
Preventing Coking

## Slide 12
Preventing Coking

## Slide 13
Partial Oxidation
Alternative reaction route
is mildly exothermic and is much more energy efficient;
a smaller reactor can be used to achieve high CH4 conversion and selectivities to CO and H2 with short contact time;
no need for large amounts of expensive superheated steam
It may be carried out with a much broader range of compounds,
from Natural Gas to heavy residues and even coal

## Slide 14
Methane Partial Oxidation Mechanism
Alternative reaction route
Two reaction pathways are
generally accepted:
Direct Partial Oxidation (DPO)
Combustion-Reforming Reactions (CRR)

## Slide 15
Partial Oxidation di CH4: MPO su Rh(1%)@Al2O3
Fino a 410°C:
Oltre a 410°C:
Meccanismo CRR:
Combustione + Reforming
CH4 (2.0%) + O2 (1.0%) in Ar
GHSV = 700000 mL g-1 h-1

## Slide 16
Partial Oxidation di CH4: MPO su Rh(1%)@Al2O3

## Slide 17
Partial Oxidation di CH4: MPO su Rh(1%)@Al2O3
Thermographic picture of the Rh1 catalyst during the autothermal tests of methane partial oxidation (CH4/O2/He = 2/1/4, reaction gas mixture .
Catal. Today 64 (2001) 21-30

## Slide 18
Rh(1%)@Al2O3 : Caratterizzazione
Sinterizzazione della fase attiva
HRTEM
Nanoparticelle di Rh
2 nm
Campione attivato
Campione secco
Campione disattivato

## Slide 19
= O2 per 1minuto
Rh(1%)@Al2O3
“Ringiovanimento” del catalizzatore
Stabilità
CH4 (2.0%) + O2 (1.0%) in Ar
GHSV ~ 700000 mL g-1 h-1
T = 750°C

## Slide 20: Alternative reaction route
Autothermal Reforming
Its main benefit lies in compensating for the endothermic reaction of Steam Reforming with the exothermic reaction of Partial Oxidation
no extra heating
no extra cooling
e.g. Methane
It is probably the most interesting among coming developments
in H2 production processes from hydrocarbons.

## Slide 21: ... Ethanol
GREAT ATTENTION

## Slide 22: Ethanol Steam Reforming Reaction Pathway
S.Cavallaro, Energy & Fuels 14(2000)1195

## Slide 23
Al2O3
EtOH + H2O 1 : 5
GHSV = 150000 mL g-1 h-1
Temperature (°C)
Conversion/Yield (%)
T. Montini, Appl. Catal. B: Environ. 71 (2007). 125-134

## Slide 24: Rh(1% wt)@Al2O3
Temperature (°C)
Conversion/Yield (%)
Water Gas
Shift
EtOH + H2O 1 : 5
GHSV = 150000 mL g-1 h-1
T. Montini, Appl. Catal. B: Environ. 71 (2007). 125-134

## Slide 25
Temperature (°C)
Conversion/Yield (%)
Rh(1% wt)@Ce0.2Zr0.8O2(40%)/Al2O3
EtOH + H2O 1 : 5
GHSV = 150000 mL g-1 h-1
T. Montini, Appl. Catal. B: Environ. 71 (2007). 125-134

## Slide 26: Effect of promoters on the catalytic performance
Yield (%)
T = 450 °C
EtOH + H2O 1 : 5
GHSV = 150000 mL g-1 h-1
T. Montini, Appl. Catal. B: Environ. 71 (2007). 125-134

## Slide 27
mmol CO2 min-1
= 0.1 mmol CO2 min-1
EtOH-SR su Rh(1%)@CexZr1-XO2(YY%)-Al2O3 :
Deposizione di coke
TPO dopo reazione
a 600°C per 150h

## Slide 28
Hydrogen production from steam reforming of ethanol and glycerol over ceria-supported metal catalysts
B. Zhang, X. Tang, Y. Li, Y. Xu, W. Shen, Int. J. Hydrogen Energy 32 (2007) 2367-2373
CeO2-supported Ni, Co and Ir catalysts
Deposition-precipitation method over commercial CeO2.
Temperature between 250 – 550 ºC
Pressure: 1 bar
EtOH or Gly/H2O/He= 2/18/80 vol%
Ethanol reforming
Glycerol reforming
Complete conversion of ethanol at T > 400 ºC.
Good selectivity values at that temperature.
Ir/CeO2 is the most selective catalyst for ethanol and glycerol reforming.

## Slide 29
B. Zhang, X. Tang, Y. Li, Y. Xu, W. Shen, Int. J. Hydrogen Energy 32 (2007) 2367-2373
Ethanol reforming: stability tests
(350 ºC)
Over Ir/CeO2, ethanol was totally converted into methane, CO, CO2 and H2. Stable catalyst for at least 16 h.
For Co/CeO2 the formation of significant amount of acetone (8%) indicated that decarbonylation of acetaldehyde takes place and the activity is too low to promote the reforming reactions.
The Ni/CeO2 sample exhibited good activity for ethanol decomposition to methane and CO, and the later was converted into CO2 by the water gas shift reaction.
Hydrogen production from steam reforming of ethanol and glycerol over ceria-supported metal catalysts

## Slide 30
S. Adhikari, S.D. Fernando, S.D. Filip To, R. Mark Bricka, P.H. Steele, A. Haryanto, Energy and Fuels 22 (2008) 1220-1226
CeO2, MgO and TiO2-supported Ni catalysts
Incipient wetness technique over commercial supports.
Temperature between 550 – 650 ºC
Pressure: 1 bar
Water/glycerol= 6:1
Ni/CeO2 and Ni/TiO2 show slow deactivation while Ni/MgO does not deactivate.
Conversion of glycerol to hydrogen via a steam reforming process over nickel catalysts

## Slide 31
H2 selectivity increases with an increase in temperature.
The maximum H2 yield was 66% for Ni/CeO2 followed by 52% for Ni/MgO and 47% for Ni/TiO2 at 650 ºC.
The lower activity of Ni/TiO2 can be due to the higher coke formation (higher acidity of the support)
Effect of temperature on H2 selectivity
Effect of temperature on glycerol conversion
Coke formation
S. Adhikari, S.D. Fernando, S.D. Filip To, R. Mark Bricka, P.H. Steele, A. Haryanto, Energy and Fuels 22 (2008) 1220-1226
Conversion of glycerol to hydrogen via a steam reforming process over nickel catalysts

## Slide 32
S. Adhikari, S. Fernando, A. Haryanto, Catal. Today 129 (2007) 355-365
Alumina-supported catalysts
Incipient wetness technique
Temperature between 700 – 900 ºC
Pressure: 1 bar
Glycerin/H2O= 1:6 vol
Feed: 0.15 ml/min
The highest H2 selectivity was obtained over Ni/Al2O3. 60, 56 and 48% at 900, 800 and 700 ºC. This could be due to the promotion of C-C ruptures over Ni.
H2 selectivity pattern: Ni > Ir > Ru > Pt > Rh, Pd.
Conversions are favoured at higher temperatures due to the endothermicity of reforming.
Alumina-supported samples
Production of hydrogen by steam reforming of glycerin over alumina-supported metal catalysts

## Slide 33
The highest H2 selectivity was obtained over Pd/CeO2/Al2O3 at 900 ºC and Rh/CeO2/Al2O3 at 800 ºC. However at 700 ºC the most selective is Ni/CeO2/Al2O3.
With the addition of CeO2 all the samples show a higher H2 selectivity (WGSR promoted)
Glycerin conversions show mixed results with the addition of CeO2.
CeO2/Al2O3-supported samples
S. Adhikari, S. Fernando, A. Haryanto, Catal. Today 129 (2007) 355-365
Production of hydrogen by steam reforming of glycerin over alumina-supported metal catalysts

## Slide 34
The H2 selectivity and glycerin conversion increased with a decrease in flow rate.
With the increase in water/glycerin ratio the glycerin conversion increased monotonously for Ni/Al2O3. Mixed results over other samples.
With an increase in metal loading, the glycerin conversion increased for Ni/Al2O3 and Rh/CeO2/Al2O3.
The samples Ni/Al2O3 and Rh/CeO/Al2O3 were stable for at least 13 h of operation.
Rh/CeO2/Al2O3
Ni/Al2O3
S. Adhikari, S. Fernando, A. Haryanto, Catal. Today 129 (2007) 355-365
Production of hydrogen by steam reforming of glycerin over alumina-supported metal catalysts

## Slide 35
E.L. Kunkes, R.R. Soares, D.A. Simonetti, J.A. Dumesic, Appl. Catal. B 90 (2009) 693-698
Pt-Re/C is the most active sample.
Glycerol conversion
Pt-based bimetallic catalysts supported on C (reforming)
Incipient wetness impregnation
CeZrOx catalyst (WGSR)
Temperature between 548 – 623 K
Pressure: 1 bar
30<wt% Glycerin
Feed: 0.32 ml/min
An integrated catalytic approach for the production of hydrogen by glycerol reforming coupled with water-gas shift

## Slide 36
It was possible to produce syngas with controlled H2:CO ratios using two catalytic beds.
First bed of Pt-Re/C gives high conversions of glycerol to produce H2/CO gas mixture.
Second bed consisting of Pt(1%)/CeO2/ZrO2 promotes WGSR in a stable way.
E.L. Kunkes, R.R. Soares, D.A. Simonetti, J.A. Dumesic, Appl. Catal. B 90 (2009) 693-698
An integrated catalytic approach for the production of hydrogen by glycerol reforming coupled with water-gas shift

## Slide 37
P.J. Dauenhauer, J.R. Salge, L.D. Schmidt, J. Catal. 244 (2006) 238-247
High selectivities to H2 can be achieved by adjusting the fuel/air and fuel/steam feed ratios, as well the catalyst.
Pt and Rh-based catalysts supported on alumina
Incipient wetness impregnation
Temperature between 519 – 1055 ºC
Pressure: 1 bar
The addition of steam suppress CO selectivity while increasing selectivity to H2. Rh/CeO2/Al2O3 showed high fuel conversion and H2 selectivity.
Renewable hydrogen by autothermal steam reforming of volatile carbohydrates

## Slide 38
S.M. Swami, M.A. Abraham, Energy & Fuels 20 (2006) 2616-2622
The addition of oxygen enhanced the breakdown of the glycerol reactant, and decreased the formation of coke precursor, improving the H2 production.
Catalyst containing Cu, Ni and Pd (Pd/Ni/Cu/Al2O3)
Sequential wet impregnation technique
Temperature between 500 – 800 ºC
Pressure: 1 bar
Autothermal reforming of glucose
H2 yield up to 60% can be achieved at 750 ºC. If the amount of oxygen increases in the feed, the amount of CO2 also increases.
Integrated catalytic approach for conversion of biomass to hydrogen

## Slide 39: Aqueous-Phase Reforming (APR) Process
Science 2003, 300, 2075
Angew.Chem.Int.Ed. 2006, 45, 3982
Nature 2002, 418, 964

## Slide 40: Aqueous-Phase Reforming (APR) Process
Methanol
Ethylene Glycol
Glycerol
Sugars (Glucose) (Xylose)
Sugar Alcohols (Sorbitol)
Liquid-Phase Reforming
Single Reactor System
Low Temperature
160 – 265 oC
Relatively Low Pressure
Less Than 68 bar
Simple Vapor-Liquid Separator
Hydrogen-Rich Gas
Less than 100 ppm CO
Liquid-Water
Eliminates Energy required to vaporize water
Allows processing bioproducts that cannot be vaporized without decomposition
Compatible with processing wet feedstocks, avoiding need for an initial dehydration step
Operates at low T compared with conventional reforming, reducing energy costs
Water gas shift reaction occurs simultaneously with reforming
Pressurized product is compatible with membrane or p swing H2 purification

## Slide 41
Process Conditions
It is possible to obtain
a product of the desired specifications
R.R. Davida et al., Appl.Catal.B 56(2005)171
APR PROCESS
29/37

## Slide 42
R.R. Davida et al., Appl.Catal.B 56(2005)171
APR PROCESS: FACTORS CONTROLLING THE SELECTIVITY
30/37

## Slide 43
Nature 418, 964 (2002)
Reaction pathways for production of H2 by reactions of oxygenated hydrocarbons with water. (Asterisk represents a surface metal site.)
31/37

## Slide 44
Science 300, 2075 (2003)
Hydrogen was produced by aqueous-phase reforming of biomass-derived oxygenated hydrocarbons at T near 500 K over a tin-promoted Raney-nickel catalyst.
The performance of this non–precious metal catalyst compares favorably with that of platinum-based catalysts for production of hydrogen from ethylene glycol, glycerol, and sorbitol.
The addition of tin to nickel decreases the rate of methane formation from
C-O bond cleavage while maintaining the high rates of C-C bond cleavage required for hydrogen formation.
32/37

## Slide 45
Angew.Chem.Int.Ed. 45(2006)3983

## Slide 46
Chem.Commun. (2004)36
Reaction pathways involved in
glucose and sorbitol reforming.
Schematic representation of the recycle loop for
generation of hydrogen by APR of glucose.
34/37

## Slide 47
K. Lehnert, P. Claus, Catal. Comm. 9 (2008) 2543-2546
Increasing particles size produces higher catalytic activity and higher selectivity to H2.
APR of glycerol is structure sensitive. It is assumed that the adsorption of glycerol for subsequent cleavage of a C-C bond can be realized preferably on face positions.
Pt(3%)/Al2O3 catalysts
Calcination Temp: 260 – 600 ºC
Temperature: 523 K
Pressure: 20 bar
10 wt% glycerol
Influence of Pt particle size and support type on the aqueous-phase reforming of glycerol

## Slide 48
The nature of the metal precursor does not influence the catalytic activity.
Although lower H2 yields are obtained, even crude glycerol can be converted
Effect of the Pt loading
Effect of the glycerol purity
K. Lehnert, P. Claus, Catal. Comm. 9 (2008) 2543-2546
Influence of Pt particle size and support type on the aqueous-phase reforming of glycerol

## Slide 49
G. Wen, Y. Xu, H. Ma, Z. Xu, Z. Tian; Int. J. Hydrogen energy 33 (2008) 6657-6666
M/Al2O3 catalysts
Pt/support catalysts
Temperature: 503 K
Pressure: 3.2 MPa
10 wt% glycerol
Hydrogen production decreases in the order: Pt > Cu > Ni > Co.
Pt/Al2O3 is the only stable catalyst.
Production of hydrogen by aqueous phase reforming of glycerol

## Slide 50
G.W. Huber, J.W. Shabaker, S.T. Evans, J.A. Dumesic, Appl. Catal. B 62 (2006) 226-235
Pt/Al2O3, Pd/Al2O3, bimetallic Pt-M/Al2O3 and Pd-M/Al2O3 (more than 130 samples)
Temperature: 423-498 K
Pressure: 4.8 – 25.8 bar
5 wt% ethylene glycol
PtNi, PtCo, PtFe, PdFe were significantly more active than Pt and Pd monometallic samples.
Alloying Pt with Ni, Co or Fe improves the activity for H2 production by lowering the heats of CO and H2 adsorption, increasing the fraction of the available sites for reaction.
Aqueous-phase reforming of ethylene glycol over supported Pt and Pd bimetallic catalysts
Notes: Adsorbimento competitivo di

## Slide 51
Purification of H2 from Syn-Gas
basso contenuto di CO (<10ppm)
basse temperature per reforming
PEMFC

## Slide 52
Water - Gas Shift Reaction
Cu, Ni, Fe, Co, Pd, Pt su CeO2
Au / CeO2
CO + H2O
CO2 + H2
HTS: Fe2O3 / Cr2O3
LTS: Cu/ZnO/Al2O3
PReferential OXidation
of CO in excess H2
Pt / CeO2 / Al2O3
Au / CeO2
CuO / CeO2
CO + 1/2 O2
CO2
Processes for CO removal
Notes: PROX è selettivo se il metallo adsorbe preferenzialmente CO e non H2.

## Slide 53
WGSR
“Redox” mechanism
“Associative formate with –OH regeneration” mechanism
The factor governing WGSR is the extension of the metal-promoter interface, as a result of a good contact between the two components.

## Slide 54
WGSR
J. Mater. Chem. A, 5 (2017), 20024–20034

## Slide 55
J. Mater. Chem. A, 5 (2017), 20024–20034
WGSR
Deposition-precipitation on SBA-16
Impregnation of SBA-16 with Pt-DT and Ce(OR)4
Impregnation of hydrophobic SBA-16 with Pt-DT and Ce(OR)4
Deactivation by sintering (irreversible)
Deactivation by deposition of intermediates and/or electronic effects (reversible)