## Slide 2
Sol-Gel technique
In the case of the colloid, the particle density may be so low that a significant amount of fluid may need to be removed initially for the gel-like properties to be recognized. The simplest method is to allow time for evaporation and sedimentation to occur, and then, if necessary, pour off the remaining liquid. Centrifugation can also be used to accelerate the process of phase separation.
Removal of the remaining liquid (solvent) phase requires a drying process, which is typically accompanied by a significant amount of shrinkage and densification. The rate at which the solvent can be removed is ultimately determined by the distribution of porosity in the gel. The ultimate microstructure of the final component will clearly be strongly influenced by changes imposed upon the structural template during this phase of processing.

## Slide 3
Sol-Gel technique

## Slide 4
Sol-Gel technique

## Slide 5
Sol-Gel technique
The zeta potential is a key indicator of the stability of colloidal dispersions. The magnitude of the zeta potential indicates the degree of electrostatic repulsion between adjacent, similarly charged particles in a dispersion. For molecules and particles that are small enough, a high zeta potential will confer stability, i.e., the solution or dispersion will resist aggregation.
At low pH the particle surface is protonated and positively charged.
At high pH the particle surface is negativelly charged.
Surface charge is compensated by ions in solution.

## Slide 6
Zeta potential (mV) | Stability behavior
0 to ±5 | Rapid coagulation or flocculation
± 10 to ± 30 | Incipient instability
± 30 to ± 40 | Moderate stability
± 40 to ± 60 | Good stability
> 61 | Excellent stability
Stability behavior of a colloid depending on zeta potential
Energies 2014, 7, 568-590
Gelation time is minimum at zero zeta potential (IEP)
Dependence of Silica gelation time from pH and concentration

## Slide 10
FTIR spectra of hydroxyl cover of γ-Al2O3 (a) and γ-Al2O3 after hydrothermal treatment for 3 h at 150 (b), 180 (c) and 200 °C (d). The samples were calcined and outgassed at 500 °C

## Slide 13
Sol-Gel method for TiO2 nanoparticle preparation

## Slide 14
Sol-Gel method for SiO2 aerogel preparation
https://www.youtube.com/watch?v=hFSbgANbKuw

## Slide 15
Reverse
Microemulsion
aqueous core
5–10 nm.
Microemulsion
1–100 nm.
Spherical shape. The core size can be tune by varying the concentration of the dispersed phase and the surfactants
Microemulsion : nanoreactors
A polar phase (water), a nonpolar phase (oil) and an emulsifier (surfactant)
* Co-surfactant : a medium chain alcohol
A microemulsion is a macroscopically homogeneous system and possesses spherical droplets of the size <50 nm that do not require the higher input of energy and shear reaction conditions, in contrast to conventional emulsions, which are cloudy, kinetically stable and thermodynamically unstable systems

## Slide 16
Microemulsion : nanoreactors

## Slide 17: hydrophilic-lipophilic balance (HLB) value
HLB = 20 for a 100 % hydrophilic non ionic surfactant

## Slide 18
bicontinuous “sponge” to water-swollen inverse micelles dispersed in oil (W/O microemulsion) phase
Mixture of (O/W and W/O)
Depending on the hydrophilic-lipophilic balance (HLB) value of the surfactant and the oil/water ratio, the formed microstructure can exist in oil-in-water (O/W), water-in-oil (W/O), hexagonal, reverse hexagonal, or a mixture of (O/W and W/O) called bicontinuous/lamellar phase. In general, the surfactants having HLB of 3–6 promote the formation of W/O microemulsions whereas with HLB of 8–18 facilitate the formation of O/W microemulsions.
Microemulsion : nanoreactors

## Slide 20
Metallic nanoparticles : Ag, Au, Pt, Pd, Cu, Ni, Mo, Ru, Se, Fe, Ce
and their oxides, sulfides, fluorides, chromates, phosphates
Quantum dots: CdX (X = S, Se, Te), carbon dots, Si QDs, graphene QDs, Ag2Se, Ag2S, ZnS, InP, etc
https://www.intechopen.com/books/microemulsion-a-chemical-nanoreactor/microemulsions-as-nanotemplates-a-soft-and-versatile-approach
Microemulsion : nanoreactors

## Slide 21
Thiol-functionalized Au NPs (having diameter 3–4 nm) by using W/O microemulsion (toluene/tetraoctylammonium bromide/water) where HAuCl4 was employed as a precursor and NaBH4 as a reducing agent.
Particuology, Volume 37, April 2018, Pages 33-36
A microemulsion method for preparation of thiol-functionalized nano Au
the two-phase
Brust method

## Slide 22
TEM images of stabilized AuNP colloid solutions, prepared by the (a) two- phase Brust method and the (b) microemulsion technique.
Particuology, Volume 37, April 2018, Pages 33-36
A microemulsion method for preparation of thiol-functionalized nano Au

## Slide 23
Tetraethyl orthosilicate (TEOS) is exploited as the common source of silicon alkoxide
W/O
https://pubs.acs.org/doi/10.1021/la0624283
The final particle size increases with the number of collisions or micellar exchanges.
Acid catalysis, in contrast, promotes hydrolysis but hinders both condensation and dissolution reactions.
Base catalysis of sol−gel reactions promotes hydrolysis, condensation, and, more importantly, dissolution.
Nucleation in water-in-oil microemulsions takes place when the concentration of hydrolyzed precursors present in the reverse micelle droplets exceeds the nucleation threshold Cn.
A microemulsion method for preparation of SiO2

## Slide 27: Reazione idrotermale
Questo metodo di sintesi consiste nella dissoluzione e ricristallizzazione di materiali a bassa solubilità. In questo processo una sospensione/soluzione viene trattata in condizioni di alta T e P (differisce da un semplice processo di “ageing” per le condizioni)

Evoluzione verso sistemi termodinamicamente più stabili (ingrossamento di cristalli, trasformazioni strutturali, sintesi idrotermali, cristallizzazione di amorfi)
La velocità delle trasformazioni idrotermali è generalmente bassa – lo stadio lento è la dissoluzione

Possibilità di accelerare la velocità con aggiunta di sostanze mineralizzanti (acidi, basi, complessati)

## Slide 28: Attrition
Attrition is a mechanical method for creating certain types of nanoparticles.
Macro or micro scale particles are ground in a ball mill, a planetary ball mill, or other size reducing mechanism.
The resulting particles are separated by filters and recovered.
Particle sizes range from tens to hundreds of nm.
Broad size distribution and varied particle geometry.
May contain defects and impurities from the milling process.
Generally considered to be very energy intensive.

## Slide 29: Attrition: Rotary Ball Mill
A hollow steel cylinder containing tungsten carbide (WC), corundum (α-Al2O3) or ZrO2 balls and a solid precursor rotates about its central axis.
Particle size is reduced by brittle fracturing resulting from ball-ball and ball-wall collisions.
Milling takes place in an inert gas atmosphere to reduce contamination.

## Slide 30: Attrition: Examples

## Slide 31: Pyrolysis: Industrial method for many products
Carbon Black
TiO2
SiO2
Tires
Inks
Paints
Makeup
Optical
fibers
Carbon black - 8 million tons $8 billion
TiO2 - 2.5 million tons, $5 billion
SiO2 - 2.0 million tons, $2 billion

## Slide 34
A precursor (liquid or gas) is forced through an orifice at high pressure and burned.
The resulting ash is collected to recover the nanoparticles.
Large volume of gas leads to high rate of material synthesis.
Pyrolysis: popular method for creating nanoparticles, especially oxides
Versatile
Large Variety of precursors
Controllable
Scalable
Aggregation
Condensation
Coagulation
Nucleation
Droplet evaporation
Flame Spray Pyrolysis (FSP)

## Slide 35
Pyrolysis: System Overview

## Slide 36
Aggregates and Agglomerates:
Aggregate – An assemblage of particles rigidly joined together by chemical or sinter-forces.
Agglomerate – A loosely coherent assembly of particles and/or aggregates held together by weak interactions
Current aerosol instruments cannot distinguish between them.
  Aggregates Agglomerates
Pyrolysis

## Slide 37
TiO2
Monomers
Transient Hard
Agglomerates
Spherical
Particles
Hard Agglomerates
Soft Agglomerates
Pyrolysis: Agglomerate Formation Sequence
Distinction between hard and soft agglomerates is largely empirical.
Controlled agglomeration can minimize post-grinding and other costly separation techniques.

## Slide 38
Impact of oxygen
Aids in combustion
Provides chemistry in the reaction
Acts as a dilutent, cools the flame, prevents agglomeration
All of these variables can be decoupled by burner design. Which is cheaper than increasing oxygen flow.
Excess oxygen makes the flame burn cooler resulting in smaller diameter particles
Pyrolysis: Particle Size Controlled by O2 Flow