## Slide 1: Chemisorption, surface area and metal dispersion

## Slide 2: 1.1% Pt/g-Al2O3
Adsorbimento a 573 K di H2. Curva (a) adsorbimento su 2.031 g di catalizzatore, (c) adsorbimento su 1.00 g di Al2O3, (d) adsorbimento su quantità di supporto corrispondente a quella del campione (2.00 g) ed espressa nella stessa scala della curva (a), (b) differenza tra la curva a e d.

## Slide 3
Metallic Dispersion (DM)
metal surface atoms
total metal atoms
In the case of a sphere
S / V = (4 p r2 )/ (4/3 p r3) = 3/r
r = 3 V / S d = 2r = 6 V /S
In the case of a cube, the Surface to Volume ratio is
S / V = 6 a2 / a 3 a = 6 V / S
Mean diameter of a metal particle

## Slide 4
Metallic Dispersion (DM)
metal surface atoms
total metal atoms
Mean diameter of metal particles ( spherical geometry)
= 6 V/A
area of a metal atom
volume of a metal atom in the "bulk"
atomic weight,  density Avogadro’s number

## Slide 5
M

## Slide 6
Sample pretreatment and chemisorption
We need metals to get chemisorption!!
Wet Synthesis –exposure to air. Nanoparticles surface oxidation state ? Passivation ?
Pre-reduction: typically diluted hydrogen (flow vs static, Temperature and conditions that do not change nanoparticle size/morphology) based on TPR
Degassing conditions – Removal of gas phase and chemisorbed hydrogen (up to 350-400°C)

## Slide 7
Thermoanalytical techniques
measurement of a physical or chemical property of a solid as the temperature of the solid is varied in a predetermined manner
temperature programmed
Material Characterization by
Temperature Programmed Methods

## Slide 8
Thermoanalytical techniques
Techniques dependent on dimensional changes
Techniques dependent on evolved gases
Techniques dependent on gas analysis from chemical reaction
DILATOMETRY
Techniques dependent on weight changes
Thermogravimetry
Techniques dependent on energy changes
Diff. Thermal analysis
Diff. Scanning calorim.
Temp. prog. desorption
Temp. prog. reaction
Temp. prog. reduction
TPD, TPDE, TPSR
TPRE, TP...
TPR/TPO

## Slide 9
temperature programmed desorption/decomposition
time
coverage
temperature
rate
Pretreatment of the material
Exposure to reactant gas
Desorption of physisorbed fraction
Heating of sample in an inert gas stream
Analysis of desorbed components

## Slide 10
temperature programmed reduction/oxidation
time
Degree of
reduction
temperature
reduction
rate
Pretreatment of the material
Heating of sample in the presence of reducing or oxidizing mixture
Analysis of reductant or oxidant consumption
MO(s) + H2(g) M(s) + H2O(g)
M(s) + O2(g) MO(s)

## Slide 11
temperature programmed reaction
Coadsorption of two gases and heating in inert carrier
Adsorption of one component and heating in reactive carrier gas
Heating in reactive atmosphere containing reagents
Temperature programmed methanation, hydrogenation, sulphidation, combustion…….

## Slide 12
CO
CO
CO
CO
CO
CO
CO2
CO2
CO2
O
O
CO
CO
CO
CO
CO
CO2
CO2
CO2
TPD
TPDE
TPRE
desorption vs decomposition vs reaction

## Slide 13
Characterization of reducibility of materials
Determination of binding energy of adsorbed molecules
Acidity
Characterization of surface carbon deposits
Physical parameters (surface area, dispersion…)
information that can be obtained…

## Slide 14
Experimental:
apparatus for TP studies
introduction of reactants
furnace and reactor
detector
data acquisition
time/temp.
concentration

## Slide 15
Experimental: Detector and data acquisition
Thermal conductivity detector
 Good for TPO/TPR
 Non specific gas analysis
 Concentration can be monitored continuously
Mass spectrometer
 Concentration can be monitored continuously
 Specific gas analysis
 High cost
Micro GC
 Concentration cannot be monitored continuously
(delay 1-2 min.)
 Complex gas analysis
 Accurate quantitative evaluation

## Slide 16
STRONG METAL/SUPPORT INTERACTION
(SMSI) EFFECT
S.J. Tauster et al; J. Am. Chem. Soc. 100, 170 (1978)
  Typically associated with reducible supports
  At low Tredn (200ºC) the material exhibits a
    “conventional” chemical behaviour
  At high Tredn (500ºC) strong perturbation of the
    chemisorptive and catalytic properties
  Reversibility. Reoxn. + mild Redn. allows to
    regenerate the material
Classic SMSI system: M/TiO2

## Slide 17
H/Rh Catalytic Activity*
Red. 200°C 0.43 17
Red. 500°C 0 0
Red. 500°C
Reox. 400ºC 0.23 7
Red. 200ºC
S. Bernal et al, Appl. Catal. 99, 1 (1993)
Rh(5%)/TiO2
SMSI Effect. Chemical Evidence
* Benzene hydrogenation (25ºC) (cm3 cyclohexane /gRh.s)

## Slide 18
Rh(5%)/TiO2
HREM micrograph
Catalyst reduced at 200ºC
3 nm
TiO2 – A [111]
Rh
High density of clean and well faceted Rh particles

## Slide 19
Rh(5%)/TiO2
HREM Micrograph
Catalyst reduced at 500ºC
3 nm
TiO2 – A [111]
Rh
TiO2-x migrates onto and partly covers the metal microcrystals (DECORATION)

## Slide 20
Rh(5%)/TiO2
At Tred = 500ºC:
A significant fraction of the Rh microcrystals look like clean (Partial Decoration)
Rh
HREM micrograph
Catalyst reduced at 500ºC

## Slide 21
Rh(5%)/TiO2
Reversibility of the SMSI Effect
TiO2 – R [110]
2 nm
Rh [110]
Reoxn. at 400ºC-500ºC followed by a mild reduction allows to recover the catalyst from the SMSI state
Red. 500ºC + Ox. 400ºC
+ Red. 200ºC

## Slide 22
Metal Decoration in Rh/Ce(M)O2-x
700 ºC < Tred < 900º C
Rh/CeO2 Red. 700ºC in H2

## Slide 23
Pt/CeTbOx Tred: 700ºC
Pt
0.34 nm
(111) sop.
soporte[011]
(111) Pt
Monocapa de soporte
8°
Pt [110]
Metal Decoration Effects in Pt/Ce(M)O2-x
700 ºC < Tred < 900º C
Simulated image
0.34 nm

## Slide 24
No evidence of formation of Rh-Ce intermetallics
3 nm
decoración
2.3
2.2
2.2
61°
54°
65°
3 nm
1.9
2.2
2.2
1.9
2.2
Nano-structure of HT (900ºC) reduced Rh
Tred  900º C
Twinned Rh particle.
Metal sintering on HT reduction
decoration

## Slide 25
Pt-Ce Alloying Phenomena
Tred > 900º C
5 nm
Pt/CeO2 Red. 1173 K en H2
4.66
3.02
4.22
90°
42°
[010] CePt5
CePt , CePt2
CePt5 , Ce3Pt2 , Ce7Pt3
Pt

## Slide 26
0 1 2 3 4 5 6
50
40
30
20
10
0
Frequency / %
Particle diameter / nm
TEM
H2 Chemisorption
EXAFS
dm = 2.5 nm
5 wt % Rh /Al2O3
J.Catal, 190, 2001, 182
Effect of the support on metal dispersion: Ce0.6Zr0.4O2 vs Al2O3

## Slide 27
0 1 2 3 4 5 6
50
40
30
20
10
0
Frequency / %
Particle diameter / nm
dm = 2.5 nm
dm = 1.2 nm
5 wt % Rh /Al2O3
5 wt % Rh /Ce0.6Zr0.4O2
J.Catal, 190, 2001, 182
Effect of the support on metal dispersion: Ce0.6Zr0.4O2 vs Al2O3

## Slide 28
PJ.Phys.Chem. B, 104,2000, 4667
Frequency / %
Particle diameter / nm
0
1
2
3
4
5
6
7
2.4 nm
2.4 nm
Effect of temperature on metal dispersion: Rh/Ce0.68Zr0.32O2
150°C

## Slide 29
Frequency / %
Particle diameter / nm
0
1
2
3
4
5
6
7
2.4 nm
2.4 nm
2.7 nm
PJ.Phys.Chem. B, 104,2000, 4667
150°C
500°C
Effect of temperature on metal dispersion: Rh/Ce0.68Zr0.32O2

## Slide 30
Frequency / %
Particle diameter / nm
0
1
2
3
4
5
6
7
2.4 nm
2.7 nm
4.2 nm
150°C
500°C
900°C
J.Phys.Chem. B, 104,2000, 4667
Effect of temperature on metal dispersion: Rh/Ce0.68Zr0.32O2

## Slide 31
Metal nanoparticle and chemisorption
Hydrogen spillover is the migration of hydrogen atoms from the metal catalyst onto the nonmetal support or adsorbate
Reducible oxides TiO2, CeO2
Apparent Dispersion >>> 100%
Low Temperature chemisorption (-90° C)
HR-TEM vs Chemisorption data

## Slide 32
Support
Noble metal
H2
Rh/CeO2 Reducibility

## Slide 33
CeO2 Reducibility

## Slide 34
Support
Noble metal
H2
H2 ads. (- 90ºC): DH = H/RhT
HREM: DHREM = RhS/RhT
DH / DHREM = H/RhS
J. Phys. Chem. B, 104, 2000, 4667
Rh/Ce0.68Zr0.32O2 Chemical deactivation

## Slide 35
Pd on Al2O3 and ZrO2 after treatment in 0.2 Torr O2 at 560°C
Rogriguez N.M. et al., J. Catal 157, 676-686 (1995)
PdO
Al2O3
Low Metal Loading
PdO
Al2O3
Pd
High Metal Loading
ZrO2
ZrO2
ZrO2
150°C
350 - 850 °C
> 890°C
PdO
PdO
PdO
Al2O3
Al2O3
Al2O3
150°C
350 - 650°C
> 800°C
PdO
PdO
“PdAlOx”

## Slide 36
Phase: Solid Solution
MHx
(0 < x < 0.1)
b Phase: Hydrides
MHx
( x = 1, 2, 3, ..)
Metal Hydrides and chemisorption
Metal : Al, Mg, Li, Be,….

## Slide 37
Pd nanoparticle and chemisorption
Pd bulk hydrides vs surface at room temperature
decomposes at 80 °C
Pd/Al2O3 H2 Chemisorption at 100 °C, low physisorption
Pd/CeO2 H2 Chemisorption ?? RT very low pressure
α-PdHx phase exists at x < 0.017
β -PdHx phase is realised for x > 0.58
intermediate x values correspond to α-β mixtures

## Slide 38
M/CeO2 based materials reducibility
TPR-MS profiles for fresh Rh/Ce0.68Zr0.32O2 (A), Pt/Ce0.68Zr0.32O2 (B), and Pd/Ce0.68Zr0.32O2 (C): H2 uptake (upper traces) and H2O evolution (lower traces).

## Slide 39
Pd nanoparticle and chemisorption at 25°C
(A) and the same sample oxidized at 427 °C and rereduced at 150 °C (B)