## Slide 1
Professor Francesco Stellacci
EPFL since 2010
MIT 2002-2010

## Slide 2
Prof. Federico ROSEI
Dipartimento di Scienze Chimiche e Farmaceutiche federico.rosei@units.it
C11, Aula 3
a.a. 2022-2023
Corso di
Chimica delle Macromolecole I
Microscopia a scansione di sonda

## Slide 3
Si(111) clean surface
(reconstructed 7x7)
imaged with
atomic resolution
Si(111) 7x7
First STM work:
Binnig et al.,
Phys. Rev. Lett. (1983)
Si(111) 7x7 in real space

## Slide 4
Cu(110) with atomic resolution
Cu(110) 1x1
[1 –1 0]
[0 0 1]
100 x 100 Å2

## Slide 5
Au(110)-(1x2)
Missing row reconstruction

## Slide 6
The Herringbone Reconstruction on the Au(111) Surface
87 x 90 Å2
1211 x 1227 Å2

## Slide 7
Nano–tools
“The problems of chemistry and biology can be greatly helped if our ability to see what we are doing, and to do things on an atomic level, is ultimately developed – a development which I think cannot be avoided”
From: R. Feynman: There's Plenty of Room at the Bottom (1959)
By increasing by a factor of 10 the resolving power of the Human eye, Galileo was able to discover Jupiter’s satellites
”The principles of physics, as far as I can see, do not speak against the possibility of maneuvering things atom by atom”

## Slide 8
100 mm
10 mm
100 nm
10 nm
1 nm
1 mm
Scanning Probe
Microscopy
Electron
Microscopy
Optical
Microscopy
Human hair
Cells
Lithography
Integrated circuits
Biological
Macromolecules
Atoms and
molecules
Length scales – Nano–tools

## Slide 10: Scanning Probe Microscopy
Principle of a scanning probe microscope.
Surface is scanned line by line with a probe using a fine positioning system (scanner).
With a coarse positioning device, the distance between the sample and the probe is reduced until the interaction regime is reached.
Vibration isolation shields the microscope from external vibrations.

## Slide 11
The STM principle
G. Binnig and H. Rohrer,
(Nobel Prize in Physics, 1986)
A sharp metal tip (W, Pt–Ir) is brought into close proximity
of a conducting sample, and a bias is applied:
electrons tunnel from tip to sample (or viceversa)

## Slide 12
Principle of a scanning tunnelling microscope.
Once the gap between tip and sample is about as small as the diameter of an atom, a tunnelling current flows between a conductive tip and sample.
The STM principle

## Slide 13
Operation of an STM1,2
[1] C. Julian Chen, Introduction to Scanning Tunnelling Microscopy, Oxford (1993)
[2] G.A.D. Briggs and A. J. Fisher, Surf. Sci. Rep. 33, 1 (1999)

## Slide 14
Scanning Tunneling Microscopy
Pt(110)–(1x2)
with atomic resolution
Once the tip is in ”tunneling contact”, it is scanned above the surface using three separate piezoelectric transducers for precise movements in x,y,z

## Slide 15
gentle touch of a nano-finger:
If the interaction between tip and sample decays sufficiently rapidly on the atomic scale, only the two atoms that are closest to each other are able to ‘‘feel’’ each other.
Principle of a local probe
G. Binnig, H. Röhrer,
Rev. Mod. Phys. 71, S324 (1999)

## Slide 16
Scanning Probe Microscopy was developed following the need to obtain local information on morphology, structure, etc.
Other advantages over “similar” techniques (e.g. SEM): SPM is less damaging, and it can be used to “manipulate” objects on the atomic scale

## Slide 17
Tunneling Current
Q…. Workfunction, typically 3-5 eV
z….. Tip-sample separation, typically 4-10 A
D z = 1 A --> D I one order of magnitude !
It  Vt exp(-A z)

## Slide 18
Unknown/Challenges:
1. Chemical nature of STM tip
(problem for spectroscopy, corrugation)
2. Relaxation of tip/surface atoms
(tip sample separation not equal to piezo scale)
3. Effect of tip potential on electronic
surface structure (quenching of surface states)
4. Influence of magnetic properties
on tunnelling current/surface corrugation
(is spin-STM possible?)
5. Relative importance of the effects

## Slide 19
Surface
adsorbed atom or molecule
The tunneling resistance R = V / I measures the separation of the tip from the surface:
I ~ V exp (-2kz)
STM tip
Lateral Manipulation of individual atoms and molecules by STM
By reducing V / I, the tip approaches the substrate, thus leading to a stronger tip–surface interaction

## Slide 20
”freezing” the motion of single adsorbates: low (variable)
temperature STM
long operating time and working at low coverages
(0.001–0.01 ML); requirements:
    high cleanliness: scanner completely surrounded by 4 K
  Radiation shield
    controlled deposition of small amounts of adsorbates:
  small hole in the radiation shield, with small solid angle
  (1:3000)
  flexible and precise tip positioning; requirements:
    high x,y,z stability
    I(V): electronic / vibrational spectroscopy
    I(z): tip – adsorbate interaction
    Tip height / current during manipulation
Important features for STM manipulation

## Slide 21
Idealized sketch of picking up / putting down of CO molecules on Cu(111).
CO stands upright on the surface and has
to switch its orientation when transferred to the tip.
Bartels et al., Appl. Phys. Lett. 71, 213 (1997)
Vertical Manipulation of CO on Cu(111)

## Slide 22
Bartels et al., Appl. Phys. Lett. 71, 213 (1997)
Transfer of single CO
molecules from the right to the left terrace by vertical manipulation
CO molecules are imaged as depressions with a metal tip and as protrusions with a CO tip
Cu(111) terrace
intersected by
a lower terrace
Vertical Manipulation of CO on Cu(111)

## Slide 23
Pushing and pulling single atoms
Using the tip of a Scanning Tunnelling Microscope
Quantum Corral (Fe on Cu):
Visualization of electron wavelets
D. Eigler, IBM Almaden
Xe on Ni(111) at 4 K
D. Eigler, IBM Almaden

## Slide 24
Japanese Kanji
character for Atom, written with atoms
D. Eigler, IBM Almaden
Manipulation – Atom by atom

## Slide 25
Single–molecule synthesis by STM
S.W. Hla et al., Phys. Rev. Lett. 85, 2777 (2000)
Synthesis of biphenyl (C12H10) from iodobenzene (C6H5I)
STM tip-induced synthesis steps of a biphenyl molecule. (a), (b) Electron–induced abstraction of iodine from iodobenzene. (c) Removal of iodine by lateral manipulation. (d) Bringing together two phenyls by lateral manipulation. (e) Electron–induced chemical association of the phenyl couple to biphenyl. (f ) Pulling the synthesized molecule with the STM tip to confirm the association.

## Slide 26
STM movies: Diffusion of Pt adatoms
T.R. Linderoth et al., Phys. Rev. Lett. 78, 4978 (1997)
More STM Movies: www.phys.au.dk/camp
Diffusion of Pt adatoms on Pt(110)–(1x2)

## Slide 27
DC Movies
500x500 Å2
T = 251 K
500x500 Å2
T = 235 K
1 D Diffusion along the close packed direction [110] of Cu(110)
15 seconds
per image
image size:
compromise between good statistics and good resolution
[1,-1,0]
[001]
M. Schunack, T.R. Linderoth, F. Rosei et al., Phys. Rev. Lett. 88, 156102 (2002)

## Slide 28
HtBDC Movies
500x500 Å2
T = 194 K
500x500 Å2
T = 203 K
1 D Diffusion along the close packed direction [110] of Cu(110)
~15 seconds per image
M. Schunack, T.R. Linderoth, F. Rosei et al., Phys. Rev. Lett. 88, 156102 (2002)

## Slide 29
Surface diffusion: in general, it is a 2 D random walk
ED
 = 0 exp(-ED/kT)
    Hopping rate: counting the proportion of molecules that have not moved between two consecutive images:
    P0 = M / N = F(ht)

## Slide 30: Surface diffusion
hopping rate:
random walk:
ln D
1/kT
tracer diffusion coefficient:
 - RMS jump length
h = h0 exp(-ED/kT)
D = D0 exp(-ED/kT)
with D0 = h02/2
(Δx)2 = 2 ht
D = (Δx)2/2t
Δx
ED
PΔx
ED
D0
T1 T2

## Slide 31
Displacement distribution: HtBDC
Temperature: 185 K
Time per image: 13.5 sec
Temperature: 194 K
Time per image: 13.7 sec

## Slide 32
Tunneling resistance  5 GΩ (V  -1.5 V, I  -0.3 nA)
Displacement distribution:
  symmetric
  Δx  0.0 ± 0.8 Å
Controlled manipulations
  DC:  0.1 GΩ
  HtBDC:  1 GΩ
below usual imaging conditions
}
Tip influence? - No!

## Slide 33: Arrhenius analysis: D
DC
220 – 250 K
HtBDC
170 – 200 K
ED=0.71±0.05 eV
D0 =10-1.0±1.0 cm2s-1
ED=0.62±0.04eV
D0=100.9±1.0cm2s-1
=> Arrhenius parameters are related to molecular structure

## Slide 34
DC
220 – 250 K
HtBDC
170 – 200 K
Arrhenius analysis: h
ED=0.71±0.05 eV
h0 =1013.9±0.7 s-1
ED=0.62±0.04eV
h0=1013.5±0.4 s-1
In general, ED is a fraction of the adsorption energy

## Slide 35: Jump lengths – results
DC/Cu(110)  = 3.9 ± 0.2
Pt/Pt(110)  = 1.11 ± 0.01
(10% of jumps are non- nearest neighbor)
HtBDC/Cu(110)  = 6.8 ± 0.3
ht
(Δx)2 [(NN-dist)2]
  (Δx)2 = 2 ht
M. Schunack, T.R. Linderoth, F. Rosei et al., Phys. Rev. Lett. 88, 156102 (2002)

## Slide 36: Molecular conformations
Upon adsorption, the molecule adapts to the substrate
The conformation(s) it adopts will largely determine its properties on the surface (diffusion, conductivity, etc.)
This is true for molecular devices for nanoelectronics as it is for biomolecules (proteins, etc.)

## Slide 37: Molecular diffusion on Cu(110)
[001]
[110]
Cu(110) is anisotropic!

## Slide 38
Diffusion coupled to rotation
with high resolution we observed the rotation of single molecules, coupled to diffusion: the molecules behave like nano-disks
Diffusion of DC
on Cu(110), high
resolution movie
200 x 200 Å2

## Slide 39
Atomic Force Microscope (AFM)
Binnig, Quate, Gerber (1986)
It also works
on insulators!

## Slide 40
Atomic Force Microscope

## Slide 41: The first AFM

## Slide 42
Atomic Force Microscopy

## Slide 43: AFM principle
Principle of a atomic force microscope. A sharp tip is brought close to the sample.
The forces acting between tip and sample lead to a deflection of the spring.
The deflection is then measured e.g. optically

## Slide 44
Measuring Forces

## Slide 45: Forces between atoms
‘Back of the envelope’:
• Atomic energy scale:
Ebond ~ 1-4 eV ~ 2-6 • 10-19 J
• Typical bonding length:
a~0.2 nm
• Typical forces:
F = E/a ~ 1-3 nN
Bonding energies:
• Quantum mechanical
(covalent, metallic
bonds): 1–3 nN
• Coulomb (dipole, ionic): 0.1–5 nN
• Polarization (induced dipoles): 0.02–0.1 nN
J. Israelachvili, ‘Intermolecular and Surface Forces’, Academic Press

## Slide 46: Comparing forces
Comparison of the distance dependence of a short range force with the tunneling current.

## Slide 47: Electrostatic forces

## Slide 49: Deflection sensors

## Slide 50
Laser beam deflection detection systems as often used in ambient AFMs.
Interferometric cantilever detection system, a popular choice for low-temperature AFMs.

## Slide 51: Feedback modes

## Slide 52: Piezoelectric scanners

## Slide 53
The tunneling current is measured with a current-to-voltage converter and is used to measure the distance between tip and sample. The current noise sources in the current-to-voltage converter have to be small enough such that the corresponding vertical noise is considerably smaller than the atomic corrugation of the sample.
A simple form of such a circuit is shown in figure 3. It uses a low noise operational amplifier (OPA) and a feedback resistor (Rfb) with a typical impedance of R = 100 MW. To get a maximum signal-to-noise ratio the bandwidth should be maximized while the noise should be as small as possible.

## Slide 54: Imaging artifacts

## Slide 55: Thermal drift
Touching the microscope (e.g. sample, cantilever) will change its temperature T. Shining light on it too! Cantilever has a mass of ~ 1 ng, and thus a VERY small heat capacity.
So what!?!
ΔL/L = const ΔT; const ~ 10-5

## Slide 56: Van der Waals forces

## Slide 57
(a) The cytoplasmic surface of the hexagonally packed intermediate layer is an essential part of the cell envelope of Deinococcus radiodurans. It has a protective function and acts as a molecular sieve. The pores in protruding cores are the channels of this sieve, and exhibit two conformations that change dynamically. The unit cell size is 18 nm, and the brightness range corresponds to 3 nm. (b) Two-dimensional crystals of bacteriophage F 29 head-tail connectors recorded with AFM in buffer solution. The connectors are packed in up-and-down originations, exposing their narrow ends that connect to the tail and their wide ends that connect to the head. The unit cell size is 16.5 nm, whereas the brightness range corresponds to 4 nm.
AFM on biological systems

## Slide 60
DNA in buffer (200nm x 200nm)
Bacterial cellulose (2.0µm x 2.0µm)

## Slide 61
Bacterial cell (H. pylori) (5.5µm x 5.5µm)
Living fibroblast cells in PBS (60µm x 60µm)

## Slide 62
polivinilpiridina

## Slide 63
Amino-functionalized
polymethacrylate

## Slide 64
Immagine della grafite mediante AFM. L’alta risoluzione permette di vedere la disposizione esagonale degli atomi nella cella unitaria.
Dimensioni dell’immagine 2×2
nm2.

## Slide 65: Studi sulla morfologia di polimeri biologici
Fibre di actina visualizzate in modo contatto AFM
L'actina è una proteina globulare con peso molecolare di 43 kDa. Ha un diametro di 5,46nm e determina la possibilità di movimenti cellulari. E’ presente in tutte le cellule del corpo e specialmente nelle cellule muscolari. La quantità di actina nelle cellule può raggiungere il 10% di quella proteica totale.

## Slide 66: Immagine AFM
di segmenti di DNA doppia elica
depositato su mica. La dimensione laterale della doppia elica di DNA è 2 nm (anche utilizzata come standard di calibrazione).
Immagine prodotta dal Dr. Andy Baker.

## Slide 67
diverse morfologie che il DNA assume in seguito al compattamento dovuto all’aggiunta di una proteina chiamata AbF2.
Questa serie di immagini visualizza in modo molto accurato la capacità di ripiegamento del DNA similmente a quanto avviene nei nucleosomi che costituiscono la base della struttura dei cromosomi.

## Slide 68
Cellula alveolare di topo. Immagine ottenuta in modo contatto.
L’AFM può anche essere utilizzata per visualizzare oggetti più grandi come cellule
pneumociti di tipo I, definiti anche piccole cellule alveolari, ricoprono circa il 90% della superficie alveolare totale. Sono cellule piccole, sottili le quali si sviluppano come un sottile film che ricopre la superficie dell' alveolo.

## Slide 69: Immagine 3D di un Biofilm batterico
Graffio con parziale rimozione del film
Batteri disidratati dopo divisione
Film senza batteri
15x15 m2

## Slide 70
Stretching polysaccharides on live cells using single molecule force
spectroscopy
Nature Protocols volume 4, pages 939–946 (2009) 28 May 2009

## Slide 72
Conclusions….

## Slide 74
Campioni di aggregati marini

## Slide 75: Outlook
AFM provides imaging, spectroscopy and
manipulation capabilities in almost any
environment:
ambient, UHV, liquid
at temperatures ranging from mK – 900 K
with atomic resolution and sensitivity
Derivative techniques:
  Magnetic Force Microscopy (MFM)
  Piezoresponse Force Microscopy (PFM)

## Slide 76
Molecule–molecule interactions –
STM studies at the solid–liquid interface: physisorption on graphite

## Slide 77
Assembly, Self–Assembly, Forced Assembly
Molecular self–assembly is the spontaneous association of molecules under equilibrium conditions into stable, structurally well defined aggregates joined by non–covalent bonds. Whitesides et al. Science 254, 1312 (1991)
Useful interactions (Non–covalent) for self–assembly:
Hydrogen bonds
Van der Waals interactions
Metal–organic coordination
Self–assembly of
15–hydroxypentadecanoic acid (HO(CH2)14COOH) on graphite (HOPG)
J.A. Miwa et al., unpublished

## Slide 78: Molecule–Molecule Interactions
hydrogen bonding:
physisorption; geometry & functionality
15–hydroxypentadecanoic acid
Trimesic acid (TMA)
Graphite HOPG:
Fairly inert, so that
coupling to the
substrate is weak

## Slide 79
Models of the different crystallographic structures found with their corresponding H–bonding scheme:
chickenwire structure, a ) b ) 1.7 nm, γ) 60°, area ) 2.5 nm2, 2 molecules per unit cell
(b) flower structure, a ) b ) 2.5 nm, γ) 60°, area ) 5.4 nm2, 6 molecules per unit cell.
Two possible structures for TMA:
Chickenwire or Flower (depending on the solvent)
Trimesic Acid SAM structures
Langmuir 20, 9403 (2004)

## Slide 80
Molecule–Molecule Interactions
hydrogen bonding:
physisorption; geometry & functionality
Trimesic acid (TMA)
Graphite HOPG: fairly inert, so that coupling to the substrate is weak
TMA + Heptanoic Acid on HOPG
a = b = 1.66 nm
Vs = –0.95 V, It = 250 pA
a = b = 2.63 nm
Vs = –0.95 V, It = 200 pA
Flower Structure
Chicken–wire structure

## Slide 81: H-bonded TMA molecular networks on HOPG
These structures were first observed in low temperature UHV-STM of TMA on HOPG
  Griessl et al., Single Mol. 3 (2002) 1, 25-31
At the solution/solid interface, these TMA structures exhibit a solvent-induced polymorphism
  Lackinger et al., Langmuir 21(2005), 4984-4988
Chicken-wire
Flower structure
a = b = 1.66 nm
a = b = 2.63 nm
Heptanoic acid
(n = 7)
Solvents
carboxylic acids with the general formula
CnH2nO
n > 7 = chicken wire TMA
n < 7 = flower TMA
Vs = –0.95 V, It = 250 pA
Vs = –0.95 V, It = 200 pA

## Slide 82: Mixing TMA and undecanol
J. Am. Chem. Soc. 128, 4212-4213 (2006)
TMA co-adsorbs with undecanol on HOPG
The alcohol ‘breaks’ the 3-fold symmetry of the substrate and the H-bonding unit, forming 1-dimensional tapes spaced by the alcohol itself
spacing: 3.5 nm
C11H23OH,
D = 1.85 nm, P = 3.5 nm

## Slide 83: Linear TMA patterns formed through cooperative adsorption
When alcohols co-adsorb with TMA, a linear pattern forms, made of dimerized TMA separated by alcohol lamellae
5.5 x 5.5 nm2, Vs = -800 mV, It = 20 pA
TMA/C17H35OH (heptanoic acid)
Alcohols
Fatty alcohols with the general formula
CnH2n+1OH
where 7 ≤ n ≤ 30
Undecanol
(n = 11)
J. Am. Chem. Soc. 128, 4212-4213 (2006)
J. Phys. Chem. C 111, 16996 (2007)

## Slide 84
16.3 x 16.3 nm2
TMA+ Heptanoic acid + Hexadecanol (C16) on HOPG
6.5 x 6.5 nm2
Dependence on Alcohol chain
C16, d~3.4 nm
J. Am. Chem. Soc. 128, 4212-4213 (2006)

## Slide 85
C16H33OH, D = 1.7 nm, P = 3.4 nm
600 Tilted orientation (zigzag plane II to HOPG)
Orthogonal orientation (zigzag plane ┴ to HOPG)
C17H35OH, D = 2.4 nm, P = 4.1 nm
Modulation induced by alcohol chains

## Slide 86
C11, d~3.5 nm
C16, d~3.4 nm
C17, d~4.1 nm
d
Modulation induced by different
Alcohol chains
d
d

## Slide 87
Rational modulation & Odd-even effect
All odd alcohols assemble with ~90o tilt vs lamellas direction
All even alcohols assemble with ~60o tilt vs lamellas direction
J. Phys. Chem. C 111, 16996 (2007)

## Slide 88: Parity effect
Even
Geometry of the TMA/alcohol bond depends on the parity of carbon count in the alcohol
  Odd alcohols prefer to orient at ~90° to the TMA dimer tape
  Even alcohols prefer to orient at ~60° to the TMA dimer tape
Odd
TMA/C22H45OH
(heptanoic acid)
7.5 × 7.5 nm2
Vs = –2.1 V, It = 100 pA
TMA/C17H35OH
(heptanoic acid)
8.3 × 8.3 nm2
Vs = –0.9 V, It = 90 pA
J. Phys. Chem. C 111, 16996 (2007)

## Slide 89
Shortest alcohol chains: C7, C8 (C6 does not work)
Longest chains: C27, C30
The adsorption properties of the alcohol are related to the length of the chain and to the parity of C atoms in the chain
Rational modulation
J. Am. Chem. Soc. 128, 4212-4213 (2006)
J. Phys. Chem. C 111, 16996 (2007)
Alcohol | L (nm)[a] | P (nm)[b] |  (o)[c]
C7H15OH | 1.06 | 2.74±0.16 | 83±2
C8H17OH | 1.19 | 2.69±0.12 | 64±2
C10H21OH | 1.44 | 2.91±0.07 | 64±2
C11H23OH | 1.57 | 3.36±0.09 | 86±2
C16H33OH | 2.21 | 3.57±0.10 | 66±2
C17H35OH | 2.34 | 4.10±0.09 | 83±2
C22H45OH | 2.99 | 4.29±0.07 | 64±3
C27H55OH | 3.63 | 5.32±0.15 | 82±3
C30H61OH | 4.02 | 5.08±0.11 | 66±2

## Slide 90: Chirality in TMA/alcohol SAMNs
TMA dimer tapes are prochiral
In STM images, chirality is communicated through the alcohol tilt
TMA/alcohol SAMN forms chiral domains
TMA (half) dimer enantiomers
TMA/C8H15OH (heptanoic acid)
13.5 × 13.5 nm2
Vs = –0.87 V, It = 250 pA
(b) 13.5 × 13.5 nm2
Vs = –0.93 V, It = 278 pA
J. Phys. Chem. C 111, 16996 (2007)

## Slide 91: X-ray crystallography of 3D crystals
The in-plane structure of TMA/alcohol SAMN is mimicked in 3D crystals
TMA/C6H13OH crystal
Even
TMA/C5H11OH crystal
Odd
Plan view
Section
TMA bonding/alcohol lamellae are analogous to SAMN
Parity effect is suppressed by additional freedom for bond rotation
J. Phys. Chem. C 111, 16996 (2007)

## Slide 92: New polymorphs at domain boundaries
Unusual TMA bonding geometries can be stabilized at domain boundaries in the TMA/alcohol SAMN
TMA/C16H33OH (octanoic acid)
15 × 15 nm2, Vs = -1.0 V, It = 300 pA
TMA/C16H33OH (octanoic acid)
20 × 20 nm2, Vs = -1.0 V, It = 300 pA
Boundaries of three domains can contain a fully-trimerically bonded TMA region
The “superflower” structure, predicted
by Lackinger et al. (Langmuir 2005)
The incomplete structure has the features of a next-generation polymorph related to chicken-wire and flower structure.
Nanotechnology 18, 424031 (2007)

## Slide 93: Homologic order of TMA polymorphs
Together with the known chicken-wire and flower structures, these new polymorphs imply a homologic order of TMA phases comprising trimeric and dimeric associations
Nanotechnology 18, 424031 (2007)

## Slide 94: TMA guest/host architectures
Griessl et al., J. Phys. Chem. B, Vol. 108, No. 31, 2004.
The open pores of the TMA chicken wire network can host C60 molecules.
C60
d ~ 0.7 nm
TMA/C17H35OH + chicken wire (heptanoic acid)
TMA/C22H45OH + flower (heptanoic acid)
62 × 53 nm2, Vs = -1.2 V, It = 300 pA
26 × 20 nm2, Vs = -0.9 V, It = 75 pA
Nanotechnology 18, 424031 (2007)

## Slide 95: TMA networks host other molecules
New molecule: sulflower
(d ~ 0.79 nm)
Chernichenko et al, Angew Chem Int Ed Engl. 2006 45:7367
TMA chicken wire + sulflower (heptanoic acid)
29 × 29 nm2, Vs = -1.2 V, It = 200 pA
TMA/C22H45OH chicken wire + sulflower (heptanoic acid)
60 × 60 nm2, Vs = -0.8 V, It = 75 pA

## Slide 96: Self-assembly of ‘sulflower’ molecules
Heterocirculenes: Sulflower, Selenosulflower – immobilized in a H-bonded matrix of TMA at the solid-liquid interface, imaged by STM
Circulenes: a rare class of polyaromatic compounds built from arenes annulated into macrocycles.
Coronene: the only planar benzenoid circulene
(a), (b) STM images with models (c), (d) of sulflower-TMA and selenosulflower-TMA SAMNs, respectively. 2.0×2.2 nm2 zoom of TMA/sulflower image next to model in (c).
Synthesis: K. Yu. Chernichenko et al., Angew. Chem. Int. Ed, 2006, 45, 7367.
Organic Electronics: A. Dadvand, F. Cicoira, K.Yu. Chernichenko, E.S. Balenkova, R.M. Osuna, F. Rosei, V.G. Nenajdenko, D.F. Perepichka, Chem. Comm. 5354 (2008)
Chem. Comm. 10, 1192 (2009)

## Slide 97: Modifying the TMA network
1.2 nm
Terthienophenetricarboxylic acid
(TTB)
A larger, three-fold hydrogen-bonding unit can be accommodated in the TMA chicken-wire phase
TMA/TTB chicken wire + TMA chicken wire (heptanoic acid)
30×30 nm2, Vs = -1.0 V, It = 100 pA
Unstrained TMA chicken-wire
Strained TTB+TMA chicken-wire

## Slide 98
J. Am. Chem. Soc. 131, 16844 (2009)
TTBTA/C60 guest/host architecture
TTBTA-C60 host-guest architectures with sparse fullerene coverage (a); one (b), two (c), and three (d) fullerenes per chicken wire unit cell.
Tentative molecular models are assigned to a 10.7×10.7 nm2 area of each image (indicated by dashed boxes in b-d).
10.7x10.7 nm2
18x18 nm2
18x18 nm2
18x18 nm2

## Slide 99
STM image (a) and model (b) of the TTBTA chicken wire structure formed at the HOPG/heptanoic acid interface.
TTBTA: new polymorph (close packed)
J. Am. Chem. Soc. 131, 16844 (2009)
STM image (a) and model (b) of the TTBTA close-packed structure formed at the HOPG/heptanoic acid interface (high solution concentration).
12.9x12.9 nm2
7.5x7.5 nm2

## Slide 100: Substrate-SAMN interactions
SAMN
Vs = -1600 mV
It = 200 pA
HOPG
Vs = -200 mV
It = 200 pA
TMA/C17H35OH (heptanoic acid)
[01-20]
Imaging the HOPG substrate and the SAMN in the same frame shows their relative alignment
Molecular mechanics simulations find an energy minimum for alcohol alignment along [01-20].

## Slide 101
Other bonding interactions:
halogen–halogen
Gutzler et al., Chem. Comm. 47, 9453 (2011)
Gutzler et al., Nanoscale 4, 5965 (2012)
Gatti et al., J. Phys. Chem. C 118, 25505 (2014)
Halogen–H interactions => new binding motifs
(a) TBTTA. (b) TBTTA monolayer at 1,2,4-trichlorobenzene/HOPG interface. Blue rectangle: unit cell of moiré pattern. (c) TBTTA monolayer with molecular model. Blue Rectangle: unit cell with one molecule (single-molecule defect in blue) (d) Enantiomeric counterpart to (c).
It = 100 pA, Vt = -800 mV
C-Br bond is stronger than X-H in H-bonded SAMNs => Advantageous in charge transport

## Slide 102: Orientation of TMA/alcohol domains
TMA/C17H35OH (heptanoic acid)
15 × 15 nm2
Vs = –800 mV (SAMN), Vs = –19 mV (HOPG), It = 80 pA
[01-20]
Domain orientation is guided predominantly by attractive C–H···π interactions between the alcohol alkyl chains and HOPG.
Odd/even effect may be suppressed due to substrate interaction
In general, in large-area images only TMA dimer tapes are imaged
TMA/ C17H35OH (heptanoic acid)
150 × 150 nm2
Vs = –850 mV, It = 60 pA

## Slide 103
From 2D to quasi-1D assemblies Making anisotropic patterns
J. Phys. Chem. 1996, 100, 19636.
As in 3D crystal engineering, 2D assembly of molecules is not easy to predict

## Slide 105: Studi Morfologici e Topologici (SHAPE & SIZE)
La microscopia di forza atomica (AFM: Atomic Force Microscopy) è una delle numerose possibilità che offre la microscopia che utilizza sonde di prossimità a scansione.
Tutte queste tecniche funzionano mediante la misura di proprietà locali (altezza, assorbimento di radiazione, magnetismo) attraverso una sonda o “punta” sistemata molto vicino al campione.

## Slide 106: La piccola distanza che c’è tra campione e sonda (dell’ordine della risoluzione strumentale) rende possibile eseguire la misura su un’area molto piccola che viene sistematicamente esplorata dalla sonda contemporaneamente alla misura della proprietà fisica in studio.
Contrariamente ai microscopi tradizionali, i sistemi con sonde
a scansione non utilizzano generalmente lenti e quindi la risoluzione è limitata più dalle dimensioni del campione che dagli effetti di diffrazione.

## Slide 107
Attraverso l’AFM si può non solo ottenere un’immagine (o meglio una mappa delle proprietà in studio) della superficie a risoluzione atomica, ma anche misurare la forza tra
superficie e sonda a livello di nano-newton.

## Slide 108: (SPM)

## Slide 109
La dimensione della porzione della sonda che si utilizza nella analisi (l’apice della punta) è di circa 10 nanometri.
La distanza tipica tra punta e campione negli SPM è circa 0.1 – 10 nm.
I diversi tipi di SPM sfruttano diversi tipi di interazione tra punta e campione. Per esempio l’STM si basa sul fenomeno della corrente di tunnel tra una punta metallica e un campione conduttore; e su diversi tipi di forza si basa il funzionamento dei microscopi a forza atomica, a forza magnetica e a forza elettrica.
Qui prendiamo in considerazione le caratteristiche comuni ai vari tipi di microscopi a scansione, supponendo che l’interazione punta campione sia descritta da un generico parametro P.

## Slide 111
L’immagine topografica della superficie può essere ottenuta in due modi:
a corrente costante, illustrato in Fig. 42 (a), la punta si muove sopra la superficie mentre il sistema di retroazione (FS) mantiene costante la distanza punta-campione ed il segnale Z=f(x,y) fornito all’elettrodo Z del piezoelettrico viene memorizzato, ed in seguito visualizzato come topografia.
ad altezza costante (Z = cost), risulta più efficace nell’analizzare superfici straordinariamente piatte. In questo caso la punta si muove sopra la superficie ad una distanza di alcuni Angstrom, e si memorizza il segnale di corrente I=f(x,y) come immagine STM (Fig. 42 (b)).
Questa modalità di acquisizione permette altissime velocità di scansione consentendo di osservare cambiamenti della superficie praticamente in tempo reale.

## Slide 112: (SPM)

## Slide 114
Laser
Specchio
Fotorivelatore
Amplificatore
Registratore
Campione
Sonda
Micro-leva

## Slide 116
L’effetto piezoelettrico=capacità di un
materiale di fornire una differenza di potenziale quando sollecitato
meccanicamente ovvero di deformarsi
se sottoposto ad un campo elettrico

## Slide 120
la punta AFM viene attratta a grandi distanze e respinta a brevi distanze dal campione

## Slide 127: Una visione ravvicinata delle punte mostra che esse sono arrotondate e la forma della punta generalmente limita la risoluzione della tecnica AFM per cui c’è una continua ricerca nel modo di produrre punte con una riproducibilità alta ed anche maggiormente affilate
Microfotografia di una punta per microscopia AFM. La barra delle dimensioni indica la lunghezza di un micrometro
1 m

## Slide 133: RISOLUZIONE DEGLI ESPERIMENTI AFM
La risoluzione laterale è generalmente definita dall’abilità di distinguere due punti separati su un’immagine. La risoluzione è determinata dalla geometria apicale della punta e dalla geometria del campione.
Generalmente la larghezza di una doppia elica di DNA viene utilizzata per valutare la risoluzione poiché il suo diametro è noto essere pari a 2,0 nm nella forma B.

## Slide 134: Paragone di diverse tecniche microscopiche.
 | conventional optical microscopy | scanning electron microscopy (SEM) | atomic force microscopy (AFM)
microscopic environment | ambient liquid vacuum | vacuum | ambient liquid vacuum
field depth | small | high | medium
focus depth | medium | small | small
Resolution x,y z | 100 nm n/a | 5 nm n/a | 0,1 - 1,0 nm 0,01 nm
magnification | 1x – 2∗103x | 10x - 106x | 5x102x - 108x
necessary sample preparation | low | critical point drying or freeze-drying, coating | low
necessary sample properties | samples do not have to be completely transparent for visible light | samples should not be charged and have to be vacuum compatible | samples should do not have excessive changes in height compared to tip geometry

## Slide 135: AFM imaging artifacts
West, Starostina, Pacific Nanotechnology, Inc.

## Slide 136
(Fillosilicati KAl2(Si3Al)O10(OH,F)2 )

## Slide 140: CURVE DI FORZA
Misura delle curve di forza
Il dispositivo AFM può anche registrare la quantità di forza sentita dalla leva quando la punta viene posta in vicinanza del campione – o anche tocca il campione – e poi viene allontanata.
Questa tecnica può essere utilizzata per misurare la forza attrattiva o repulsiva a lunga distanza tra la punta ed il campione; in questo modo si ottengono informazioni su proprietà chimiche e meccaniche locali del campione come per esempio l’adesione e l’elasticità oppure anche le dimensioni dello strato di molecole assorbite o la lunghezza di rottura di un legame.
Misure di questo tipo possono essere eseguite anche in modo oscillante sia in misura di ampiezza che in misura di fase che aggiungono ulteriori informazioni circa le proprietà dei campioni come dettagli circa le proprietà elettriche e magnetiche sulla superficie e le sue proprietà viscoelastiche.

## Slide 141
Al contrario della cristallografia a raggi X e della
microscopia permette non solo di ottenere
elettronica (TEM/SEM), l’AFM immagini dei campioni in condizioni
fisiologiche, ma anche di
“vedere” processi biologici mentre si svolgono.
Inoltre, in virtù del rapporto segnale-rumore (S/N) alto le informazioni che possono essere ottenute non sono ristrette ai soli campioni cristallini. Quindi, singole (macro)molecole anche non simmetriche possono essere visualizzate direttamente nel loro ambiente nativo.