## Slide 1
Flame Pyrolysis
Particle Formation and Growth by Gas Phase Chemical Reaction, Coagulation, Sintering and Surface Growth:
O2
TTIP
Molecules
TiO2
Molecules
TiO2
Particles
Ti
C3H7O
C3H7O
OC3H7
OC3H7
Titanium-Tetra-Iso-Propoxide
TiO2
Aggregates
Decreasing Temperature

## Slide 2
Flame Pyrolysis: Jet Design
CH4
CH4
CH4
Air
Air
Air
TiCl4
TiCl4
TiCl4
TiCl4
Air
Air

## Slide 3
Effect of Oxidant Composition on TiO2 Morphology:
CH4
CH4
Oxidant
Oxidant
TiCl4
TiCl4
Flame mixing B
Flame mixing C
Flame Pyrolysis: Jet Design

## Slide 4
Flame Pyrolysis: Nozzle Quenching
Vapor
Flame length is controlled by rapid quenching
Prevents agglomeration by inhibiting growth processes in the early stages of growth.
Provides precise control of particle size
Desired

## Slide 5
Nozzle Quenching controls flame length and particle size.
Flame Pyrolysis: Nozzle Quenching

## Slide 6
Flame Pyrolysis: Nozzle Quenching
TiO2 Particle Size Control by Nozzle Quenching

## Slide 7
Pyrolysis: Electrostatic Charging
Particle size can also be controlled by generating an electric field across the flame.
A large electric field (hundreds of kV/m) is generated between two plate electrodes situated on opposite sides of the flame.
Similar to nozzle quenching, the electric field limits particle growth by reducing the residence time in the high temperature region of the flame.
In addition, the electric field charges the particles. This results in electrostatic repulsion between newly formed particles, preventing coagulation.
S. Vemury, S.E. Pratsinis, L. Kibbey, Electrically-controlled flame synthesis of nanophase TiO2, SiO2, and SnO2 powders. JMR, Vol. 12, 1031-1042. 1997.

## Slide 8
Pyrolysis: Electrostatic Charging

## Slide 9
Pyrolysis is a high yield method that can fulfill the strong demand for nanoparticles.
Can be customized to produce unique nanoparticles.
Broad distribution of particle sizes and morphology.
Flame Pyrolysis: Advantages & Disadvantages

## Slide 10
Spray Pyrolysis
An aerosol process that
atomize a solution and
heats the droplets to
produce solid particles.
Simple and low cost for powder and thin film deposition process
Applicable to large areas;
No need of exotic or expensive precursors;
No need of vacuum.

## Slide 11
Spray Pyrolysis
Metals (Cu, Ni, Co,…) and metal oxides powders
Converting microsized liquid droplets of precursors or precursors mixture into solid particles trough heating
Droplets  evaporation  solute condensation  decomposition & reaction  sintering
e.g. silver particles made from Ag2CO3 or AgNO3 with NH4HCO3 @ 400 °C

## Slide 12
Spray Pyrolysis
The precursor must be dissolved in the liquid, but not react with it.
The product must not dissolve in the liquid, and must not react with the liquid.
There must be a large volume decrease for the reaction of precursor to product.
Transport of the leaching agent in the liquid and the fugitive compounds formed must be sufficiently rapid.

## Slide 13
Spray Pyrolysis Advantages
Spherical morphology
Narrow particle size distribution
Easy preparation of powders with complex formation
Relatively homogeneous composition
Continuously production
Reaction occurs at the microcapsule reactor (droplets)

## Slide 14
Spray Pyrolysis limitations
Technique is quite empirical, with a number of variables that can affect the final product:
- solute concentration
- atomization technique
- temperature, temperature gradient
- residence time in furnace
- carrier gases

## Slide 15
Spray Pyrolysis

## Slide 16
Spray Pyrolysis
Nozzle to substrate distance
Droplet size: relates to size of product
Substrate temperature
Solution concentration
Solution flow rate
Atomization rate – affects scalability of the process
Droplet velocity – affects residence time with the furnaces and ultimately size particle

## Slide 17
Spray Pyrolysis

## Slide 18
Messing et al. J. Am.Ceram.Soc 1993
Spray Pyrolysis

## Slide 19
Droplet to particles conversion process
Spray Pyrolysis

## Slide 20
Heating Time, Heating Temperature

## Slide 21
Spray Pyrolysis

## Slide 22
Low temperature and high initial solute concentrations Dense particles (aggregates of nanocrystals)
High temperature and high solvent evaporation rate Hallow particles
Nanoparticle < 100 nm
Dilute solutions and
very small initial droplet size
Spray Pyrolysis

## Slide 23
Conventional Spray Pyrolysis

## Slide 24
Low Pressure Spray Pyrolysis

## Slide 25
Low Pressure Spray Pyrolysis

## Slide 26
Salt-assisted Spray Pyrolysis

## Slide 27
Conventional vs Salt-assisted Spray Pyrolysis
Conventional Salt-assisted

## Slide 28
Electrospray Pyrolysis
By applying a 3KV electric field to the liquid coming from a cylindrical tube, it becomes conic.

## Slide 29
Electrospray Pyrolysis

## Slide 30
https://www.youtube.com/watch?v=I4w0nlrVU94

## Slide 31
https://www.youtube.com/watch?v=hRDD4l1dzaI

## Slide 32
https://www.youtube.com/watch?v=mmtXFlIQD9E
Spray Process

## Slide 33
Spray Pyrolysis: nanofilm
https://www.youtube.com/watch?v=eJbuY4HJFV0

## Slide 34
Flame Spray Pyrolysis: nanofilm
https://www.youtube.com/watch?v=pAYsH7xnV6s

## Slide 35: Chemical Vapor Deposition
Chemical vapor deposition (CVD) is a vacuum deposition method used to produce high quality, high-performance, solid materials from a gas precursor.
Thermal decomposition :
SiH4 (g) ⟶ Si (s) + 2 H2 (g) 650 °C
Reduction :
  WF6 (g) + 3 H2 (g) <-> W(s) + 6 HF (g) 300 °C
Oxidation :
SiH4 (g) + O2 (g) ⟶ SiO2 (s) + 2 H2 (g) 450 °C
Compound formation :
BF3 (g) + NH3 (g) ⟶ BN (s) + 3 HF (g) 1100 °C

## Slide 36: Chemical Vapor Deposition

## Slide 37
https://www.youtube.com/watch?v=9XKGVHPXXho

## Slide 38: Oxides preparation
Various metal oxides can be prepared by the reaction of a volatile metal compound (often a chloride) with O2 or water vapor:
MXn (g) + (n/4) O2 (g)  MOn/2 (s) + (n/2) X2 (g)
MXn (g) + (n/2) H2O (g)  MOn/2 (s) + n HX2 (g)
The water vapor can be directly introduced or obtain in the reaction chamber from a suitable reaction:
1) CO2 + H2 ↔ CO + H2O
2) O2 + H2  H2O
3) CxHy + O2 CO2 + H2O

## Slide 39: Chemical Vapor Deposition
Ultrahigh vacuum CVD (UHVCVD) – CVD at very low pressure, typically below 10−6 Pa ( ≈ 10−8 torr).
Low-pressure CVD (LPCVD) – CVD at sub-atmospheric pressures. Reduced pressures tend to reduce unwanted gas-phase reactions and improve product uniformity.
Atmospheric pressure CVD (APCVD) – CVD at atmospheric pressure.

## Slide 40: LPCVD
https://www.coursera.org/lecture/nanotechnology/chemical-vapor-deposition-process-demonstration-EWSQl

## Slide 41: CVD Classification by type of substrate heating
Hot wall CVD – CVD in which the chamber is heated by an external power source and the substrate is heated by radiation from the heated chamber walls.
Cold wall CVD – CVD in which only the substrate is directly heated either by induction or by passing current through the substrate itself or a heater in contact with the substrate. The chamber walls are at room temperature.

## Slide 42
CVD and Plasma methods
Plasma is a state of matter in which an ionized gases becomes highly electrically conductive to the point that long-range electric and magnetic fields dominate the behavior of the matter.
Plasma Enhanced CVD (PECVD)
CVD that utilizes plasma to enhance chemical reaction rates of the precursors. PECVD processing allows deposition at lower temperatures, which is often critical in the manufacture of semiconductors. The lower temperatures also allow for the deposition of organic coatings, such as plasma polymers, that have been used for nanoparticle surface functionalization.

## Slide 43
https://www.youtube.com/watch?v=gtJqNqXLg9w

## Slide 44
Direct synthesis of graphene on silicon oxide by low temperature plasma enhanced chemical vapor deposition
Nanoscale, 2018,10, 12779-12787

## Slide 45
Microwave plasma-assisted CVD (MPCVD)

## Slide 46
MW Plasma
Dissociation

## Slide 47
https://www.youtube.com/watch?v=n4hjudErUsQ
http://www.chm.bris.ac.uk/pt/diamond/mwpecvd1.htm

## Slide 48
N-V center defect consists of a nitrogen atom in place of a carbon atom next to a vacancy within the diamond’s lattice structure.
Nitrogen-vacancy Center: the blue atoms represent Carbon atoms, red atom represents Nitrogen atom substituting for a Carbon atom, and yellow atom represents a lattice vacancy

## Slide 49
Nanodiamonds: inertness and hardness
Skin care: Nanodiamonds are well-absorbed by human skin. They also absorb more of the ingredients in skin care products than skin itself. Thus they cause more of the ingredients to penetrate the deeper layers of the skin. Nanodiamonds also form strong bonds with water, helping to hydrate the skin.
Micro-abrasive: Polishes and engine oil additives for lubrication.
Catalysis: Support or metal free catalyst
Medical: low cytotoxicity of diamond nanoparticles affirms their utilization as biologically compatible materials. Drug delivery.
Sensors: electro- mechanical- system and response to magnetic field.
Optical and Quantum computing: Single-defect nanodiamonds.

## Slide 50
Remote Plasma-Enhanced CVD (RPECVD)
Similar to PECVD except that the wafer substrate is not directly in the plasma discharge region. Removing the wafer from the plasma region allows processing temperatures down to room temperature.

## Slide 51
CVD employing a high density, low energy plasma to obtain epitaxial deposition of semiconductor materials at high rates and low temperatures.
Low-Energy Plasma-Enhanced CVD (LEPECVD)

## Slide 52: RF Plasma Synthesis

## Slide 53: RF Plasma Synthesis
https://www.youtube.com/watch?v=5Un_HnOl6lQ