## Slide 3
Band-gap energies and relative band position of different semiconductors relative to the water oxidation/reduction potential (vs. NHE)
-2.0
-1.0
0
1.0
2.0
3.0
4.0
V vs NHE (pH=0)
H+/H2
ZrO2
TiO2
MoS2
KTaO3
SrTiO3
WO3
Fe2O3
ZnS
CdS
CdSe
GaP
SiC
Si
5.0
3.4
3.2
3.6
2.4
3.0
1.7
2.25
3.0
1.1
1.75
2.8
2.3 eV
O2/H2O

## Slide 4
Metal / TiO2
Conduction Band
Valence band
2H+
H2
e-
h+
hν
TiO2
H2O
2H++½O2
Thechnological solution: separation of red and Ox reactions
Chemical solution: use of sacrifical agents
Inorganic compounds: S2-/SO32-, Ce4+/Ce3+, IO3-/I-
Organic compounds: EDTA, methanol, ethanol, glycerol, etc.
Metal
H2O
+ ½ O2
cat

## Slide 5
Metal / TiO2
Formation of Schottky barrier
depends on metal work function
ChemistrySelect 2020, 5, 1013 –1019

## Slide 7
Pt/TiO2 photocatalysts were prepared through photodeposition procedure

## Slide 8
Cu/TiO2 photocatalysts were prepared through wet impregnation procedure
675 mmol h-1 g-1

## Slide 9
Pt/TiO2 photocatalyst was prepared through impregnation procedure
Unknown amount of Pt deposited on TiO2 films
Max H2 production in EtOH/water:
Approx. 11000 mmol h-1 g-1

## Slide 10
H2 production from ethanol
Possible pathway
Accumulated
in solution
ChemCatChem 3 (2011), 574-577

## Slide 11
TUNING TiO2 COMPOSITION
Rutile
Anatase
Brookite
R + A
A + B
A + B
160°C x 24h
+ Urea
TiO2
Appl. Catal. A-Gen. 518 (2016), 167-175

## Slide 12
TUNING TiO2 COMPOSITION
Ethanol/water solution
Simulated sunlight
Brookite:
Favorable electronic properties
Well defined morphology and exposed facets
Appl. Catal. A-Gen. 518 (2016), 167-175
Per mass
Per surface area
Pt 0.2 wt% added as co-catalysts

## Slide 13
TiO2 BROOKITE NANORODS
Montini et al. Proc. Nat. Acad. Sci., 113 (2016), 3966-3971

## Slide 14
TiO2 BROOKITE NANORODS
Montini et al. Proc. Nat. Acad. Sci., 113 (2016), 3966-3971
Per mass
Per surface area

## Slide 15
TiO2 BROOKITE NANORODS
Montini et al. Proc. Nat. Acad. Sci., 113 (2016), 3966-3971
Per surface area
50 fs ultraviolet (4.0 eV) pump pulse
Increase life-time of electron/hole pairs with length

## Slide 16
Pt/TiO2 photocatalysts were prepared through wet impregnation procedure

## Slide 17
Accumulated
in solution
H2 production from glycerol
Possible pathway
ChemCatChem 3 (2011), 574-577

## Slide 18
W.-D. Zhang, B. Xu, L.-C. Jiang, J. Mater. Chem. 20 (2010), 6383.
CNTs as electron sink
CNTs as sensitizer
TiO2/CARBON NANOMATERIALS
Formation of hybrid materials

## Slide 19
500 nm
20 nm
After calcination
Pd@TiO2/CARBON NANOTUBES
Green Chem. doi: 10.1039/C6GC01979J
EF-TEM
Porous Pd@TiO2 shell around CNT
Anatase phase

## Slide 20
Ethanol/water solution
Glycerol/water solution
Pd@TiO2/CARBON NANOTUBES
Green Chem. doi: 10.1039/C6GC01979J
H2 production under
UV-vis irradiation

## Slide 21
Pd@TiO2/CARBON NANOTUBES@Fe
Purification by magnetic separation
Before
After
Appl. Catal. B-Environ. 227 (2018), 356-365

## Slide 22
Pd@TiO2/CARBON NANOTUBES@Fe
Pd@TiO2/Fe@CNT-magnetic
Pd@TiO2/Fe@CNT-filtered
Pd@TiO2
EtOH : H2O = 1:1
UV-vis irradiation
Appl. Catal. B-Environ. 227 (2018), 356-365

## Slide 23
Pd@TiO2/CARBON NANOTUBES@Fe
Pd@TiO2/Fe@CNT-magnetic
EtOH : H2O = 1:1
Simulated Sunlight irradiation
Easily reusable by magnetic recovery from the reaction mixture!!!
Appl. Catal. B-Environ. 227 (2018), 356-365

## Slide 24
DYE SENSITIZED PHOTOCATALYSTS
Materials active under visible light (λ > 420nm)
Not sustainable Sacrificial Electron Donor

## Slide 25
ChemSusChem 8 (2015), 4216-4228
PHENOTIAZINE-BASED DYES
Effect of molecular structure

## Slide 26
ChemSusChem 8 (2015), 4216-4228
PHENOTIAZINE-BASED DYES
Active
&
Stable
Effect of molecular structure

## Slide 27
Sustain. Energ. Fuels, 1 (2017), 694-698
PHENOTIAZINE-BASED DYES
Effect of aromatic structure
Phenotiazine
Phenoxazine
Carbazole

## Slide 28
PHENOTIAZINE-BASED DYES
Effect of aromatic structure
High energy of LUMO
Ligand-to-Metal Charge Trasfer
Sustain. Energ. Fuels, 1 (2017), 694-698

## Slide 29
TRIPHENYLAMINE-BASED DYES
Toward sustainability
ChemSusChem 11 (2018), 793-805
AD48
TTZ3
TTZ4
TTZ5
EtOH / water solution
as sacrificial electron donor
l > 420 nm

## Slide 30
Chemical Vapor Deposition (CVD)
+
RF-sputtering
Morphology
Doping with F
Phase composition
THIN FILM PHOTOCATALYSTS

## Slide 31
a-Fe2O3
e-Fe2O3
b-Fe2O3
Montini et al. Adv. Funct. Mater. 24 (2014), 372-378
Ethanol/water solution
Simulated sunlight
Active for glycerol and glucose!!
b-Fe2O3
e-Fe2O3
Fe2O3 POLYMORPHS

## Slide 32
Fe2O3 POLYMORPHS

## Slide 33
Ethanol/water solution
Simulated sunlight
Montini et al. RSC Advances 4 (2014), 32174-32179
Ag/e-Fe2O3
Au/e-Fe2O3
Au/e-Fe2O3 active under vivible light (l > 420 nm)
Ag/e-Fe2O3 AND Au/e-Fe2O3