## Slide 1
TiO2 polymorphs
Appl. Catal. A - Gen. 2016, 518, 167–175

## Slide 2
TiO2 polymorphs
Appl. Catal. A - Gen. 2016, 518, 167–175

## Slide 3
TiO2 polymorphs
Appl. Catal. A - Gen. 2016, 518, 167–175

## Slide 4
Pt-Pd Bimetallic nanoparticles
Appl. Catal. B-Environ., 2018, 236, 88-98

## Slide 5
Pt-Pd Bimetallic nanoparticles
K2PdCl4
+
K2PtCl4
+ MUA + NaBH4
H2O/Acetone
CoRed nanoparticles
Appl. Catal. B-Environ., 2018, 236, 88-98

## Slide 6
Pt-Pd Bimetallic nanoparticles
K2PdCl4
+
K2PtCl4
+ MUA + NaBH4
H2O/Acetone
Appl. Catal. B-Environ., 2018, 236, 88-98

## Slide 7
Pt-Pd Bimetallic nanoparticles
Appl. Catal. B-Environ., 2018, 236, 88-98
K2PdCl4
+
Pt NPs
+ MUA + NaBH4
H2O/Acetone
PreRed nanoparticles

## Slide 8
MWCNT/Pd@TiO2 hybrid materials
​Green Chem. 2017, 19, 2379-2389

## Slide 9
MWCNT/Pd@TiO2 hybrid materials
​Green Chem. 2017, 19, 2379-2389

## Slide 10
MWCNT/Pd@TiO2 hybrid materials
​Green Chem. 2017, 19, 2379-2389

## Slide 11
MWCNT/Pd@TiO2 hybrid materials
EDS mapping
​Green Chem. 2017, 19, 2379-2389

## Slide 12
Fe@CNT/Pd@TiO2
hybrid materials
A) low magnification and B) high magnification HRTEM and C) HAADF-STEM images of sample Fe@CNTs/Pd@TiO2-magn thermally treated (inset of C: magnification showing the individual Pd NPs); D) EDX mapping showing carbon (red) and iron (green); E) EDX mapping showing titanium (blue), oxygen (red) and iron (green). (For interpretation of the references to colour in this figure legend, the reader is referred to the web version of this article.)
Appl. Catal. B-Environ., 2018, 227, 356-365

## Slide 13
Pd/CeO2/Al2O3 catalysts for CH4 combustion
Fresh

## Slide 14
Pd/CeO2/Al2O3 catalysts for CH4 combustion
Used 650°C for 72h

## Slide 15
Pt/CeO2/Al2O3 catalysts for CH4 combustion
Fresh

## Slide 16
Pt/CeO2/Al2O3 catalysts for CH4 combustion
Used 650°C for 72h

## Slide 17
Pd-Pt/CeO2/Al2O3 catalysts for CH4 combustion
Fresh

## Slide 18
Pd-Pt/CeO2/Al2O3 catalysts for CH4 combustion
Used 650°C for 72h