## Slide 1: Microscopia a scansione ad effetto tunnel
Punta
CORRENTE
COS’È?
Se sulla superficie ci sono delle asperità anche piccolissime la corrente di tunneling cambia intensità

## Slide 2
COME SI USA?
Percorso seguito dalla punta

## Slide 3
COSA VEDO?
Superficie (111) di Pt

## Slide 4
STM: Scanning Tunneling Microscopy
Developed by Binning and Rohrer at the IBM Zürich research laboratory in the early 1982 (Noble Prize in 1986)
Based on a new concept:
To examine a surface at very close range (near field) with a scanning probe, the position of which can be perfectly controlled in three dimensions to within ± 0.1 nm. The signal generated on each point by the interaction between the probe and the surface atoms is translated electronically into an image of the surface.
Technique for “topografical” investigation of surfaces

## Slide 5
Principle of the technique
“The principle of STM in straightforward. It consists essentially in scanning a metal tip over the surface at constant tunnel current. The displacements of the metal tip given by the voltage applied to the piezodrives then yield a topographic picture of the surface. The very high resolution of STM rests on the strong dependence of the tunnel current on the distance between the two electrodes, i.e., the metal tip and the scanned surface.”
G. Binning et al. Phys. Rev. Lett. 49 (1), 57-61 (1982)
Surface
Tip
Tunnel
Current
<1nm

## Slide 6
Tunnel effect
In classical physics, an electron cannot penetrate into or across a potential barrier if its energy E is smaller than the potential  within the barrier.
The quantum mechanics treatment predicts that an electron have a finite probability to exist behind the potential barrier.
This is called TUNNEL EFFECT

## Slide 7
Theoretical basis of tunnel effect
A quantum mechanic treatment predicts an exponential decaying solution for the electron wave function in the barrier. For a rectangular barrier of width d:
where

## Slide 8
Theoretical basis of tunnel effect
A quantum mechanic treatment predicts an exponential decaying solution for the electron wave function in the barrier. For a rectangular barrier of width d:
where
The probability of finding an electron behind the barrier of the width d is:
When a little bias potenzial V is applied between 2 electrodes (sample and tip, in this case), the tunneling of electrons results in a tunneling current I.
The tunneling current is proportional to propability of electrons to tunnel through the barrier:
It is necessary that the tip is very close to the surface to have a measureable current!

## Slide 9
Theoretical basis of tunnel effect – Bardeen Approach
In case of a negative potential on the sample the occupied states generate the current, whereas in case of a positive bias the unoccupied states of the sample are of importance. It should finally be mentioned that the probability of tunneling is larger for electrons which are close to the fermi edge due to the lower barrier.
The current is given by a combination of the local densities of states of the sample and the tip.

## Slide 10
Theoretical basis of tunnel effect – Bardeen Approach
Examples:
Imaging the occupied states of SiC() 3x3
Imaging the unoccupied states of SiC() 3x3

## Slide 11
Lateral resolution
Calculations and experiments showed that there is often a dz2 like state near the Fermi edge present at the apex atom which also predominantely contributes to the tunneling current. It is understood that this state (and also the pz like state) is advantageous for a «sharp» tip.
It is possible to obtain ATOMIC RESOLUTION of the surfaces investigated.

## Slide 12
Schematic rappresentation of an STM apparatus

## Slide 13
Modes of operation
1. Constant Current Mode
By using a feedback loop the tip is vertically adjusted in such a way that the current always stays constant.
A kind of a topographic image of the surface is generated by recording the vertical position of the tip.

## Slide 14
Modes of operation
1. Constant Current Mode
By using a feedback loop the tip is vertically adjusted in such a way that the current always stays constant.
A kind of a topographic image of the surface is generated by recording the vertical position of the tip.
2. Constant Height Mode
In this mode the vertical position of the tip is not changed. The current as a function of lateral position represents the surface image. This mode is only appropriate for atomically flat surfaces as otherwise a tip crash would be inevitable.

## Slide 15
COME È FATTO LO STRUMENTO?
0.38 mm

## Slide 16
Molecole di NH3 su una superficie Pt (111)

## Slide 17: Applicazioni alla catalisi
Struttura intermedia nella formazione di un ossido sul rodio
4030 nm2
5353 Å2
Distanza lungo il profilo
Altezza
3.0 Å invece di 2.7 Å
Rh (110) saturata con O

## Slide 18
L’STM COME UNA VIDEOCAMERA
Catalizzatore di rodio ricoperto di ossigeno esposto ad idrogeno
Superficie iniziale
1515 nm2
I step: l’onda
1 min
II step: la reazione continua
3 min
Superficie pulita
11 min
Un’onda chimica spazza il catalizzatore
Rh (110) saturata con O

## Slide 19
Rh (110) saturata con O

## Slide 20
Superficie iniziale
5050 nm2
Coppie di ossigeni
1 min
Specie intermedia
3 min
Fase finale
7 min
Si formano dei prodotti intermedi

## Slide 21
Superficie iniziale
6060 nm2
Reazione
4 min
Superficie pulita
10 min
Superficie finale
2h 39 min
Gli atomi di superficie si riarrangiano

## Slide 22
L’STM PER MISURE STATICHE
NO
NH3
NH3 + NO
Ammoniaca (NH3) + monossido di azoto (NO) sul platino (Pt)

## Slide 23
Example: CeO2 (111)
Surface of the crystal
200nm x 200nm
Flat
Terraces
Large enough for topographical study of the surface
Crystal of CeO2 provided by Commercial Crystal Inc., grown with (111) orientation

## Slide 25
Example: CeO2 (111)
10nm x 5 nm
M.A. Henderson et al.
Surface Science 526 (1-2), 1-18 (2003)
Cleaned surface
The main contribution to the STM image contrast originates from the oxygen 2p states.
H. Nöremberg et al. Physical Review Letters 79 (21), 4222-4225 (1997)

## Slide 26
Example: CeO2 (111)
20nm x 20nm
After cleaning:
sputtering with Ar+ + annealing in O2 up to 1000°C

## Slide 27
20nm x 20nm
Example: CeO2 (111)
After 3h H2 1x10-8 mbar 400°C
Single vacancy
Line
defect

## Slide 28
Example: CeO2 (111)
After 3h H2 1x10-8 mbar 400°C
Oxygen atoms around the vacancies are brighter.
Oxygen vacancies corrisponds to a CeIII in the first sub-layer.
For the explanation of the enhanced brightness of oxygen atoms one has to consider the possibility of a small charge transfer from vacancies to these oxygen atoms.
20nm x 20nm

## Slide 29
Difetti superficiali su CeO2 (111)
F. Esch, S. Fabris, L. Zhou, T. Montini, C. Africh, P. Fornasiero, G. Comelli, R. Rosei Science 309 (2005), 752
Annealing a 900°C
1 min
5 min

## Slide 30: Difetti singoli su CeO2 (111)
F. Esch, S. Fabris, L. Zhou, T. Montini, C. Africh, P. Fornasiero, G. Comelli, R. Rosei Science 309 (2005), 752

## Slide 31: Difetti multipli sotto superficiali su CeO2 (111)
Difetti superficiali di CeO2:
Siti di attivazione di piccole molecole
Stabilizzazione di cluster di Au attraverso interazione con difetti superficiali / sotto superficiali
F. Esch, S. Fabris, L. Zhou, T. Montini, C. Africh, P. Fornasiero, G. Comelli, R. Rosei Science 309 (2005), 752