## Slide 1
Important industrial processes
Process | Products
Reforming | Syn-gas (H2+CO+CO2) from HC
Water Gas Shift | H2 purification
Haber- Bosch | Ammonia synthesis
Fisher-Tropsch | Synthetic fuel from syn-gas
Methanol | Methanol from syn-gas
MTO | Olefins from methanol
HDS & HDN | Fuel purification
Hydrogenation | Fuel upgrading
Hydrocacking | Fuel upgrading
TWC | Exhaust purification

## Slide 2
Ammonia synthesis
Haber-Bosch process
T = 450°C, P = 100-300bar
Pressure
XNH3
T = 300 °C
T = 400 °C
T = 500 °C

## Slide 3
Ammonia synthesis
Catalysts: BASF-S6-10
Fe3O4 + Al2O3 + CaO + K2O
i = 0.50 - 0.67
Under reaction conditions, Fe3O4 is reduced to Fe.
Al2O3 and CaO have a structural effect, maintaining the surface area.
K2O has an electronic effect lowering Eatt.

## Slide 4
Ammonia synthesis
Surface composition of the catalyst

## Slide 5
Ammonia synthesis
Surface composition of the catalyst

## Slide 6
Ammonia synthesis
Extreme stability of the catalyst
At the operative temperature, the catalyst is in a “quasi liquid” form, allowing constant regeneration of the surface.

## Slide 7
Ammonia synthesis
Atomic or molecular route?
g
a
b
g
a
b

## Slide 8
Ammonia synthesis
Atomic or molecular route?

## Slide 9
Ammonia synthesis
Molecular route:
the surface would necessarily be saturated with N(ad) under steady-state conditions, since there would exist no channel through which this species could be removed.
Atomic route:
The steady-state concentration of N(ad) is:
N(ad) should decrease as pH2 increases.
It is possible to measure N(ad)

## Slide 10
Ammonia synthesis
The reaction proceeds through the atomic route and formation of N(ad) in the rate determining step.

## Slide 11
Ammonia synthesis
Potential energy diagram
Reaction steps

## Slide 12
Ammonia synthesis
Effect of K
K increases the sticking coefficient for N2.

## Slide 13
Ammonia synthesis
Effect of K
To favor N2 dissociation, back-donation must be promoted.
K
Fe
N
N
Promoter (K)
Poison
p*
s
N2
Fe

## Slide 15
Plant for Ammonia Synthesis

## Slide 16
The catalyst beds in a reactor for production of 1500 t NH3/day are, in round numbers, 100 m3 and contain 250 t of catalyst.
Reactor for Ammonia Synthesis

## Slide 17
The reactor may contain 2 catalyst beds and 2 internal heat exchangers inside a pressure shell:
Lower heat
exchanger
Upper heat
exchanger
First bed
Second bed
Reactor for Ammonia Synthesis

## Slide 18
A: The main flow (pale blue) first flows along the pressure shell and cools it. The gas is then heated in the lower heat exchanger and quench gas (green) is added.
B: In the first bed, both the temperature and the concentration increases. At the outlet from the first bed, the state of the gas is very near equilibrium (red curve).
C: The gas is cooled in the upper heat exchanger and the third inlet gas stream (dark blue) is added. This inlet stream was preheated in the upper heat exchanger.
D:In the second bed, both the temperature and the concentration increases.
E: The gas is cooled in the lower heat exchanger and leaves the reactor as the outlet stream (red).
Reactor for Ammonia Synthesis

## Slide 19
Methanol from syn-gas
Syn-gas
CO
CO2
H2
H2O
CH3OH
HCHO
CH3COOH
Fuels (MTO Process)
Additives (MTBE)
Catalyst: Cu/ZnO/Al2O3
T = 250 – 300 °C
P = 50 – 100 atm
Efficiency = 99%

## Slide 20
Methanol from syn-gas
Where does methanol come from?

## Slide 21
CO is not dissociated
13C16O + 12C18O + H2
CH3OH
Notes: Bassa resa

## Slide 22
Role of CO2: main source of CH3OH
CO
14CO2
H2
14CH3OH
The amounts of 14CO is negligible.
Methanol is produced from CO2 and no scrambling with CO takes place
Notes: Resa aumenta se viene aggiunta H2O e/o CO2

## Slide 23
The state of copper in the working catalyst
Auger / XPS / UV-vis
Cu(I)
BUT …. Characterization techniques are employed under conditions far from the real working conditions of the catalyst.

## Slide 24
The state of copper in the working catalyst
Later….
The surface of Cu in real-life catalyst is in a dynamic state, in which the most part of Cu(0) with partially oxidized Cu(I) formed by Oads and OHads.

## Slide 25
The role of ZnO and Al2O3
Al2O3 increases surface area of the catalyst.
ZnO increases surface area and dispersion of Cu(0) species involved in the rate determining step and stops any sulphur impurity, increase longevity of the catalyst.

## Slide 26
Views on the mechanism of the reaction
Notes: Non accordo assoluto su quale sia il reale funzionamento del catalizzatore. TPR, TPD, IR etc. suggeriscono che….

## Slide 27
The reactor
Methanol synthesis is exothermic
Equilibrium favored by high pressure

## Slide 28
Fischer-Tropsch process
Syn-gas
Hydrocarbons
Germany: World War II
USA: 1950s
South Africa: SASOL I (1)955) & SASOL II (1980)
South African Synthetic Oil Ltd.
All exothermic reactions

## Slide 29
Fischer-Tropsch process
The process can be considered as a polymerazion of –CH2– units, even if they are not present initially.

## Slide 30
Fischer-Tropsch process: suggested mechanisms
Hydroxymethylene intermediate
CO insertion mechanism

## Slide 31
Fischer-Tropsch process: suggested mechanisms
Hydroxymethylene intermediate
CO insertion mechanism
Never detected by experimental techniques

## Slide 32
Fischer-Tropsch process: first step requires CO dissociation
All the metals that promotes FT synthesis also dissociates CO easily to its elemental components. In FT process, it is later converted into CHads and CH2ads (confirmed by 13C NMR and HREELS).
Mechanicistic studies using diazomethane CH2N2
CH2N2 in inter gas flow
It forms adsorbed CH2 immediately when in contact with metal surface
Dimerization & desorption
No polymerization
Notes: Co, Ni, Fe, Pd, Ru

## Slide 33
Fischer-Tropsch process: first step requires CO dissociation
CH2N2 + H2 vs CO + H2
Mechanicistic studies using diazomethane CH2N2
Notes: Cu non è in grado di dissociare H2: quindi formazione di H è fondamentale per la produzione di idrocarburi.

## Slide 34
Fischer-Tropsch process: first step requires CO dissociation
CH2N2 + H2 vs CO + H2
Mechanicistic studies using diazomethane CH2N2

## Slide 35
Fischer-Tropsch process: first step requires CO dissociation
CH2N2 + H2 vs CO + H2
Mechanicistic studies using diazomethane CH2N2

## Slide 36
Fischer-Tropsch process
Schultz – Flory distribution
Propagation
Termination
(b-hydride elimination + terminal reduction)
Notes: Rn = frammento alchilico di lunghezza n
Pn = prodotto di lunghezza n
kp e kt siano indipendenti da n

## Slide 37
Fischer-Tropsch process
Schultz – Flory distribution
The distribution of products concentrations is governed by:
A succession of i steps will occur with probability . The chance to obtain the product Pi is proportional to or, in other words,
Notes: Rn = frammento alchilico di lunghezza n
Pn = prodotto di lunghezza n
kp e kt siano indipendenti da n

## Slide 38
Fischer-Tropsch process

## Slide 39
Fischer-Tropsch process
Notes: CO si adsorbe e si dissocia.
H2 si adsorbe e si dissocia.
O adsorbito viene rimosso come H2O o CO2, liberando i siti per adsorbimento di altro CO.
CHx formati polimerizzano per dare i prodotti

## Slide 40
Fischer-Tropsch process
The real mechanism is more complicated, considering that a complex mixture of products is obtained, comprising alkanes, alkenes, alcohols and aldehydes.

## Slide 41
Fischer-Tropsch process
The catalyst composition must be tuned to manipulate
Active phase with high : long C chains
Active phase with high : short C Chains
Catalyst:
Fe2O3 + CuO + K2SiO3
SASOL Process:
Fe + Cu + K2O + SiO2
Catalyst:
Oxygenated synthesis
Rh-based material
Main products: Alcohols, mainly ethanol
Catalyst for FT
Promoter for Fe2O3 reduction
Stabilizer for texture
????

## Slide 42
Fischer-Tropsch process
The catalyst composition must be tuned to manipulate
Active phase with high : long C chains
Active phase with high : short C Chains
Catalyst:
Fe2O3 + CuO + K2SiO3
SASOL Process:
Fe + Cu + K2O + SiO2
Catalyst:
Oxygenated synthesis
Rh-based material
Main products: Alcohols, mainly ethanol
Catalyst for FT
Promoter for Fe2O3 reduction
Stabilizer for texture
Promoter for CO dissociation

## Slide 43
Fischer-Tropsch process: SASOL I & II
Fixed bed reactor
220-350°C, 30bar
Low space velocity
Products: C1-C35 (waxes 45%, diesel & gasoline 32%)
Fluidized bed reactor
320-360°C, 25bar
High space velocity
Products: C5-C11 (gasoline)
FEED
H2 43%, CO 43%, CH4 12%, CO2 1%, N2 balance