## Slide 12
Position of the redox potentials of various metallic couples related to the energy levels of the conduction and valence bands of TiO2 Degussa P25 at pH=0

## Slide 14
Z-Scheme
Harvesting of visible light
Allowing the occurence of more energy demanding semireactions

## Slide 16
Types of photocatalytic reactions

## Slide 17
Mineralization of organic pollutants
Organic pollutant + O2
CO2 + H2O + minerals
semiconductor
hn> Ebg
The reaction is non-selective and pratically all organic pollutants can be degraded under selected conditions

## Slide 18
Mineralization of organic pollutants
Photoreactor
Sampling and analysis at various irradiation times

## Slide 20
Photocatalysis
Dyes degradation: TiO2-based materials
Chem. Phys. 339 (2007), 111-123.
J. Hazard. Mat. 146 (2007), 529-534.
Inorg. Chim. Acta 361 (2008), 3980-3987.
Apparent first order constant
for Methyl Orange degradation
TiO2
TiO2-B9
TiO2-N5
TiO2-B9N5
P25
Doping with B and/or N affects structure and activity.
B and /or N induces defects formation, increasing absorption of light.
k
Degradation products
MO
Notes: 20

## Slide 21
J. Am. Chem. Soc. 130 (2008), 9658-9659.
Photophys. Photochem. Sc. 8 (2009), 677-682.
Chem. Phys. Lett. 472 (2009), 212-216.
Chem. Phys. Lett. 483 (2009), 254-261.
Chem. Phys. Lett. 498 (2010), 113-119.
Photocatalysis
Dyes degradation: other materials
Bi2O3/Bi2O4-x nanocomposite
Methylene Blue
Decolourization (%)
Improved activity by formation of nanocomposites (Bi2O3, ZnO, NiO).
Un-conventional photocatalysts (MWO4, M = Co, Ni, Cu, Zn)
Bi2O3
Bi2O4-x
Notes: 21

## Slide 23
Photocatalytic deNOx

## Slide 24
Photocatalytic deVOCs

## Slide 27
Band-gap energies and relative band position of different semiconductors relative to the water oxidation/reduction potential (vs. NHE)
-2.0
-1.0
0
1.0
2.0
3.0
4.0
V vs NHE (pH=0)
H+/H2
ZrO2
TiO2
MoS2
KTaO3
SrTiO3
WO3
Fe2O3
ZnS
CdS
CdSe
GaP
SiC
Si
5.0
3.4
3.2
3.6
2.4
3.0
1.7
2.25
3.0
1.1
1.75
2.8
2.3 eV
O2/H2O

## Slide 28
Metal / TiO2
Conduction Band
Valence band
2H+
H2
e-
h+
hν
TiO2
H2O
2H++½O2
Thechnological solution: separation of red and Ox reactions
Chemical solution: use of sacrifical agents
Inorganic compounds: S2-/SO32-, Ce4+/Ce3+, IO3-/I-
Organic compounds: EDTA, methanol, ethanol, glycerol, etc.
Metal
H2O
+ ½ O2
cat

## Slide 29
Metal / TiO2
Formation of Schottky barrier
depends on metal work function
ChemistrySelect 2020, 5, 1013 –1019

## Slide 31
Pt/TiO2 photocatalysts were prepared through photodeposition procedure

## Slide 32
Cu/TiO2 photocatalysts were prepared through wet impregnation procedure
675 mmol h-1 g-1

## Slide 33
Pt/TiO2 photocatalyst was prepared through impregnation procedure
Unknown amount of Pt deposited on TiO2 films
Max H2 production in EtOH/water:
Approx. 11000 mmol h-1 g-1

## Slide 34
H2 production from ethanol
Possible pathway
Accumulated
in solution
ChemCatChem 3 (2011), 574-577

## Slide 35
TUNING TiO2 COMPOSITION
Rutile
Anatase
Brookite
R + A
A + B
A + B
160°C x 24h
+ Urea
TiO2
Appl. Catal. A-Gen. 518 (2016), 167-175

## Slide 36
TUNING TiO2 COMPOSITION
Ethanol/water solution
Simulated sunlight
Brookite:
Favorable electronic properties
Well defined morphology and exposed facets
Appl. Catal. A-Gen. 518 (2016), 167-175
Per mass
Per surface area
Pt 0.2 wt% added as co-catalysts

## Slide 37
TiO2 BROOKITE NANORODS
Montini et al. Proc. Nat. Acad. Sci., 113 (2016), 3966-3971

## Slide 38
TiO2 BROOKITE NANORODS
Montini et al. Proc. Nat. Acad. Sci., 113 (2016), 3966-3971
Per mass
Per surface area

## Slide 39
TiO2 BROOKITE NANORODS
Montini et al. Proc. Nat. Acad. Sci., 113 (2016), 3966-3971
Per surface area
50 fs ultraviolet (4.0 eV) pump pulse
Increase life-time of electron/hole pairs with length

## Slide 40
Pt/TiO2 photocatalysts were prepared through wet impregnation procedure

## Slide 41
Accumulated
in solution
H2 production from glycerol
Possible pathway
ChemCatChem 3 (2011), 574-577

## Slide 42
W.-D. Zhang, B. Xu, L.-C. Jiang, J. Mater. Chem. 20 (2010), 6383.
CNTs as electron sink
CNTs as sensitizer
TiO2/CARBON NANOMATERIALS
Formation of hybrid materials

## Slide 43
500 nm
20 nm
After calcination
Pd@TiO2/CARBON NANOTUBES
Green Chem. doi: 10.1039/C6GC01979J
EF-TEM
Porous Pd@TiO2 shell around CNT
Anatase phase

## Slide 44
Ethanol/water solution
Glycerol/water solution
Pd@TiO2/CARBON NANOTUBES
Green Chem. doi: 10.1039/C6GC01979J
H2 production under
UV-vis irradiation

## Slide 45
Pd@TiO2/CARBON NANOTUBES@Fe
Purification by magnetic separation
Before
After
Appl. Catal. B-Environ. 227 (2018), 356-365

## Slide 46
Pd@TiO2/CARBON NANOTUBES@Fe
Pd@TiO2/Fe@CNT-magnetic
Pd@TiO2/Fe@CNT-filtered
Pd@TiO2
EtOH : H2O = 1:1
UV-vis irradiation
Appl. Catal. B-Environ. 227 (2018), 356-365

## Slide 47
Pd@TiO2/CARBON NANOTUBES@Fe
Pd@TiO2/Fe@CNT-magnetic
EtOH : H2O = 1:1
Simulated Sunlight irradiation
Easily reusable by magnetic recovery from the reaction mixture!!!
Appl. Catal. B-Environ. 227 (2018), 356-365