## Slide 3
Band-gap energies and relative band position of different semiconductors relative to the water oxidation/reduction potential (vs. NHE)
-2.0
-1.0
0
1.0
2.0
3.0
4.0
V vs NHE (pH=0)
H+/H2
ZrO2
TiO2
MoS2
KTaO3
SrTiO3
WO3
Fe2O3
ZnS
CdS
CdSe
GaP
SiC
Si
5.0
3.4
3.2
3.6
2.4
3.0
1.7
2.25
3.0
1.1
1.75
2.8
2.3 eV
O2/H2O

## Slide 4
Metal / TiO2
Conduction Band
Valence band
2H+
H2
e-
h+
hν
TiO2
H2O
2H++½O2
Thechnological solution: separation of red and Ox reactions
Chemical solution: use of sacrifical agents
Inorganic compounds: S2-/SO32-, Ce4+/Ce3+, IO3-/I-
Organic compounds: EDTA, methanol, ethanol, glycerol, etc.
Metal
H2O
+ ½ O2
cat

## Slide 5
Metal / TiO2
Formation of Schottky barrier
depends on metal work function
ChemistrySelect 2020, 5, 1013 –1019

## Slide 6: Green Hydrogen production by photocatalysis
Overall water splitting
Drawbacks:
Easy recombination of H2 and O2
Possible photoleaching of materials

## Slide 7: Water splitting
Domen et al. Chem. Sci., 2019, 10, 3196
CoOOH/RhCrOx/SrTiO3:Al photocatalyst

## Slide 8: Water splitting
Domen et al. Chem. Sci., 2019, 10, 3196
Al is dopant of SrTiO3 reducing band gap
In the absence of CoOOH, holes migrate to RhCrOx, indicing leaching of Cr(VI)
Cr-deficient RhCrOx is able to activate O2 and recombine it with H2
CoOOH collect photoexcited holes and catalyse H2O oxidation, avoiding oxidative corrosion of the RhCrOx cocatalyst and corrosion
Amorphous TiO2 is used as protecting layer

## Slide 9: Water splitting
Domen et al. Joule 2, 2018, 509–520
STH = 0.4%
AQY

## Slide 10: Water splitting
Domen et al. Nature 598, 2021, 304-307
Photocatalytic solar hydrogen production from water on a 100 m2 scale
Installed at the Kakioka Research Facility within the University of Tokyo
More efficient separation membranes are required to produce high-purity H2

## Slide 11: Green Hydrogen production by photocatalysis
Overall water splitting
H2 evolution reaction
LHC

## Slide 13: Water splitting
BE AWARE !!!

## Slide 14: Water splitting
BE AWARE !!!

## Slide 15
Pt/TiO2 photocatalysts were prepared through photodeposition procedure

## Slide 16
Cu/TiO2 photocatalysts were prepared through wet impregnation procedure
675 mmol h-1 g-1

## Slide 17
Pt/TiO2 photocatalyst was prepared through impregnation procedure
Unknown amount of Pt deposited on TiO2 films
Max H2 production in EtOH/water:
Approx. 11000 mmol h-1 g-1

## Slide 18
H2 production from ethanol
Possible pathway
Accumulated
in solution
ChemCatChem 3 (2011), 574-577

## Slide 19
TUNING TiO2 COMPOSITION
Rutile
Anatase
Brookite
R + A
A + B
A + B
160°C x 24h
+ Urea
TiO2
Appl. Catal. A-Gen. 518 (2016), 167-175

## Slide 20
TUNING TiO2 COMPOSITION
Ethanol/water solution
Simulated sunlight
Brookite:
Favorable electronic properties
Well defined morphology and exposed facets
Appl. Catal. A-Gen. 518 (2016), 167-175
Per mass
Per surface area
Pt 0.2 wt% added as co-catalysts

## Slide 21
TiO2 BROOKITE NANORODS
Montini et al. Proc. Nat. Acad. Sci., 113 (2016), 3966-3971

## Slide 22
TiO2 BROOKITE NANORODS
Montini et al. Proc. Nat. Acad. Sci., 113 (2016), 3966-3971
Per mass
Per surface area

## Slide 23
TiO2 BROOKITE NANORODS
Montini et al. Proc. Nat. Acad. Sci., 113 (2016), 3966-3971
Per surface area
50 fs ultraviolet (4.0 eV) pump pulse
Increase life-time of electron/hole pairs with length

## Slide 24
Pt/TiO2 photocatalysts were prepared through wet impregnation procedure

## Slide 25
Accumulated
in solution
H2 production from glycerol
Possible pathway
ChemCatChem 3 (2011), 574-577

## Slide 26
W.-D. Zhang, B. Xu, L.-C. Jiang, J. Mater. Chem. 20 (2010), 6383.
CNTs as electron sink
CNTs as sensitizer
TiO2/CARBON NANOMATERIALS
Formation of hybrid materials

## Slide 27
500 nm
20 nm
After calcination
Pd@TiO2/CARBON NANOTUBES
Green Chem. doi: 10.1039/C6GC01979J
EF-TEM
Porous Pd@TiO2 shell around CNT
Anatase phase

## Slide 28
Ethanol/water solution
Glycerol/water solution
Pd@TiO2/CARBON NANOTUBES
Green Chem. doi: 10.1039/C6GC01979J
H2 production under
UV-vis irradiation

## Slide 29
Pd@TiO2/CARBON NANOTUBES@Fe
Purification by magnetic separation
Before
After
Appl. Catal. B-Environ. 227 (2018), 356-365

## Slide 30
Pd@TiO2/CARBON NANOTUBES@Fe
Pd@TiO2/Fe@CNT-magnetic
Pd@TiO2/Fe@CNT-filtered
Pd@TiO2
EtOH : H2O = 1:1
UV-vis irradiation
Appl. Catal. B-Environ. 227 (2018), 356-365

## Slide 31
Pd@TiO2/CARBON NANOTUBES@Fe
Pd@TiO2/Fe@CNT-magnetic
EtOH : H2O = 1:1
Simulated Sunlight irradiation
Easily reusable by magnetic recovery from the reaction mixture!!!
Appl. Catal. B-Environ. 227 (2018), 356-365

## Slide 32
DYE SENSITIZED PHOTOCATALYSTS
Materials active under visible light (λ > 420nm)
Not sustainable Sacrificial Electron Donor

## Slide 33
ChemSusChem 8 (2015), 4216-4228
PHENOTIAZINE-BASED DYES
Effect of molecular structure

## Slide 34
ChemSusChem 8 (2015), 4216-4228
PHENOTIAZINE-BASED DYES
Active
&
Stable
Effect of molecular structure

## Slide 35
Sustain. Energ. Fuels, 1 (2017), 694-698
PHENOTIAZINE-BASED DYES
Effect of aromatic structure
Phenotiazine
Phenoxazine
Carbazole

## Slide 36
PHENOTIAZINE-BASED DYES
Effect of aromatic structure
High energy of LUMO
Ligand-to-Metal Charge Trasfer
Sustain. Energ. Fuels, 1 (2017), 694-698