## Slide 1
TRIPHENYLAMINE-BASED DYES
Toward sustainability
ChemSusChem 11 (2018), 793-805
AD48
TTZ3
TTZ4
TTZ5
EtOH / water solution
as sacrificial electron donor
l > 420 nm

## Slide 2
Chemical Vapor Deposition (CVD)
+
RF-sputtering
Morphology
Doping with F
Phase composition
THIN FILM PHOTOCATALYSTS

## Slide 3
a-Fe2O3
e-Fe2O3
b-Fe2O3
Montini et al. Adv. Funct. Mater. 24 (2014), 372-378
Ethanol/water solution
Simulated sunlight
Active for glycerol and glucose!!
b-Fe2O3
e-Fe2O3
Fe2O3 POLYMORPHS

## Slide 4
Fe2O3 POLYMORPHS

## Slide 5
Ethanol/water solution
Simulated sunlight
Montini et al. RSC Advances 4 (2014), 32174-32179
Ag/e-Fe2O3
Au/e-Fe2O3
Au/e-Fe2O3 active under vivible light (l > 420 nm)
Ag/e-Fe2O3 AND Au/e-Fe2O3

## Slide 6
Photocatalytic oxidation of naphtalene in aqueous and organic solvents

## Slide 7
J. Catal. 2002, 211, 434-444
Selective oxidation of alcohols in gas phase using light activated TiO2

## Slide 8
Electric Vehicles Smart Fleets
Electric Unmanned aerial vehicles
ELECTRICAL VEHICLES

## Slide 9
1 MJ/Kg
2 hrs 250 Kg of batterie
7 hrs 260,000 Kg of batteries
ELECTRIC / HYBRID AIRCRAFT
43 MJ/Kg

## Slide 10
Nature Energy 4 (2019), 575-584
VISIBLE-LIGHT-DRIVEN COPRODUCTION OF DIESEL FUEL PRECURSORS AND HYDROGEN

## Slide 11
VISIBLE-LIGHT-DRIVEN COPRODUCTION OF DIESEL FUEL PRECURSORS AND HYDROGEN
Nature Energy 4 (2019), 575-584

## Slide 12
VISIBLE-LIGHT-DRIVEN COPRODUCTION OF DIESEL FUEL PRECURSORS AND HYDROGEN
Nature Energy 4 (2019), 575-584
Doped-ZnIn2S4 photocatalysts

## Slide 13
VISIBLE-LIGHT-DRIVEN COPRODUCTION OF DIESEL FUEL PRECURSORS AND HYDROGEN
Nature Energy 4 (2019), 575-584
3.3 mmol of H2 g cat-1 h-1
0.56 g of DPF g cat-1 h-1
AQY 15.2 %
2,5-DMF
2-MF
2,5-DMF + 2-MF
Ru-ZnIn2S4 photocatalyst

## Slide 14
VISIBLE-LIGHT-DRIVEN COPRODUCTION OF DIESEL FUEL PRECURSORS AND HYDROGEN
Ru-ZnIn2S4 photocatalyst
Nature Energy 4 (2019), 575-584

## Slide 15
VISIBLE-LIGHT-DRIVEN COPRODUCTION OF DIESEL FUEL PRECURSORS AND HYDROGEN
Ru-ZnIn2S4 photocatalyst
Nature Energy 4 (2019), 575-584
Radical mechanism
confirmed

## Slide 16
VISIBLE-LIGHT-DRIVEN COPRODUCTION OF DIESEL FUEL PRECURSORS AND HYDROGEN
Ru-ZnIn2S4 photocatalyst: role of Ru
Nature Energy 4 (2019), 575-584
Decreased band gap
Stabilization of e-/h+ pairs
Reduction of Ru ions to Ru(0) justifies slight deactivation

## Slide 17
Conventional synthesis of benzimidazoles:
Very toxic and
carcinogenic
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
T = 100 – 200 °C
Strong acidic conditions
Strong oxidants
Synthesis of natural products and pharmaceuticals (bactericides, anticarcinogens, peptic ulcera agents, etc.)
Metal complexes (homogeneous catalysts, sensors, etc.)

## Slide 18
Very toxic and
carcinogenic
T = 100 – 200 °C
Strong acidic conditions
Strong oxidants
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
Conventional synthesis of benzimidazoles:

## Slide 19
Alternative processes:
Less toxic reagents
Renewable and cheap solvent
[H]ads
hn, cat
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES

## Slide 20
Anatase
Brookite
Rutile
TiO2
TiO2-B,N
 | Composition (wt%) |  |  | Crystallite size (nm) |  |  | Surface area (m2 g-1)
 | Anatase | Brookite | Rutile | Anatase | Brookite | Rutile | 
TiO2 | 64 | 28 | 8 | 11 | 11 | 32 | 80
TiO2-B,N | 68 | 26 | 6 | 8 | 7 | 12 | 138
Mixture of polymorphs
High surface area
Improved by B,N doping
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
Inorg. Chim. Acta 520 (2021), n° 120289
TiO2-B,N

## Slide 21
Metal photodeposition
Metal/TiO2-B,N
Support +
metal nitrate
50% water- 50% ethanol
UV-vis irradiation
Pd 0.5wt%
Ag 0.5wt%
Pt 0.5wt%
Cu 1.0wt%
HAADF-STEM
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES

## Slide 22: Characterization of the M/TiO2-B,N
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
Inorg. Chim. Acta 520 (2021), n° 120289

## Slide 23: H2 production from ETHANOL 96%
Gas phase
Effect of:
Support
Metal
Doping TiO2, leaching is significantly reduced
More stable performances for TiO2-B,N supported catalysts
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
Cu/TiO2
Cu/TiO2-B,N
Inorg. Chim. Acta 520 (2021), n° 120289

## Slide 24: Synthesis of 2-methylbenzimidazole
Conditions:
60 mL DNB/NA 2mM in EtOH 96%
150 mg Pd/TiO2-B,N
Ar flow, 30°C
Simulated sunlight irradiation
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
Inorg. Chim. Acta 520 (2021), n° 120289

## Slide 25: Synthesis of 2-methylbenzimidazole
Conditions:
60 mL DNB/NA 2mM in EtOH 96%
150 mg Pd/TiO2-B,N
Ar flow, 30°C
Simulated sunlight irradiation
0
200
400
600
800
1000
1200
H
2
production rate
(
m
mol g
-1
h
-1
)
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
Inorg. Chim. Acta 520 (2021), n° 120289

## Slide 26
Inorg. Chim. Acta 520 (2021), n° 120289
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES

## Slide 27: Substituted 2-methylbenzimidazole
Br
Futher functionalization
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
Inorg. Chim. Acta 520 (2021), n° 120289

## Slide 28: 5-bromo-2-methylbenzimidazole
Br
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
Br-2-MBI
N-Et-2-MBI
2-MBI
Br-N-Et-2-MBI
Pt highly active and selective
Pd promotes hydrodehalogenation
Ag and Cu take long reaction time and selectivity is not satifactory
Inorg. Chim. Acta 520 (2021), n° 120289

## Slide 29: 5,6-dichloro-2-methylbenzimidazole
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
diCl-2-MBI
2-MBI
Cl-2-MBI
Pt highly active and selective
Pd promotes hydrodehalogenation
Inorg. Chim. Acta 520 (2021), n° 120289

## Slide 30: 5-carboxymethyl-2-methylbenzimidazole
PHOTOCATALYTIC SYNTHESIS OF BENZIMIDAZOLES
COOMe-2-MBI
COOMe-
2-MBI
COOMe-
N-Et-2-MBI
COOMe-
N-Et-2-MBI
Inorg. Chim. Acta 520 (2021), n° 120289

## Slide 31
Photocatalytic reduction of CO2 to solar fuels

## Slide 32
Photocatalytic reduction of CO2 to solar fuels
pH = 7
Highly negative reduction potential arises from change in ibridization of C
Proton-Coupled Electron Transfer (PCET) are preferred

## Slide 33
Photocatalytic reduction of CO2 to solar fuels
Schematic of the possible CO2 adsorption
configurations on surfaces of photocatalysts
The reduction potentials for the PCET reactions are within the range of −0.7 to −0.2 V and are close to the reduction potential of water (−0.414 V at pH 7). The reduction products of CO2 (HCHO, CH3OH, and CH4) require multielectron transfer, whereas the reduction of water is a two-electron process. Reduction of water therefore competes with the reduction of CO2. Because of this, the extent of hydrogen generation is greater in liquid-phase reactions compared to vapor-phase reactions.

## Slide 34
Photocatalytic reduction of CO2 to solar fuels
Photocatalytic CO2 reduction on (a) Ag-NaTaO3:Ca, (b) Ag-NaTaO3:Sr, and (c) Ag-NaTaO3:Ba in the liquid phase under UV irradiation. Figure legends: hydrogen (open circle), oxygen (solid circle), and CO (triangle).
ChemSusChem 2017, 10, 112– 118

## Slide 35
Photocatalytic reduction of CO2 to solar fuels
(a) Electronic absorption spectra of nitridation products of Zn2GeO4 and (b) corresponding photocatalytic methane product activities. (c) Curve depicting the recyclability and stablitity of the photocatalyst.
Eur. J. Inorg. Chem. 2017, 2017, 2195– 2200

## Slide 36
Photocatalytic reduction of CO2 to solar fuels
Comparison of (a) density of states and (b) relative band positions in (001) and (101) facets of TiO2. (c) Photocatalytic CO2 reduction to CH4 with different ratios of (001) to (010) facets in TiO2.
TEM image of HF0 and (b and c) FESEM images of HF4.5 and HF9.
J. Am. Chem. Soc. 2014, 136, 8839– 8842

## Slide 37
Photocatalytic reduction of CO2 to solar fuels
(a) Schematic illustration of the process of charge transfer and CO2 reduction in Cu2ZnSnS4/TiO2 heterostructures. (b) Comparison of photocatalytic activities of Cu2ZnSnS4/TiO2 with different compositions and individual Cu2ZnSnS4 and TiO2.
RSC Adv. 2017, 6, 38964– 38971

## Slide 38
Photocatalytic reduction of CO2 to solar fuels
(a) Schematic illustration of the process of Z-scheme charge transfer and CO2 reduction in α-Fe2O3/Cu2O heterostructures. (b) Comparison of yield of CO production with varying the Cu content in these heterostructures.
ACS Appl. Mater. Interfaces 2015, 7, 8631– 8639

## Slide 39
Photocatalytic reduction of CO2 to solar fuels
Tandem CH3OH oxidation and CO2 reduction by Ag and Ru complex, respectively. [Ru(bpy)3]2+ derivative and TaON are light absorbers.
Ru catalyst on
visible light absorbing C3N4
Re catalyst and organic dye on TiO2.