## Slide 1
Lattice Planes in 2 D
a
b
γ
Unit cell
Crystal lattice
Nodes
Three non-collinear lattice nodes define a crystallographic plane.
Because all nodes are equivalent, each lattice node lies on this plane
or on an equivalent plane by translation.
The set of equivalent planes forms a family of crystallographic planes.
They are parallel and equally spaced by a constant distance d (spacing).
Crystallographic Lattice Planes

## Slide 2
a
b
c
d211
1
2
1
1
2
1/2
a
b
c
1
2
1
1
2
Tacking one lattice node as the origin
one plane of the hkl family passes through it.
The successive parallel plane of the family cuts the crystallographic axes at a/h, b/k, c/l at a distance dhkl from the origin
Considering three non-collinear points of the lattice
a plane passing through these nodes is representative of the parallel family planes
In all lattice nodes passes one plane of this family
hkl are three integers that identify the family planes
The lattice planes are identified by integer triplets:
Miller Indices

## Slide 3: Families of Planes and Miller Indices
A family of planes parallel to an axis has index 0 for that axis (intercept at ∞)
True lattice planes have Miller indices that are coprime integers
It is convenient to extend Miller indices to all positive and negative integers (negative indicated with a bar)
In this way, one also accounts for families of planes that are not lattice planes in the strict sense (passing through nodes), but are parallel to lattice planes and have spacings that are integer submultiples of those of true lattice planes
Two families differing only by sign represent the same planes viewed in opposite directions
True lattice planes
True lattice planes

## Slide 4: Family of planes, crystal faces and crystal direction
The Miller indices hkl are used to indicate:
Indices of reflection from a family of planes: hkl without brackets
Family of planes or Crystal face: (hkl) with round brackets
All symmetrically equivalent faces or planes: {hkl} with curly brackets
Crystal direction: [uvw] with square brackets (direction passing through the origin and the lattice node uvw)
[010]
[001]
[100]
(001)
(010)

## Slide 5: Crystal Morphology – Bravais Law
Crystal faces are parallel to lattice planes with high node density.
Flat faces and sharp edges

## Slide 6
Scattering of Light
A charged particle generates an electric field.
Charged particles are accelerated by electric fields.
The acceleration of a charged particle perturbs the electric field.
The acceleration of electrons generates photons!
This process is called scattering.
When an electron interacts with an electromagnetic wave, it can oscillate at the same frequency and become a source of radiation.
From the analysis of scattering, one can determine the position of the scatterers.

## Slide 7
Distance Between Sources
3 wavelengths
1°
2°
3°
Distance Between Sources
5 wavelengths
1°
2°
3°
4°
5°

## Slide 8: Waves in the Argand Diagram
Waves F are characterized by an amplitude |F| and a phase f
F = |F| exp(if) = |F| (cosf+isenf)
Monochromatic radiation
Waves can be represented as complex numbers

## Slide 9: Interference of Electromagnetic Waves
The result of the sum of two coherent waves (same frequency) depends on the phase difference (Interference).
In phase
(constructive interference)
In opposite phase
(destructive interference)
Partially out of phase

## Slide 10: Sum of Waves in the Argand Diagram
Two waves in phase
constructive interference
total amplitude |F|t = 2|F|
Two waves not in phase
partially destructive interference
total amplitude |F|t < 2|F|
Two waves in opposite phase
destructive interference
total amplitude |F|t = 0

## Slide 11: The Crystal Lattice
N atoms per unit cell
N equivalent interpenetrating lattices,
each with corresponding atoms at the vertices

## Slide 12: Reflection
q1’
q2
O
P
q1 = q2 reflection condition
Constructive interference when optical paths are equal
optical path = optical path
Constructive interference of waves scattered by a crystal plane

## Slide 13: Bragg Law
q
q
O
P
Constructive interference 2dsenq = nl
d
q
Constructive interference of waves scattered by a family of crystallographic planes

## Slide 14
Constructive interference 2dhklsenqn(hkl) = nl
true lattice planes (coprime integers)
n = reflection order
d102
Bragg Law and Miller indices
2dn(hkl)senqn(hkl) = l
2dhklsenqhkl = l
Miller indices with any integer
2d102senq2°(102) = 2l
2d204senq204 = l
d204
q204
q204

## Slide 15
Family planes1 0
Reflection 1 0
Family planes2 0
Family planes-1 0
Reflection -1 0
Reflection 2 0
Family planes-2 0
Reflection -2 0
Family planes0 -1
Reflection 0 -1
Family planes0 1
Reflection 0 1
Family planes0 -2
Reflection 0 -2
Family planes0 2
Reflection 0 2
Family planes1 -1
Reflection 1 -1
Family planes-1 1
Reflection -1 1
Family planes1 1
Reflection 1 1
Family planes-1 -1
Reflection -1 -1
Real lattice
Reciprocal lattice

## Slide 16: Direct and Reciprocal lattice
a*┴ b
a*┴ c
b*┴ a
b*┴ c
c*┴ a
c*┴ b
a*·b = 0
a*·c = 0
a*·a = 1
b*·b = 1
b*·c = 0
b*·a = 0
c*·b = 0
c*·c = 1
c*·a = 0
a*=1/a·cos(a*a)=Abc/Vabc
^
b*=1/b·cos(b*b)=Aac/Vabc
^
c*=1/c·cos(c*c)=Aab/Vabc
^

## Slide 17
The diffraction pattern is a 2D projection of the 3D reciprocal lattice.
Ewald sphere
Each time a reciprocal lattice point hkl intersects the Ewald sphere, a diffracted beam hkl is produced.
2 senq/l = 1/dhkl
d

## Slide 18
X-ray source
Detector
Diffraction experiment