## Slide 2
Coprecipitation

## Slide 4
Example: hydroxyapatite
Ca10(PO4)6(OH)2
Simple precipitation by increase of pH

## Slide 5
Direct coprecipitation
https://doi.org/10.1016/j.heliyon.2024.e34413
Phase purity
Broad size distribution
Key points are :
Comparable solubility of hydroxides
Intermediate aging (dissolution – reprecipitation)
CoFe2O4

## Slide 6
Direct coprecipitation
Zr(OH)4 pH  2
Ce(OH)3 pH  7.5
Zr(OH)4 pH  2
Ce(OH)4 pH  1
Preliminar oxidation of CeIII to CeIV woth (NH4)2S2O8
With
(NH4)2S2O8
Without
(NH4)2S2O8
Ce0.5Zr0.5O2
Precipitation of Ce and Zr precursors by addition of NH4OH.
XRD analysis of samples calcined at 1000 °C

## Slide 7
Inverse coprecipitation
Ce0.5Zr0.5O2
Precipitation by addition of Ce and Zr precursors to NH4OH.
Instantaneous quantitative precipitation of metal ions.
The statistical distribution of cations is «freezed» and maintained in the final oxide product.
XRD analysis of samples calcined at 1000 °C