## Slide 1
Detector
Sample
X-rays
Absorption
X-rays
Sample
I
wavelength
Imaging
Detector
X-rays
Elemental analysis
8800
0.0
8800
9000
9200
9400
9600
9800
10000
1.0
2.0
E (eV)
9000
9200
9400
9600
9800
10000
Energy
m
Detector
Fluorescence

## Slide 2
sample
x-rays
I0
I1
transmission experiment
XANES
X-ray Absorption Near Edge Structure
EXAFS Extended X-ray Absorption Fine Structure
measured at Alba/CLÆSS
XAFS: X-ray Absorption Fine Structure

## Slide 3
Beamline structure
Optical hutch
Experimental hutch
Front-end

## Slide 4
Beamline structure
Optical hutch
Mirrors
Metal thin film on substrate
Bended by piezoelectric devices

## Slide 5
Monochromator
Beamline structure
Monochromator:
Si single crystals
(111)
(220)
(311)
Double-crystal
monochromator

## Slide 6
Monochromator – harmonic rejection by detuning
Rocking curve
Depends on l
l is diffracted by both the crystals and exits the monochromator.
l/2 is eliminated from the beam.
Detuning

## Slide 7
Monochromator – harmonic rejection by mirrors
Mirrors work under gracing incidence
Transmitted (higher frequency)
Reflected (lower frequency)

## Slide 8
Experimental hutch
Ionization
chamber

## Slide 9
Experimental hutch
Ionization chamber
Fluo detector

## Slide 13
Ex-ray
Qualitative Picture of XAFS
x-ray
Ex-ray
E photoelectron
K 1s
L2 2p1/2
L3 2p3/2
L1 2s
M1–M5
continuum
EF
X
Isolated atom
The outgoing wave is scattered by neighbors
X
Single
Scattering

## Slide 14
Qualitative Picture of XAFS
constructive interference –
absorption maximum
destructive interference –
absorption minimum
Here is where the interference is important!
X
Multiple
Scattering

## Slide 15
A. Di Cicco, A. Filipponi, J. P. Itié and A. Polian, Phys. Rev. B 54 (1996) 9086-9098
High-pressure EXAFS of solid and liquid Kr
Liquid
Solid
Gas

## Slide 16
XANES vs EXAFS
Inelastic mean free path

## Slide 17
EXAFS standard formula

## Slide 18
EXAFS standard formula
  absorber-scatterer distance: Ri
  coordination numbers: Ni
disorder along the absorber – scatterer distance: s2
passive electron relaxation: S02
finite photo-electron mean free path: l(k)
function of scattering amplitude: fi(k)
  phase function: i(k)
A
Sj
Ri
Notes: mettere colori secondo che si voglia conoscere o si conoscano i parametri

## Slide 19
E0
m0
Dm
FT[
]
Outline of EXAFS analysis
2
1
Background subtraction
2
Fourier Transform
Ni K-edge
1

## Slide 20
Subtraction of atomic background and normalization

## Slide 21
Subtraction of atomic background and normalization

## Slide 22
Extraction of EXAFS signal

## Slide 23
The FT-c(k)

## Slide 24
The FT-c(k)
Unpleasant thing about EXAFS: FT positions are shifted towards small distances. More unpleasant: Each FT peak has its own shift.
Because of the phase shifts, extracting the
structural information from EXAFS requires curve fitting with assumed (calculated) phase shifts.

## Slide 25
The back-trasformed c(k)

## Slide 26
R = 1.25 – 3.0
R = 3.0 – 5.5
The back-trasformed c(k)

## Slide 27
The back-trasformed c(k)
R = 1.25 – 3.0
R = 3.0 – 5.5

## Slide 28
What we can learn from XANES: a) Pre-edge Peak
Dipole selection rule (only in central-symmetric case!): l = ±1
Consider K-absorption for transition metals:
initial state = 1s (l=0)
states near EF are formed by nd electrons (l=2)
central-symmetry | non-central symmetry
no resonance | resonance (pre-edge peak)
from [F. Farges, G. E. Brown, J. J. Rehr,
Phys. Rev. B 56 (1997) 1809]
T. Ressler et al. J. Phys. Chem. B 104, 27 (2000) 6360-6370

## Slide 29
What we can learn from XANES: a) Pre-edge Peak

## Slide 30: What we can learn from XANES: b) Edge Shift
T. Ressler, R. E. Jentoft, J. Wienold, M. M. Günter and O. Timpe:
J. Phys. Chem. B 104, 27 (2000) 6360-6370
I. Arčon, B. Mirtič, A. Kodre, J. Am. Ceram. Soc. 81 (1998) 222–224
Why does it shift?
1) Electrostatic: it is harder for the photoelectron to leave a positive (oxidized) atom
2) Shorter bonds at higher oxidation states  Fermi energy is higher

## Slide 31: What we can learn from XANES: b) Edge Shift
Why does it shift?
1) Electrostatic: it is harder for the photoelectron to leave a positive (oxidized) atom
2) Shorter bonds at higher oxidation states  Fermi energy is higher

## Slide 32: What we can learn from XANES: b) Edge Shift
Why does it shift?
1) Electrostatic: it is harder for the photoelectron to leave a positive (oxidized) atom
2) Shorter bonds at higher oxidation states  Fermi energy is higher
Au(iPr2Im)ACN

## Slide 33
a) Pt3 triangle (dashes), Pt4 tetrahedron (solid), Pt5 triangular bipyramid (dash-dot), and Pt6 octahedron (dash-dot-dot);
(b) Pt7 and Pt4 clusters of different shape: planar ‘‘honeycomb,(dashes), D5h bipyramid (solid) , single-capped
octahedron (long dashdot), Pt4 tetrahedron (dots), and Pt4 planar rhombus (dash-dot).
from A. L. Ankudinov, J. J. Rehr, J. J. Low, and S. R. Bare, J. Chem. Phys. 116 (2002) 1911
What we can learn from XANES: c) White Line
G. Meitzner, G. H. Via, F. W. Lytle, and J. H. Sinfelt, J. Phys. Chem. 96 (1992) 4960
L3 absorption edges for 5d metals:
(transition 2p3/2  5d)
Intensity is proportional to the number of free 5d states and also depends on valence state. But…
…white line also depends on particle size and morphology:

## Slide 34
What we can learn from XANES: c) White Line

## Slide 35
What we can learn from XANES: d) Speciation
By Linear Combination Analysis

## Slide 36
What we can learn from XANES: d) Speciation
By Linear Combination Analysis
G(CN)-Au sample is composed by 48.6 mol% of Au(0) and 51.4 mol% of Au(I).

## Slide 37: XAS and small objects: coordination numbers
Infinite lattice
A common subject: bulk metal versus metal clusters.
All atoms are both absorber and scattering centers.
Bulk: any atom is equivalent to the others;
Cluster: surface atoms have a diminished coordination number.
The average first coordination number depends on the size, i.e. surface to bulk ratio.
Small cluster
The EXAFS coordination number
is the weighted average
of the coordination numbers of all absorbers.

## Slide 38
Example: Ag/CeO2

## Slide 39
Reduction treatment: in 5%H2/He atmosphere, stepwise with T=50°C.
Measurements at LN2 temperature in order not to have interference of two effects: (i) due to different temperature vibrations and (ii) due to different particle sizes.
Example: Application of EXAFS to Pd,Pt/C Catalysts (b)

## Slide 40
Reference compound: metallic Pd foil
The difference between a simply reduced Pd/C sample (hydrided) and one subsequently blown out by He flow (dehydrided)
Example: Application of EXAFS to Pd,Pt/C Catalysts (c)
Checking your amplitudes and phases with reference spectra must be always the first step in every EXAFS study!

## Slide 41
Metallic nanoparticle size determination by EXAFS
Zastita Materijala 57 (2016), 101 – 109
doi:10.5937/ZasMat1601101M

## Slide 43
Mean coordination number for concentric shells

## Slide 44
Size determination by EXAFS

## Slide 45
Determination of shape by EXAFS
J. Catal. 190 (2000), 182–190

## Slide 46
FFT (k3 )
R (Å)
Ridotto a 773 K
Cubottaedro
FFT (k3 )
R (Å)
Ridotto a 773 K
Icosaedro
FFT (k3 )
R (Å)
Ridotto a 773 K
Decaedro
Determination of shape by EXAFS
J. Catal. 190 (2000), 182–190

## Slide 47
Oxide nanoparticle size determination by EXAFS
Nanosized NiO
IUCrJ 1 (2014), 571–589
doi:10.1107/S2052252514021101

## Slide 48
Oxide nanoparticle size determination by EXAFS
Nanosized NiO
IUCrJ 1 (2014), 571–589
doi:10.1107/S2052252514021101

## Slide 49
Oxide nanoparticle size determination by EXAFS
Nanosized NiO
IUCrJ 1 (2014), 571–589
doi:10.1107/S2052252514021101

## Slide 50
J. Electrochem. Soc., 165 (2018) J3222-J3230
Pt(ML)/Pd/C electrocatalyst for ORR
N(PtPt) = 5.8 ± 0.8
N(PtPd) = 2.7 ± 0.7
The total coordination
number for Pd atom,
N(PdM) = 11 ± 0.7
Estimated Particle size: 5.0 nm
From Pt L3 edge
From Pd K edge