## Slide 1
Synthesis
Nanosized material: ZnS quantum dots for sensing
Nanocomposite materials: TiO2 by sol-gel
Nanostructured materials: Ti-MCM-41

## Slide 2
Nanosized material: ZnS quantum dots for sensing
Mn-doped ZnS QDs were synthesized according to a reported method with some modification (Scheme 1).
Fifty milliliters of 0.03 M NAC, 5 mL of 0.10 M ZnSO4 and 1.5 mL of 0.01 M MnCl2 were added to a three-necked flask. The mixed solution was adjusted to pH ≈ 11 with 2 M NaOH and stirred under nitrogen at room temperature for 40 min. Five milliliters of 0.10 M Na2S were then quickly injected into the solution. The mixture was stirred for 40 min, and then the solution was aged at 50 °C under air for 2.5 h to form NAC-capped Mn-doped ZnS QDs. The QDs were precipitated with ethanol, separated by centrifuging, washed with ethanol and dried in a vacuum. The prepared QDs powder is highly soluble in water.
Colloidal synthesis

## Slide 3
Nanosized material: ZnS quantum dots for sensing
Student | V NAC | V Zn2+ | V Mn2+ | V S2-
1 | 100 | 5.00 | 0 | 5.00
2 | 100 | 5.00 | 1.50 | 5.00
3 | 100 | 5.00 | 3.00 | 5.00
Prepare the NAC solution
Add solutions with Zn2+ and Mn2+
Correct pH to 11 using NaOH 2M (use indicator paper)
Stir for 20 min
Add solution with S2- and stir 20 min
Increase temperature to 50°C and stir for 2 h
Separate the suspension in 4 vials
Precipitate Mn:ZnS-NAC QDs adding 25 mL of 2-PrOH in each vial
Centrifuge 5000 rpm, 10 min
Disperse the product in 10 mL of H2O and precipitate with 25 mL of 2-PrOH
Disperse the product in 10 mL of 2-PrOH and transfer into a single vial.
Centrifuge and dry the product in air overnight
Characterization
XRD
Fluorescence
DLS
SAXS
TEM

## Slide 4
Nanosized material: ZnS quantum dots for sensing
Prepare a solution of Mn:ZnS-NAC in water with 50 mg/L
Fluorimetric detection of Co2+
Test | V Mn:ZnS-NAC | V PBS | V Co2+ | V H2O
1 | 4.0 | 5.0 | 0 | 1.0
2 | 4.0 | 5.0 | 0.9 | 0.1
3 | 4.0 | 5.0 | 0.8 | 0.2
4 | 4.0 | 5.0 | 0.6 | 0.4
Prepare the mixtures into a 15 mL vial
Measure the fluorescence spectrum of the QDs using lexc = 315 nm
Plot F0/F vs [Co2+]

## Slide 5
Nanocomposite materials: TiO2 by sol-gel
TiO2 samples were prepared by a sol–gel method as follows. Typically, 17.0 g of Ti(OBu)4 were dissolved at 25 °C in 40.0 mL of anhydrous ethanol to form the solution 1. Meanwhile, 3.0 mL of concentrated HNO3 were mixed with 35.0 mL of anhydrous ethanol and 15.0 mL of water to prepare the solution 2. Then the solution 1 was added drop-wise into the solution 2 within 20 min under vigorous stirring. The solution was continuously stirred for 30–60 min until the formation of TiO2 gel. After aging for at least 24 h at room temperature, the as-prepared TiO2 gel was dried at 120 °C for 12 h. The obtained solid was ground and annealed at 450 °C for 6 h with a heating rate of 3 °C/min.

## Slide 6
Nanocomposite materials: TiO2 by sol-gel
Student | Solution 1 |  | Solution 2 |  | 
 | m Ti(OBu)4 | V EtOH | V H2O | V EtOH | V HNO3
1 | 8.5 g | 15 + 5 mL | 7.5 mL | 17.5 mL | 1.0 mL
2 | 8.5 g | 15 + 5 mL | 7.5 mL | 17.5 mL | 2.0 mL
3 | 8.5 g | 15 + 5 mL | 7.5 mL | 17.5 mL | 3.0 mL
Prepare Solution 1 in a plastic vial. Close carefully the vial to avoid hydrolysis
Prepare Solution 2 into a 100 mL flask with magnetic stirrer
Withdraw Solution 1 with a 20 mL plastic syringe and drop it slowly into Solution 2 under stirring.
Rinse the vial with 5 mL of EtOH and add it into the flask
Start a timer on your smartphone
Continue stirring gently: when the gel will be formed, the magnetic bar will stop!
Stop the timer and record the time required to form the gel
Leave the gel standing for at least 24 h
Dry the material at 120 °C overnight
Grind the solid product into a mortar and calcine at 450 °C for 6 hours (heating rate of 3 °C/min)
Characterization
XRD
In-situ XRD
Physisorption

## Slide 7
Nanostructured materials: Ti-MCM-41
Pore-expanded titanium-containing mesoporous catalysts were directly synthesized under a microwave irradiation condition, using organic water-insoluble agent as a pore expander. Detailed synthetic procedure was carried out as follows:
CTAB (3.64 g) and a certain amount of SA were dissolved in 90 mL of deionized water under vigorous stirring at 313 K, and then TEOS (15.32 g) was added dropwise to the surfactant solution followed by an adjustment of pH value to 11.0 through gradual addition of a NaOH solution. After 10 min, TBOT (0.50 g) dissolved in i-PrOH was dropped into the mixture. The stirring was maintained for 40 min for the sufficient hydrolysis of TEOS and TBOT. Molar composition of final gel was 1:7.35:0.147:1.5:500:7.35 CTAB:TEOS:TBOT:NaOH:H2O:i-PrOH. The SA/CTAB molar ratio was 1. The resultant suspension was transferred into Teflon vessels and heated via nonpulsed microwave irradiation in a Multiwave 3000 microwave reaction system (Anton Paar) that is equipped with an 8-rotor tray. Combined with a temperature sensor, a pressure sensor, and an adjustable power output (maximum 1200 W), the microwave system provides an efficient way for rapid and uniform heating. Crystallization was performed in the temperature controlled mode where the temperature was ramped for 5 min and hold 393 K for 40 min. After cooling to room temperature, the solid products were isolated by filtering, washed with deionized water, and dried in air at 373 K for 12 h. Subsequently, the dried samples were calcined at 823 K for 6 h in air with a heating rate of 2 K/min.

## Slide 8
Nanostructured materials: Ti-MCM-41
Student | CTAB | H2O | TEOS | TBOT | 2-PrOH | NaOH 2.0M | SA
1 | 1.213 g | 27.5 mL | 5.43 mL | 0.167 mL | 1.82 mL | 2.5 mL | ----
2 | 1.213 g | 27.5 mL | 5.43 mL | 0.167 mL | 1.82 mL | 2.5 mL | n-heptane 0.488 mL
3 | 1.213 g | 27.5 mL | 5.43 mL | 0.167 mL | 1.82 mL | 2.5 mL | Dodecylamine 0.766 mL
In a 100 mL flask, mix CTAB and H2O and heat the system under stirring at 40°C
Add SA (if required) and let the system gently stirring overnight
Add TEOS dropwise and NaOH 2.0 M
After 10 min, add dropwise the solution of TBOT in 2-PrOH
Stir gently for 10 minutes
Transfer the gel into 2 Teflon vessel
Perform hydrothermal aging at 120°C for 40 minutes under microwave irradiation
Prepare the washing solution mixign 100 mL of H2O with 50 mL of EtOH
After cooling, wash the precipitate with 30 mL of the washing solution, shake for 30 sec and centrifuge (5000 rpm for 10 min) for 3 times + 1 final washign with 30 mL of EtOH
Dry the powder at 70 °C overnight
Grind the powder in a mortar and calcine at 550 °C for 6 h, heating rate 2 °C/min
Characterization
XRD – low angle
Physisorption
TEM