## Slide 1: EXAFS in a nutshell
E. Fonda
Synchrotron SOLEIL
Trieste Practicals
May 27th, 2026

## Slide 2
EXAFS: Extended X-ray Absorption Fine Structure
EXAFS
Extended X-ray Absorption Fine Structure
XANES
X-ray Absorption Near Edge Structure
pre-edge
Mn K-edge
µ : linear absorption coefficient
c : EXAFS signal
Electron Mean Free Path l(E)
XANES
EXAFS
e-

## Slide 3
A. Di Cicco, A. Filipponi, J. P. Itié and A. Polian, Phys. Rev. B 54 (1996) 9086-9098
High-pressure EXAFS of solid and liquid Kr
Liquid
Solid
Gas…
EXAFS explained in a single figure

## Slide 4
Absorber
Scatterer
R
As the wave travels, it’s shifted by absorber, scatterer and again absorber potentials.
It’s backscattered (angle= ) with effective amplitude f
Excitation
Propagation
Back scattering
Core orbital
Projection over core orbital
Photoelectron wavenumber:

## Slide 5
scillates with
Frequency = 2 R
Spherical wave
Polarization
EXAFS equation
Simplifies to 1 in the following
if anysotropy can be neglected

## Slide 6
1.95Å
2.00Å
2.05Å
scillates with
Frequency = 2 R
Spherical wave
Cu-O
1.95Å
2.00Å
2.05Å
k3
Fourier Transform

## Slide 7
Absorbing Atom
Scattering Atom
Different neighbors have different phases
and scattering amplitudes.
Higher Z higher |f| at higher |k| values
Absorber
Scatterer
R
Scatt.
Abs
Nuclei
Potential
R

## Slide 8
Pair distance distribution :
Picture of thermal motion, EXAFS depends on T
Damping term: « Debye Waller factor like»
Temperature effect

## Slide 9
Pair distance distribution :
Picture of thermal motion, EXAFS depends on T
Structural average + structural disorder
Damping term: « Debye Waller factor like»
Akaganeite

## Slide 10: Adding up more atoms
bcc Fe
8 Fe-Fe 2.45 Å
4 Fe-Fe 2.83 Å
12 Fe-Fe 3.97 Å
24 Fe-Fe 4.67 Å
k

## Slide 11: EXAFS examples: Fe bcc vs Fe in Goethite
8 Fe-Fe 2.45 Å
4 Fe-Fe 2.83 Å
12 Fe-Fe 3.97 Å
24 Fe-Fe 4.67 Å
3 Fe-O 1.96 Å
3 Fe-O 2.11 Å
2 Fe-Fe 3.02 Å
1 Fe-O 3.21 Å
2 Fe-Fe 3.31 Å
4 Fe-Fe 3.44 Å
Too high?
FT: a pseudo radial distribution representation

## Slide 12: Multiple scattering the bcc-Fe case
8 Fe-Fe 2.45 Å
4 Fe-Fe 2.83 Å
12 Fe-Fe 3.97 Å
24 Fe-Fe 4.67 Å
MS
SS
Several intense MS
paths are possible
In collinear geometry
FEFF 8
calculations
MS requires and provides
Geometrical information

## Slide 13
EXAFS take away messages
Information provided by EXAFS and advantages
Interatomic distances
Coordination numbers
Nature of atomic neighbors (for quite different Z)
Disorder/thermal effects via Debye Waller
It can be simulated via direct analytical methods
We can stop simulations to first coordination shell
Beamlines are getting better and better to provide high S/N
Many good simulation codes are freely available
Disadvantages
Signal is weak and thermal/structural disorders reduce it even more
Resolution depends on k space = length of EXAFS
Limited information versus complex structures in many cases

## Slide 14
1. Define E0
E0
2. Extrapolate pre-edge
up to E0 as a straight line
EXAFS data analysis in a nutshell
E0
3. Extrapolate post edge down to E0
4. Obtain edge jump at E0
5. Normalize by jump
Dmx(E0)
5. Fit a spline through
as EXAFS background

## Slide 15
EXAFS data analysis in a nutshell
EXAFS
5. Fit a spline through
as EXAFS background

## Slide 16
EXAFS data analysis in a nutshell
fcc-Cu
Radial distribution function contains too much information versus EXAFS.

## Slide 17
EXAFS data analysis in a nutshell
The Fourier transform helps in isolating a narrow set of frequencies, these correspond to limited information.
fcc-Cu
Nyquist Shannon Theorem applied to EXAFS
Simulating the EXAFS signal implies:
Making a structural hypothesis
Fit a number of parameters Npar<Nidp

## Slide 18
EXAFS data analysis in a nutshell
The Fourier transform helps in isolating a narrow set of frequencies, these correspond to limited information.
fcc-Cu
Very simplified model 
Simplified Theoretical Calculation
Fitting parameters

## Slide 19
EXAFS data analysis in a nutshell
The Fourier transform helps in isolating a narrow set of frequencies, these correspond to limited information.
fcc-Cu
Very simplified model 
Simplified Theoretical Calculation
Fitting parameters

## Slide 20
EXAFS data analysis in a nutshell
A two step procedure to model signal:
Create model
Model creation
Variate parameters to fit experiment
Get your simulation over the first shell range