## Slide 1: The Structure Factor
The diffracted wave from planes (hkl) is represented by the structure factor Fhkl
It is a complex number
Whose phase depends on the choice of the origin
Diffraction intensity
Ihkl = Fhkl·F*hkl = |Fhkl|2
F*hkl is the complex conjugate of Fhkl |F*hkl| = |Fhkl| f*hkl = - fhkl
The product of two complex numbers has a magnitude equal to the product of the magnitudes and a phase equal to the sum of the phases.
Fhkl
F*hkl

## Slide 2: Origin and phase in the Argand diagram
The origin is chosen by convention on a symmetry element

## Slide 3: Reflections with restricted phase
Centrosymmetric structures:
phase = 0 or 180°
Reflections from families of planes parallel to symmetry axes have
restricted phase. For example: h0l reflections in monoclinic system

## Slide 4: Systematic absences
Reflections from planes perpendicular to symmetry with half-translation of odd order have zero intensity: e.g. 0k0 with k=2n+1 in P21
Reflections from planes perpendicular to symmetry with half-translation of even order have high intensity: e.g. 0k0 with k=2n in P21

## Slide 5: Diffraction symmetry
In the monoclinic system, hkl reflections have the same structure factor as –hk-l reflections
hkl
-hk-l
In the orthorombic system Fhkl=Fh-k-l=F-hk-l=F-h-kl
In the tetragonal system the exchange of indices Fhkl=Fkhl is added
Diffraction symmetry in one of the 32 crystalline classes

## Slide 6: Friedel law
If the atomic species forming the crystal do not introduce a relative phase shift due to scattering (scattering factor without an imaginary component or crystals formed by a single element)
hkl
-h-k-l
|Fhkl|=|F-h-k-l| fhkl=-f-h-k-l F-h-k-l=F*hkl
Fhkl2=Fhkl*F*hkl = Ihkl Ihkl=I-h-k-l
Neglecting small phase differences due to anomalous scattering, a center of symmetry is always present in diffraction intensities.
Diffraction symmetry in the 11 Laue classes

## Slide 7: Scattering by an atom
q
The wave scattered at point p (identified by the vector r) by an infinitesimal volume element dv with electron density ρ(r) has:
amplitude r(r)dv (number of electrons in the infinitesimal volume dv)
phase ϕ relative to the origin O, which depends on the optical path difference t-q = r·so-r·s
where so and s are unit vectors in the directions of the incident and scattered beams.
The phase difference is equal to: 2p·r·(so-s)/λ.
By defining: r*=(so-s)/λ, the wave scattered from point p at scattering angle 2θ is: r(r)exp(2pir·r*)dv.
The total scattered wave from an atom is obtained by integrating over the entire atomic volume:
f(r*) = ∫vol.atom r(r)exp(2pir·r*)dv
o
p
so
s
r
1
2
t
2q

## Slide 8: Atomic Scattering Factor
f(r*)
r* = 2sen/λ [Å-1]
H
C
O
Fe
Be
Be2+
f(r*)
r* = 2sen/λ [Å-1]
The atomic scattering factor (form factor), f(r*) is the Fourier transform of the atom’s electron density, r(r)
Due to spherical symmetry: f(r*) = f(|r*|) with |r*| = |so-s|/λ = 2sen/λ
The scattering factor is function of 2sen/λ
For  = 0 all scattered waves of points p are in phase
f(0) = Z the number of electrons of the neutral atom
|so-s| = 2sen
so
s
so-s
q
q

## Slide 9: Scattering from the crystallographically independent unit (Result of the interference of the N interpenetrating lattices defined by N atoms not related by symmetry)
Scattering of atom 1 f1(r*) = f1exp(2pir1.r*)
where f1 is the atomic scattering of atom 1
Total scattering F(r*) = f1 + f2 + f3 + … fN
F(r*) = ∑ fj exp(2pirj.r*)
sum of j from 1 to N
r1
r2
r3
O
1
2
3
F
f1
f2
f3
f4
r real space of the cell with fractional coordinates x,y,z
r* reciprocal space with coordinate h,k,l
r*
r
hkl
xyx
dhkl
1/dhkl
r·r*= distance of point xyz from plane hkl/dhkl
2pr·r*=  phase of the wave scattered by point xyz
with respect to the plane hkl
r·r*= hx+ky+lz

## Slide 10: Structure Factor representation
F(h,k,l) = ∑j fj exp[2pi(hxj + kyj + lzj)]
Unit Cell
Electron Density
Reflection
F
(
h
,
k
,
l
)
=
V
r
(
x
,
y
,
z
).
exp[
2
p
i
(
hx
+
ky
+
lz
)]
z
=
0
1
ò
y
=
0
1
ò
x
=
0
1
ò
.
dxdydz
Argand Diagram
Each structure factor is the vector sum of the scattering from the individual atoms
F(hkl)
2pi(hxj+kyj+lzj)
fje
|F| intensity
F color
http://www.ysbl.york.ac.uk/~cowtan/fourier/fourier.html
FOURIER TRANSFORM
F(h,k,l) = |F(hkl)|exp[i(hkl)] = A(hkl) +iB(hkl)
|F(hkl)| amplitude and (hkl) phase

## Slide 11: Electron Density
Fourier synthesis: F  
(xyz) = (1/V)∑h ∑k ∑l |F(hkl)|exp[-2pi(hx+ky+lz)-(hkl)]
INVERSE FOURIER TRANSFORM OF STRUCTURE FACTORS
Fourier
Transform
DIRECT SPACE
RECIPROCAL SPACE
ELECTRON DENSITY
STRUCTURE FACTORS

## Slide 12: Phase Problem
Fourier
Transform
Diffraction
Image
|F|(cat),f(cat)
|F|(cat)
f(cat) ?

## Slide 13: Importance of phase and amplitude
Fourier
Transform
Fourier
Transform
|F|(duck),f(duck)
|F|(cat),f(cat)
Fourier
Transform
|F|(duck),f(cat)
Fourier
Transform
|F|(cat),f(duck)

## Slide 14
Fourier
Transform
DIRECT SPACE
RECIPROCAL SPACE
ELECTRON DENSITY
STRUCTURE FACTORS

## Slide 15: Patterson Function
A
B
C
“Structure”
“Patterson”
N atoms
N(N-1) interatomic vectors
X
Y
U
V
AB
AC
BC
P(xyz) = 1/V ∑h∑k∑l I(hkl) exp[-2pi(hx+ky+lz)]
The Patterson function is the Fourier transform of the diffraction intensity
The Patterson function can be calculated directly from the measured intensities without knowing the phase
The maxima of the Patterson function represent the map of interatomic vectors of the structure