## Slide 1: Patterson interpretation
Space group P212121
1 independent atom
4 atoms in cell
In the case of metal complexes, and more generally of crystals with atoms having many core electrons, the phase problem can be solved using the heavy-atom method by interpreting the Patterson function, whose maxima are dominated by the interatomic vectors between heavy atom and heavy atom
Resolution of the phase problem by the heavy-atom
Equivalent positions

## Slide 2: Theoretical Patterson
 | x,y,z | -x+1/2,-y,z+1/2 | -x,y+1/2,-z+1/2 | x+1/2,-y+1/2,-z
x,y,z | 0,0,0 | -2x+1/2,-2y,1/2 | -2x,1/2,-2z+1/2 | 1/2,-2y+1/2,-2z
-x+1/2,-y,z+1/2 | 2x-1/2,2y,-1/2 | 0,0,0 | -1/2,2y+1/2,-2z | 2x,1/2,-2z-1/2
-x,y+1/2,-z+1/2 | 2x,-1/2,2z-1/2 | 1/2,-2y-1/2,2z | 0,0,0 | 2x+1/2,-2y,-1/2
x+1/2,-y+1/2,-z | -1/2,2y-1/2,2z | -2x,-1/2,2z+1/2 | -2x-1/2,2y,1/2 | 0,0,0
Patterson map
If the number of heavy atoms to be located is small, the sites can be found directly using the Harker sections.

## Slide 3
Relationships between symmetrically related atoms produce peaks in the Patterson function on certain planes or along certain lines. Harker sections are portions of the Patterson map that contain a large proportion of the readily interpretable information because they contain many such Harker peaks (vectors between space-group equivalent atoms).
Harker sections
0.5, 0,25, 0.60
0.25, 0.5, 0.10
Harker peaks
1/2,-2y+1/2,-2z = 0.5, 0.25, 0.60
y = 0.125 z = -0.30 or y = -0.125 z = 0.30
2x,1/2,-2z-1/2 = 0.25, 0.5, 0.10
x = 0.125 z = -0.30 or x = -0.125 z = 0.30
x = 0.125 y = 0.125 z = -0.30 or
x = -0.125 y = -0.125 z = 0.30
Harker sections

## Slide 4
From the position of the heavy atom, its contribution to the structure factor (magnitude and phase) can be calculated
With the phases, electron density maps can be calculated, from which the other atoms of the structure can be located.
The new phases will be better than the previous ones, and the new map will be clearer. New atoms can be located.
Interactive cycles continue until the structure is completed.

## Slide 5: Anomalous dispersion
If fj is real, the Friedel law is always valid:
|F(hkl)| = |F(-h-k-l)| |F(hkl)|2 = I(hkl) = I(-h-k-l)
If fj has an imaginary component and crystal in not centrosymmetric, generally:
|F(hkl)| ≠ |F(-h-k-l)| and therefore I(hkl) ≠ I(-h-k-l)
Real
Imaginary
f0
Real
Imaginary
f0
Δf’
Δf”
When the wavelength is far from an element’s absorption edges (associated with electronic transitions), its atomic scattering factor can be treated as a real number.
When the X-ray energy is close to an electronic transition (i.e., near an absorption edge), the real part of the atomic scattering factor is modified by Δf′, while the imaginary component Δf′′ appears, affecting the phase of the scattering
fj = f0 + Δf’ + iΔf”

## Slide 6: From Friedel pairs to Bijvoet pairs
A
iB
FP(hkl)
FP(-h-k-l)
FH
FH
FPH(hkl)
f”
f’
FPH(-h-k-l)
In the presence of anomalous scattering, the model with coordinates xyz can be distinguished from the model -x-y-z
It is possible to determine the handedness of crystals and the absolute configuration of molecules.

## Slide 7
Absorption K-edge of Ni
Absorption edges
Nickel filters are used to selectively absorb Cu-Kβ
radiation

## Slide 8
The imaginary dispersion correction Δf”
is directly proportional to the linear attenuator coefficient µ.
Δf”(λ)= µ(λ)/2reλ
where re is the classical electron radius = 2.818 10−15
The real dispersion correction Δf’
can be obtained by Kramers-Kronig integral
where is Cauchy principal value of the
integral (singularity for λ=λ’)
Δf′(λ) ∼ “weighted average” of Δf”​(λ′)
Selenium scattering factor corrections
Scattering factor corrections

## Slide 9
Dispersion corrections of few elements for Cu Kα radiation

## Slide 10
Solution of the phase problem using direct methods
Phases from diffraction intensities through probabilistic relationships
It uses normalized structure factors (Ehkl) with respect to the mean value for reflections at same resolution <|F|2> corresponding to a random distribution of atoms in the unit cell
|Ehkl|2=|Fhkl|2/<|F|2>
Ehkl = SEh’k’l’Eh-h’k-k’l-l’
Electron density
Atomicity: concentrated in discrete atoms
Positivity: cannot be negative.
Identical Atoms: same chemical type
(xyz) and 2(xyz) are similar
The squaring method involves the self-convolution of the structure factors, leading to the Sayre equation

## Slide 11
Considering a small set of reflections to which a set of random phases is assigned, the phases are extended to all reflections in a manner consistent with the relations of the triplets (and other relationships, such as quadruplet, etc.)
φhkl ≈ φh’k’l’ + φh-h’k-k’l-l’
From Sayre's equation, considering triplets of strong reflections that dominate the summation, relations between the phases of these reflections are obtained:
Triplet relationships
The solution consistent with positive, localized electron density and chemically consistent molecular geometry is selected by figures of merit
|Fhkl|
|Fhkl|
φhkl
φhkl
random
phases
extended phases
by relationships
xyz
electron density
figure
of merit

## Slide 12: Triplet relationship
h-h’k-k’l-l’
hkl
h’k’l’
Ehkl = f; φhkl = 0
Eh’k’l’ = f; φh’k’l’=0 
Eh-h’k-k’l-l’ = f; φh-h’k-k’l-l’ =0

## Slide 13: Triplet relationship
h-h’k-k’l-l’
hkl
h’k’l’
Ehkl = f; φhkl = 0
Eh’k’l’ = f; φh’k’l’=π 
Eh-h’k-k’l-l’ = f; φh-h’k-k’l-l’ = π

## Slide 14
Solution of the phase problem via Patterson Function Superposition
“Patterson superposition”
x
O
y
x
O
y
B
“Structure”
A
C
y
x
N atoms
y
“Patterson”
CA
AB
x
O
AC
BA
BC
CB
N2 maxima
2N massimi

## Slide 15
Algorithm of SHELXT program
Patterson overlay and model building
Iterative cycles in reciprocal space using the space group P1 (Fourier transform and inverse Fourier transform)
modifying the electron density (masks to define the atoms,
randomly removing some peaks of electron density)
Selection of the solution using figures of merit
Determination of the origin position using the phases
Determination of the space group by testing possible solutions
Assignment of chemical elements to the electron densities
Isotropic refinement
Real Space
Reciprocal Space